Supplementary Material

Performance analysis of organolead perovskite solar cells in 2013-2018 using machine learning tools

Çağla Odabaşı-Özer and Ramazan Yıldırım*

S1  Database constructed and used for analysis

The database was constructed using 800 articles published in various journals from ACS, Elsevier, Wiley and RSC databases as well as Nature and Science in 2013 and 2018 (until May 31 of 2018), and 1921 experimental data from these articles were extracted. The articles were selected based on relevance search for “perovskite solar” as a topic; we tried to take the number of papers from each database as proportional to total publications as possible. Hence, the number of articles used in database is 10% of the articles according to Web of Science search (with the keyword search of “perovskite solar” in topic segment at 16.07.2018).  The detailed database of regular and inverted cells (considering stabilized efficiencies or not) were given in Excel Table.

The “na” sign in data points represents the absence of any information in related publication. For the variable of perovskite deposition step, two-step deposition was defined to generalize the all deposition methods where halide part (ie. PbI2) and cation part (MAI) were deposited seperately and perovskite form on the surface. One-step deposition was used for the perovskite deposition methods where the perovskite was formed first in a different place, then deposited on substrate. As considering the deposition methods, some abbreviations for vapor-assisted solution process and chemical vapor deposition were written as VASP and CVD, respectively. Spin 2-3 represents spin coating of perovskite two or three times repeatedly.  In the case of a variable was used 3 or less than 3 in a related column, we define this variable as others to simplify the database. The variables named as others were indicated in red color in databases.

For the perovskite type, in the case of perovskite contains more than one cation, it was called as mixed cation perovskite. The exact molecular formula of some of the mixed cations were not written in publications, we took the molecule content from experimental procedure of the corresponding article, and use directly to describe the molecule. However we combined them as the same variable when we are constucting the models. In the case of a one cation perovskite contains more than two halides, it was called as mixed halide perovskite. If a perovskite contains Sn and does not have any Pb, it was called Sn based perovskite.  One cation perovskites which have FA or Cs cation were called as FA or Cs based perovskites. In our database , we wrote the perovskite names with their atomic ratios in our Excel sheets if it was available in some publications, however, we used a general name for each type  (such as MAPbI3-xClx) in modelling and analyses.  The perovskites synthesized using lead (II) thiocyanate (Pb(SCN)2) as a precursor solution were named as “MAPb(SCN)xI3-x “,[1,2] on the other hand, in some other studies, Pb(SCN)2 was mentioned as a precursor solution additive;[3,4] hence we did not include it in the name of perovskite structure.

For stabilized and entire database of regular structure, in order to identify the mesoporous structures in ETL-2 (second layer of ETL), “m” was written at the beginning of the material names such as mAl2O3, mTiO2 etc. For determining the structures of nanorod(nr), nanowire(nw), nanocone(nc), nanoflower(nfl), nanoflake(nfl), nanocolumnar(ncl), nanosheet(ns), nanotubes(nt) and nanofiber(nf),  we named them as nanostructures (ns) (TiO2-ns, ZnO-ns etc. ) for generalization. For ETL (compact layer) and ETL-2, some variables were defined as “0” or “no”. “no” was used in the absence of entire ETL in the cell. On the other hand, “0” implies the absence of the related layer (one of ETL or ETL-2). For ETL, some most common materials were doped with various dopants to improve performance. Instead defining all these variables as a new variable, we gave a common name as TiO2-doped or ZnO-doped to simplify the database. For the other materials, the name of the material was used only in ETL or ETL-2 columns even they were doped or not, because we had less data points for other ETL materials (ZnO-doped was used for entire dataset modeling because we had enough data points for this variable, but it was named as ZnO for modelling of stabilized database.) Some common HTL additives were named as following: Lithium bis(trifluoromethylsulfonyl)-imide salt (Li), 4-tert-butylpyridine (TBP), Co(III) complexes such as tris(2-(1H-pyrazol-1-yl)pyridine)cobalt(III) (FK102), 106 tris(2-(1H-pyrazol-1-yl)-4-tert-butylpyridine) cobalt(III) tris-(bis(trifluoromethylsulfonyl)imide)) (FK209) and tris[2-(1H-pyrazol-1-yl)pyrimidine]cobalt(III) tris[bis(trifluoromethylsulfonyl)- imide] (MY11). In two articles, the exact structure of Co(II)TFSI was not indicated (as FK102, FK209 etc); hence we also used Co(II)TFSI for his material as in the articles.

For inverted cells, PEDOT:PSS and NiOx were separated as doped or undoped in HTL column. Similar to ETL structure in regular cells, for HTL and HTL-2, some variables were again defined as “0” or “no”. “no” was used in the absence of entire HTL in the cell. On the other hand, “0” implies the absence of the related (one of HTL or HTL-2) layer. Although we had data points using doped PTAA, we did not consider it as another variable to have enough data points. For the second layer of HTL, “m” was written at the beginning of the mesoporous materials similar . Similar to PTAA, data points with doped mNiOx were not indicated as “doped” due to lack of enough data points.

For the annealing conditions, one-step deposited MAPbI3 based perovskite cells were considered only. “MS” refers to multi-step annealing of perovskite in the column of annealing tempearture. “-“ indicates that no data was collected for this structure.

S2 Computational Details

S2.1 Random forest regression

The random forest regression model was built to test the predictability of power conversion efficiency; the root mean square error (RMSE) was used as the indicator of the prediction capacity of the model. Basically, random forest model is an ensemble method that creates multiple decision trees and predicts a new data point by the majority vote. The number of the trees was optimized by 5-fold cross validation. The dataset was divided into 5 equal parts and different number of trees were implemented for each fold. Then, the average RMSE value of each each tree number within each fold was listed, the tree number with the minimum average RMSE was considered in model. 110 and 30 trees were used for stabilized dataset of regular and inverted cells whereas 600 and 250 number of trees were generated for the entire dataset of regular and inverted cells.

S2.2 Association rule mining

Association rule mining is used to determine frequent combinations, patterns, rules and associations. There are three parameters that are used to interpret and make decision in this technique: support, confidence and lift. Support indicates the frequency of the occurance of two itemsets together. Confidence is the ratio of how much a specific item found in another specific item. Lift is the ratio of how much a specific item found in another specific item to the ratio of this specific item found in overall database, hence it shows if the occurance of a this item in another specific item is significant and more frequent. An example was given in manuscript to understand these terms better. The lift value was used for the detection of any patterns or rules in this part. Support value was adjusted as any condition should fulfill at least 5 data points. 5 data points may be slightly low but we wanted to extract any less common patterns as well. We had to decrease the support for this analysis in a way that the minimum number of data points required for the rule to be reliable from five to four due to the relatively smaller size of this database.  Confidence values were set to 0.1 to see the distributions of both frequent and less frequent items. The rule deduction was performed only for the highest efficiency class (above 18.0%) for each dataset since one usually seeks to know what to do to achieve high efficiency.

S2.3 Decision tree analysis

The decision tree analysis was performed by using rpart package in RStudio. Database was classified into three groups as high (A), intermediate (B) and low (C) efficiency groups for regular structure. In decision tree analysis, the database should be normally divided into certain number of approximately equal size classes to prevent the class imbalance problem may occur (even the small fraction of incorrectly classified data from large classes may reduce the accuracy rate of neighbouring small classes). If three equal size classes were created from our databases, the minimum level for the high efficiency class would be 16.5% for stabilized ; 14% for entire datasets of regular and inverted cells. However, in order to extract rules compatible with Section 3, the limits of the highest (18.0%) and the lowest (4.5 %) groups used in distribution plots and association rule mining in Section 4 were selected to represent Class A and Class C considering that one really prefer to know the rules and conditions for significantly high conversion such as 18.0%. However, the stabilized efficiency dataset is much smaller and the data are mostly located at higher efficiencies; there are only 5 data points at 4.5% and below for the regular cells, which is clearly not sufficient for the decision tree analysis (there are only 2 cases for inverted cells).  Hence, we had to change the limits of low (C) class from 4.5% to 9 % (also covering the second lowest parts in distribution analysis) for regular and inverted cells (number of data points for C classes increased to 25 for regular cells, which were sufficient). Even this change was not sufficient for the stabilized efficiency dataset for the inverted cells; consequently, we decided not to perform decision tree analysis for this set.

We had only 38 data points (111 data points in entire dataset) in Class A and 25 data points (411 data points in entire dataset) in Class C while the remaining 186 data points (885 data points in entire database) remained in class B in regular stabilized database; this is definitely a class imbalance situation (even the small fraction of incorrectly classified data from large classes may spoil and reduce the accuracy rate of neighboring small classes). In such situations, the data points in small classes are duplicated by random sampling until they reach the size of large sample if the number of data points in small sample is large enough to have a similar statistical distribution with its enlarged version. In regular cells, the number of data points in Class A and C are sufficiently large to apply random sampling; hence the data points in class A were replicated for 4.9 times to have 186 data points (8 times to have 888 data points in entire dataset) and data in class C for 7.4 times to have 185 data points (2.2 times to have 904 data points) to have a balanced class structure. Similarly, in the entire dataset of inverted case, the number of data points in Class A and Class C were 37 and 123, respectively and they were replicated for 9.6 and 2.9 times (355 and 356 data points were obtained for Class A and C, respectively).

Various values of the minimum number of split (the minimum number of data needed in each split to continue dividing into rules, otherwise tree grow stops), depth of the tree (maximum length of the branches) and complexity parameter (the measure of the minimum increase of R2 to model continue splitting, otherwise if new split does not increase overall R2 by at least complexity parameter, the model does not continue splitting), were tested with the class structure described above, and the decision tree structure representing the data best with the maximum prediction accuracy was determined.

The performance of the classification of decision tree model was evaluated using two measures. First, the overall classification accuracy of the model (ratio of correctly classified data points to the total number of data points in database) was considered. Second measure was the precision of each class. (ratio of the correctly classified data points which belonged to Class A to number of the data points predicted as Class A) Although the accuracy (ratio of the correctly classified data points which belonged to Class A to total data number of Class A) is also an important measure for classification, this measure was more important for us than accuracy of each class because we tried to get the purest branches and nodes to implement better rules. The most of the data predicted as Class A should be pure as much as possible. Hence, the model should not predict other classes as A.

As mentioned before, for the stabilized dataset of regular cells, the low efficiency upper limit was changed to 9% for decision tree modelling due to lack of enough data points below 4.5%. Hence, this case should be taken in account while interpreting the rules.

5 fold cross validation procedure was also employed to optimize the minimum number of split, depth of the tree and complexity paramater. Then, the parameters were fine-tuned to have a tree not only with the highest classification accuracy but also to with reasonable generalizable results in the terminal nodes.

S2.4 Logistic Curve modelling

The certified record efficiencies reported by NREL were modelled using S shaped logistic growth curve presented in Equation (1),

PCE(PCE)limit=11+ae-bt  		   (1)

(PCE)limit is the  upper limit of efficiency and assumed to be 27% (31 % could be also used without changing the result significantly), a and b are constant to be determined while t represent time as years.  The equation was linearized first as

ln⁡(1-PCEPCElimitPCEPCElimit)=lna-bt            (2)

Then, constants ln(a) and (b) were  determined frm  ln⁡(1-PCEPCElimitPCEPCElimit  versus time t plot as 848.35 and 0.4213 respectively with the R2 value of 0.98.

S3. Additional Results

S3.1. Comparison of stabilized efficiency dataset with entire database

As mentioned in computational details, the hysteresis was taking into consideration, and the stabilized efficiencies have been reported in some of the articles since 2014. The stabilized efficiencies are better measure of the real performance because they are usually lower than the initial efficiencies, which are directly computed from J-V curves. As the result, we also analysed the dataset containing only the data extracted from these article to see if there are significant differences in the patterns of this subset form the entire database. Figure S1 shows the change of average efficiencies computed from the entire database and stabilized efficiency subset for three cell structures through the years starting from 2015 to 2017.  The data belonging to these years were used in both dataset; 2014 excluded due to the insufficient number of stabilized efficiency data while 2018 was not taken because it is not yet completed. It should be also noted that the entire database also contained stabilized efficiencies because the other data points in the database do not necessarily have hysteresis; simple, they are not checked for that. Surprisingly, the averages of stabilized efficiencies are slightly higher than those for entire database for all three structures but they seem the follow exactly same trend with the entire dataset; the difference is slightly higher for the inverted cells in recent years.

Figure S1. Change in average efficiencies for three cell structure through years a) regular mesoporous b) regular planar c) inverted (blue symbols are overall average, red symbols are for stabilized efficiencies and orange symbols are for best cell efficiencies of the cells which the stabilized efficiencies were given)

To understand the differences between the stabilized efficiencies only and the entire database better, we also plot the distribution of data in two groups for all three cell designs. As seen in Figure S2, the distributions for the stabilized efficiencies are narrower and shifted to the higher efficiency sides with very small fractions (even none) in the very low efficiencies. Probably, these differences come from the fact that the experienced groups, whose initial efficiencies are also higher than the average, report the stabilized efficiencies more often. The analyses presented in Section 4 also seem to support this argument; the statistical fitness of the models developed by the stabilized efficiencies are also higher (indicating higher reproducibility) than the models from the entire database. Consequently, we built and presented our machine learning models derived from the stabilized efficiencies in Section 4 while occasionally comparing them with the models of entire dataset.

On the other hand, the stabilized efficiencies data are not sufficient to appreciate the progress in the field because it does not contain the works before 2014, and only partially cover the results reported since 2014. Considering that the papers in which the hysteresis is not checked, are also the valuable parts of the experience in the field, and the two datasets follow similar trends (see Figure S1 and association rule mining results in Section 4.2); we decided to use the entire database in the part of Section 3 for the review of progress.

Figure S2. Distribution (fractions) of efficiencies in database for three cell structures a) regular mesoporous b) regular planar c) inverted; blue columns show the distribution for entire dataset, red columns are for stabilized efficiencies only, green columns are best cell efficiencies of stabilized data points.

S3.2. Analysis of thermal annealing

Figure S3. Average efficiencies of MAPbI3 based cells (coated in one-step) for different thermal annealing conditions (a,b) mesoporous, (c,d) planar, (e,d) inverted cells

Fig. S4 Efficiencies values of cells annealed at high temperatures for short time; data obtained from four papers (Table S13)

S3.3. Results for random forest model

Figure S5 Actual versus predicted performances by random forest model for entire dataset of regular cells (a) training (RMSE=2.46) (b) testing (RMSE=3.56); for entire dataset of inverted cells (c) training (RMSE=2.26) (d) testing (RMSE=3.48)

S3.4. Result for association rule mining

In order to find the common rules leading high performance cells, association rule mining was implemented. Confidence value was taken as 0.1 in order to extract the most common and strongest rules leading high perfomance as well as to see the less common but still significant rules for high efficiency. The minimum support value was adjusted to 0.02 and 0.0035 for regular stabilized and regular cells which represents that at least 5 data points should have a rule in common. However, we detected very less rules when we limit to consider minimum 5 data points, hence we changed it as 4 data points to obtain more rules (the database of inverted cells contains less data points). Support value was adjusted to 0.05 and 0.008 for inverted stabilized and inverted cells.

Table S1 Association rule mining for PCE > 18% for regular cells; comparing the results for best efficiencies of stabilized and entire dataset

| (A)Antecedent: We are interested in this efficiency levels (classes) | (C)Consequent This feature was used in cells belonging to efficiency levels in A | (S)Support (%) This is fraction of all data belonging to class in A and has feature in B | (C)Confidence This fraction of data in A has feature in B | (L)Lift (This fraction of data in A has feature in B) / (This fraction of data in all data has feature in B |
| --- | --- | --- | --- | --- |
| PCE>18% for stabilized efficiency database with best cell efficiencies (Support= 0.02, Confidence=0.1) | ETL=TiO2-doped | 0.03 | 0.11 | 4.08 |
|  | Perovskite=mixed cation | 0.13 | 0.52 | 2.46 |
|  | Perovskite deposition method=spin 2-3 | 0.07 | 0.28 | 1.88 |
|  | Perovskite solution = DMF+DMSO | 0.14 | 0.56 | 1.83 |
|  | HTL additive= Li+TBP+FK209 | 0.03 | 0.13 | 1.72 |
|  | Antisolvent treatment= diethylether | 0.03 | 0.13 | 1.72 |
|  | Antisolvent treatment=chlorobenzene | 0.09 | 0.36 | 1.63 |
|  | ETL= SnO2 | 0.04 | 0.18 | 1.60 |
|  | HTL= spiro-OMeTAD | 0.22 | 0.92 | 1.13 |
|  | Perovskite deposition procedure = one-step | 0.20 | 0.80 | 1.12 |
|  | HTL additive= Li+TBP | 0.19 | 0.77 | 1.04 |
|  | ETL-2= 0 | 0.10 | 0.41 | 1.01 |
| PCE>18% for entire database with best cell efficiencies (Support= 0.0035, Confidence=0.1) | Perovskite=mixed cation | 0.04 | 0.51 | 5.20 |
|  | ETL= SnO2 | 0.01 | 0.17 | 4.82 |
|  | ETL-2= mTiO2-doped | 0.01 | 0.13 | 4.23 |
|  | Perovskite solution = DMF+DMSO | 0.05 | 0.60 | 3.84 |
|  | Antisolvent treatment= diethylether | 0.01 | 0.11 | 2.93 |
|  | Antisolvent treatment=chlorobenzene | 0.03 | 0.32 | 2.82 |
|  | HTL additive= Li+TBP+FK209 | 0.02 | 0.20 | 2.73 |
|  | Perovskite deposition method =spin 2-3 | 0.02 | 0.30 | 2.10 |
|  | Perovskite deposition procedure = one-step | 0.06 | 0.81 | 1.37 |
|  | HTL= spiro-OMeTAD | 0.07 | 0.89 | 1.25 |
|  | Perovskite deposition method =spin | 0.05 | 0.62 | 1.11 |
|  | ETL-2= 0 | 0.03 | 0.35 | 1.07 |
|  | HTL additive= Li+TBP | 0.05 | 0.68 | 1.07 |

Table S2 Association rule mining for PCE > 18% for inverted cells; comparing the results for best efficiencies of stabilized and entire dataset

| (A)Antecedent: We are interested in this efficiency levels (classes) | (C)Consequent This feature was used in cells belonging to efficiency levels in A | (S)Support (%) This is fraction of all data belonging to class in A and has feature in B | (C)Confidence This fraction of data in A has feature in B | (L)Lift (This fraction of data in A has feature in B) / (This fraction of data in all data has feature in B |
| --- | --- | --- | --- | --- |
| PCE>18% for stabilized efficiency database with best cell efficiencies (Support= 0.05, Confidence=0.1) | ETL= others | 0.05 | 0.24 | 2.49 |
|  | Perovskite=mixed cation | 0.07 | 0.29 | 2.18 |
|  | HTL= PTAA | 0.05 | 0.24 | 1.93 |
|  | ETL= PCBM+C60 | 0.05 | 0.24 | 1.45 |
|  | Perovskite solution = DMSO+GBL | 0.05 | 0.24 | 1.45 |
|  | Antisolvent treatment=toluene | 0.05 | 0.24 | 1.45 |
|  | Perovskite deposition method=spin 2-3 | 0.09 | 0.41 | 1.27 |
|  | ETL interlayer= BCP | 0.11 | 0.47 | 1.20 |
|  | Antisolvent treatment= chlorobenzene | 0.07 | 0.29 | 1.09 |
|  | HTL-2= 0 | 0.22 | 0.94 | 1.02 |
| PCE>18% for entire database with best cell efficiencies (Support= 0.008, Confidence=0.1) | HTL= PTAA | 0.01 | 0.19 | 5.72 |
|  | ETL=others | 0.02 | 0.22 | 3.59 |
|  | Perovskite=mixed cation | 0.02 | 0.22 | 3.47 |
|  | Perovskite solution = DMF+DMSO | 0.02 | 0.32 | 2.53 |
|  | HTL= others | 0.01 | 0.14 | 1.83 |
|  | Perovskite deposition method =spin 2-3 | 0.02 | 0.32 | 1.68 |
|  | ETL interlayer= BCP | 0.03 | 0.41 | 1.65 |
|  | ETL= PCBM+C60 | 0.01 | 0.16 | 1.57 |
|  | Antisolvent treatment= chlorobenzene | 0.02 | 0.22 | 1.52 |
|  | Perovskite solution = DMSO+GBL | 0.01 | 0.19 | 1.52 |
|  | HTL= NiOx | 0.01 | 0.19 | 1.52 |
|  | Antisolvent treatment= toluene | 0.02 | 0.22 | 1.37 |
|  | Perovskite deposition procedure= one-step | 0.06 | 0.81 | 1.02 |

S3.5. Result for decision tree analysis

The minimum split number, maximum depth and complexity parameter were adjusted using 5-fold cross validation. However, in order to get a more detailed data, we also changed these values slightly to get more information from the database. The final values for minimum number of split, depth of tree and complexity parameters for each tree generated from different dataset were shown in Table S3.

Table S3 Optimized parameters in decision tree analysis

| Database used | Minimum split number | Maximum depth | Complexity parameter |
| --- | --- | --- | --- |
| Regular stabilized | 10 | 5 | 0 |
| Regular | 10 | 6 | 0 |
| Inverted | 30 | 5 | 0 |

The confusion matrix of the decision tree model for stabilized regular cells was given in Table S5. The columns show the actual data and rows show the predictions. The data in the diagonals (bold) are correctly classified data points. The accuracy of the tree was calculated by dividing the correctly classified data points to total number of data points.   173+134+154557x100, for regular stabilized database In order to calculate precision of Class A, the correctly classified data points should be divided into the number of total data points that predicted as A. The precision of Class A was found to be 87%   173173+26+0x100. In order to calculate the accuracy of class A, the number of correctly classified A should be divided into total data points of A and the accuracy was found to be 93%  173173+13+0x100. Similary, accuracy and precision for other classes were also calculated and given in Table S5. The optimization for both Class A and Class C at the same time was considered because they were the target classes for our model building besides overall accuracy.

Table S4 Confusion matrix of regular stabilized dataset

|  |  | Actual Class |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Class A | Class B | Class C | Precision |
| Predicted Class | Class A | 173 | 26 | 0 | 87% |
|  | Class B | 13 | 134 | 31 | 75% |
|  | Class C | 0 | 26 | 154 | 86% |
|  | Accuracy | 93% | 72% | 83% |  |
| Overall accuracy |  |  | 83% |  |  |

Figure S6. Decision tree model of entire regular type cells

Table S5 Confusion matrix of regular entire dataset

|  |  | Actual Class |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Class A | Class B | Class C | Precision |
| Predicted Class | Class A | 791 | 106 | 17 | 87% |
|  | Class B | 97 | 672 | 383 | 58% |
|  | Class C | 0 | 107 | 504 | 82% |
|  | Accuracy | 89% | 76% | 56% |  |
| Overall accuracy |  |  | 73% |  |  |

Figure S7. Decision tree model of entire dataset of inverted cells

Table S6 Confusion matrix of inverted entire dataset

|  |  | Actual Class |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Class A | Class B | Class C | Precision |
|  | Class A | 318 | 56 | 3 | 84% |
|  | Class B | 23 | 169 | 39 | 73% |
|  | Class C | 14 | 129 | 314 | 69% |
|  | Accuracy | 90% | 48% | 88% |  |
| Overall accuracy |  |  | 75% |  |  |

S4. Perovskite solar cells database

Table S7. Stabilized efficiencies of regular cells

| Article | Year | ETL | ETL-2 | Perovskite | Perovskite deposition procedure | Perovskite deposition method | Anti-solvent treatment | Precursor solution | Annealing temperature (°C) | Annealing time (minutes) | Annealing ambience | HTL | HTL additive | PCEstabilized (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Abate, A. et al., Nano Lett. 14, 3247–3254 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 15.2 |
| Guo, Y. et al., J. Mater. Chem. A 2, 13827–13830 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 95 | glovebox | P3HT | Li+D-TBP | 10.8 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 16411–16419 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | no | no | 5.15 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 16411–16419 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | no | no | 10.5 |
| Huang, F. et al., Nano Energy 10, 10–18 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.5 |
| Noel, N. K. et al., ACS Nano 8, 9815–9821 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.5 |
| Noel, N. K. et al., ACS Nano 8, 9815–9821 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 14.1 |
| Noel, N. K. et al., ACS Nano 8, 9815–9821 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 8.3 |
| Xiao, M. et al., Angew. Chemie 126, 10056–10061 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 13 |
| Ahn, N. et al., J. Am. Chem. Soc. 137, 8696–8699 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 18.7 |
| Bu, L. et al., ACS Appl. Mater. Interfaces 7, 17776–17781 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.4 |
| Cai, B. et al., Cuihua Xuebao/Chinese J. Catal. 36, 1183–1190 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 14.4 |
| Das, S. et al., ACS Photonics 2, 680–686 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spray | no | DMF | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 11 |
| Della Gaspera, E. et al., Nano Energy 13, 249–257 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 12.9 |
| Hou, Y. et al., Adv. Energy Mater. 5, 1500543 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | ambient | PEDOT | no | 7.2 |
| Hou, Y. et al., Adv. Energy Mater. 5, 1500543 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 11.9 |
| Hwang, I. et al., ACS Appl. Mater. Interfaces 7, 17330–17336 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.2 |
| Hwang, I. et al., ACS Appl. Mater. Interfaces 7, 17330–17336 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.7 |
| Jeon, N. J. et al., Nature 517, 476–480 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PTAA | Li+TBP | 18.5 |
| Jeong, I. et al., Nano Energy 17, 131–139 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15 |
| Lee, J. W. et al., Adv. Energy Mater. 5, 1501310 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 11.5 |
| Lee, J. W. et al., Adv. Energy Mater. 5, 1501310 (2015) | 2015 | TiO2 | 0 | FA0.9Cs0.1PbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 13.6 |
| Li, W. et al., J. Am. Chem. Soc. 137, 10399–10405 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16 |
| Li, Y. et al., J. Am. Chem. Soc. 137, 15540–15547 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.58 |
| Li, Y. et al., J. Am. Chem. Soc. 137, 15540–15547 (2015) | 2015 | TiO2 | PCBB-2CN-2C8 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.81 |
| Liu, J. et al., J. Phys. Chem. Lett. 6, 1666–1673 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | PEDOT | no | 6.6 |
| Liu, J. et al., J. Phys. Chem. Lett. 6, 1666–1673 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 9.4 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | RGO-1 | no | 9.48 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | RGO-2 | no | 8.12 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | RGO-3 | no | 7.21 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | GO | no | 5.63 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 5.72 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.01 |
| Sepalage, G. A. et al., Adv. Funct. Mater. 25, 5650–5661 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | CuI | no | 7.6 |
| Wang, Z. et al., Chem. Mater. 27, 7149–7155 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 + FACl | one-step | spin | no | DMF+FACl | 140 | na | na | spiro-OMeTAD | Li+TBP | 12.7 |
| Wang, F. et al., Adv. Funct. Mater. 25, 1120–1126 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 4.1 |
| Wang, F. et al., Adv. Funct. Mater. 25, 1120–1126 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+HCl | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 13.6 |
| Wang, F. et al., Adv. Funct. Mater. 25, 1120–1126 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+HI | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 10 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | C60 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 12.7 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 10.9 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | C60 | 0 | MAPbI3-xClx | two-step | evap-spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.9 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | evap-spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.1 |
| Wozny, S. et al., Chem. Mater. 27, 4814–4820 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | toluene | DMF | 170 | 10 | dry air | spiro-OMeTAD | Li+TBP | 16.4 |
| Xia, X. et al., ACS Appl. Mater. Interfaces 7, 16907–16912 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Yang, Z. et al., Nano Energy 15, 670–678 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-contact | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.7 |
| Yang, D. et al.,Energy Environ. Sci. 8, 3208–3214 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15.73 |
| You, P. et al., Adv. Mater. 27, 3632–3638 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 15.1 |
| Zhang, T. et al., Nano Lett. 15, 3959–3963 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.9 |
| Zhang, M. et al., Chem. Commun. 51, 10038–10041 (2015) | 2015 | TiO2 | 0 | MAPbBr3 | one-step | blowdry | no | DMF | 100 | 10 | ambient | P3HT | no | 9.7 |
| Zheng, Y. C. et al., Chem. Mater. 27, 5116–5121 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | spiro-OMeTAD | Li+TBP | 12.9 |
| Bai, Y. et al., ChemSusChem 9, 2686–2691 (2016) | 2016 | SnO2-Sb | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 17.6 |
| Chen, H. N. et al., Adv. Energy Mater. 6, 1502087 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+CYHEX | - | - | - | no | no | 13.75 |
| Chen, X. et al., J. Mater. Chem. A 4, 6521–6526 (2016) | 2016 | TiO2 | TiO2 flower like | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Cheng, N. et al., J. Power Sources 321, 71–75 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 10.9 |
| Chiang, Y.-H. et al., ChemSusChem 9, 2620–2627 (2016) | 2016 | TiO2 | mTiO2 | MAPb(SCN)xI3-x | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.1 |
| Fei, C. et al., Nano Energy 27, 17–26 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | one-step | spin | ethylacetate | DMF | 100 | 90 | na | spiro-OMeTAD | Li+TBP | 16.54 |
| Heo, J. H. and Im, S. H., Nanoscale 8, 2554–2560 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+HI | 100 | 2 | ambient | PTAA | Li+TBP | 18.7 |
| Huang, H. et al., Nano Energy 27, 352–358 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spray | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.4 |
| Jiang, X. et al., J. Phys. Chem. Lett. 7, 4142–4146 (2016) | 2016 | 0 | mTiO2 | (5-AVA)x(MA)1-xPbI3 | one-step | spin | no | GBL | 50 | na | na | no | no | 13.09 |
| Jiang, X. et al., J. Phys. Chem. Lett. 7, 4142–4146 (2016) | 2016 | TiO2 | mTiO2 | (5-AVA)x(MA)1-xPbI3 | one-step | spin | no | GBL | 50 | na | na | no | no | 13.4 |
| Ke, W. et al., Adv. Mater. 28, 5214–5221 (2016) | 2016 | SnO2 | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.57 |
| Ke, W. et al., Adv. Mater. 28, 5214–5221 (2016) | 2016 | SnO2 | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO+Pb(SCN)2 | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 18.42 |
| Ke, W. et al., J. Mater. Chem. A 4, 14276–14283 (2016) | 2016 | SnO2 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 15.51 |
| Ke, W. et al., J. Mater. Chem. A 4, 14276–14283 (2016) | 2016 | SnO2 | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 17.75 |
| Kim, J. et al., J. Phys. Chem. C 120, 11262–11267 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+HI | 160 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 13 |
| Lee, S. J. et al., J. Am. Chem. Soc. 138, 3974–3977 (2016) | 2016 | TiO2 | mTiO2 | FASnI3 | one-step | spin 2-3 | toluene | DMF+DMSO+SnF2+pyrazine | 60 | 60 | glovebox | spiro-OMeTAD | lutidiene+TBP | 4 |
| Lee, J. W. et al., Acc. Chem. Res. 49, 311–319 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 11.5 |
| Lee, J. W. et al., Acc. Chem. Res. 49, 311–319 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO+thiourea | MS | na | na | spiro-OMeTAD | Li+TBP | 13.6 |
| Li, J. et al., Nanoscale 8, 14163–14170 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 10.33 |
| Li, J. et al., Nanoscale 8, 14163–14170 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 9.38 |
| Liu, L. et al., Electrochim. Acta 222, 933–937 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| McMeekin, D. P. et al., Science 351, 151–5 (2016) | 2016 | SnO2 | PCBM | FA0.83Cs0.17Pb(I0.6Br0.4)3 | one-step | spin | no | DMF | 185 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 16 |
| Niu, G. et al., Nano Energy 27, 87–94 (2016) | 2016 | TiO2 | mTiO2 | (MAPbI3)0.9(CsPbBr3)0.1 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | MS | na | na | spiro-OMeTAD | Li+TBP | 15.7 |
| Pearson, A. J. et al., Adv. Energy Mater. 6, 1600014 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | ambient | spiro-OMeTAD | Li+TBP | 9.36 |
| Saliba, M. et al., Energy Environ. Sci. 9, 1989–1997 (2016) | 2016 | TiO2 | mTiO2-Li | Cs5(MA0.17FA0.83)95Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 21.1 |
| Saliba, M. et al., Science 354, 206–209 (2016) | 2016 | TiO2 | mTiO2 | Rb/Cs/MA/FA | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 21.6 |
| Sedighi, R. et al., ChemPhysChem 17, 2382–2388 (2016) | 2016 | TiO2 | mTiO2 | CH3NH3PbI3-xBrx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.85 |
| Sedighi, R. et al., ChemPhysChem 17, 2382–2388 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.02 |
| Sedighi, R. et al., ChemPhysChem 17, 2382–2388 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.37 |
| Shaikh, S. F. et al., J. Mater. Chem. A 4, 15478–15485 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 2 | na | spiro-OMeTAD | Li+TBP | 14.9 |
| Shin, S. S. et al., J. Phys. Chem. Lett. 7, 1845–1851 (2016) | 2016 | Zn2SnO4 | 0 | MAPbI3 | two-step | spin | toluene | DMF | - | - | - | PTAA | no | 17 |
| Song, J. et al., J. Mater. Chem. A 4, 8435–8443 (2016) | 2016 | cZnO | 0 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.7 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | no | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 0.5 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | PEIE | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 4.3 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | 0 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 1.95 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 9 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | PEIE | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 13 |
| Tai, Q. et al., Nat. Commun. 7, 11105 (2016) | 2016 | TiO2 | mTiO2 | MAPb(SCN)xI3-x | two-step | spin | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 14.2 |
| Wang, F. et al., Adv. Mater. 28, 9986–9992 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 19 |
| Wei, J. et al., Nano Energy 26, 139–147 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+PCBM+PEG | MS | na | na | spiro-OMeTAD | Li+TBP | 14 |
| Wu, W. Q. et al., J. Power Sources 329, 17–22 (2016) | 2016 | 0 | cTiO2-nanowire | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14 |
| Yoon, H. et al., Energy Environ. Sci. 9, 2262–2266 (2016) | 2016 | BCP | C60 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 17.8 |
| Yu, X. et al., J. Power Sources 325, 534–540 (2016) | 2016 | TiO2 | mSiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | spiro-OMeTAD | no | 15.8 |
| Yu, Y. et al., ChemSusChem 9, 3288–3297 (2016) | 2016 | SnO2 | C60-SAM | FAPbI3 | one-step | spin | no | DMF+DMSO | 150 | 10 | na | spiro-OMeTAD | Li+TBP | 10.56 |
| Yu, Y. et al., ChemSusChem 9, 3288–3297 (2016) | 2016 | SnO2 | C60-SAM | FA0.8Cs0.2PbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14.67 |
| Yu, Y. et al., ChemSusChem 9, 3288–3297 (2016) | 2016 | SnO2 | C60-SAM | FA0.8Cs0.2PbI3 | one-step | spin | no | DMF+DMSO+Pb(SCN)2 | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.65 |
| Yuan, S. et al., RSC Adv. 6, 47459–47467 (2016) | 2016 | TiO2 | PCBM | MAPbI3 | two-step | vasp | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15 |
| Zhang, Y. et al., Chem. Commun. 52, 5674–5677 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+s-CNT | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 13.9 |
| Zhang, F. et al., Chem. Mater. 28, 802–812 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 9.3 |
| Zhang, F. et al., Chem. Mater. 28, 802–812 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 8.9 |
| Zhang, H. et al., J. Mater. Chem. A 4, 8724–8733 (2016) | 2016 | PDI | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 17.13 |
| Zhou, Z. et al., RSC Adv. 6, 78585–78594 (2016) | 2016 | TiO2 | C60 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.908 |
| Zuo, L. et al., J. Am. Chem. Soc. 138, 15710–15716 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.09 |
| Zuo, L. et al., J. Am. Chem. Soc. 138, 15710–15716 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.75 |
| Cai, F. et al., J. Mater. Chem. A 5, 9402–9411 (2017) | 2017 | TiO2-TOPD | C60-ETA | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 18 |
| Cai, F. et al., J. Mater. Chem. A 5, 9402–9411 (2017) | 2017 | TiO2-TOPD | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 20.1 |
| Chen, M. et al., Chem. Eng. J. 313, 791–800 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-drip | no | DMF | - | - | - | no | no | 6.78 |
| Chen, Z. et al., J. Power Sources 351, 123–129 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.7 |
| Chen, C. et al., ACS Energy Letters 2, 497–503 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP+Cu(bpcm) | 17.9 |
| Chen, J. Y. et al., Sol. Energy Mater. Sol. Cells 164, 47–55 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 13.746 |
| Cheng, N. et al., Electrochim. Acta 246, 990–996 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | ethanol | DMF | - | - | - | CuPc | no | 16 |
| Cimaroli, A. J. et al., J. Mater. Chem. C 5, 10152–10157 (2017) | 2017 | C60-SAM | 0 | MA0.7FA0.3PbI3 | one-step | spin | diethyl ether | DMF+DMSO+Pb(SCN)2 | MS | na | ambient | spiro-OMeTAD | Li+TBP | 11.8 |
| Conings, B. et al., ACS Appl. Mater. Interfaces 9, 8092–8099 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 16.9 |
| Conings, B. et al., ACS Appl. Mater. Interfaces 9, 8092–8099 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 6.2 |
| Ding, B. et al., J. Mater. Chem. A 5, 6840–6848 (2017) | 2017 | TiO2 | 0 | FA0.1MA0.9PbI3 | one-step | spin | no | DMF | 120 | 20 | na | spiro-OMeTAD | Li+TBP | 20.24 |
| Dong, Q. et al., Nano Energy 38, 358–367 (2017) | 2017 | SnO2 | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.14 |
| Dong, Q. et al., Nano Energy 38, 358–367 (2017) | 2017 | no | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 12.08 |
| Dong, Q. et al., Nano Energy 38, 358–367 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 14.8 |
| Eze, V. O. et al., Org. Electron. physics, Mater. Appl. 46, 253–262 (2017) | 2017 | Wox | 0 | MAPbI3 | one-step | spin | no | GBL+NMP | na | na | na | spiro-OMeTAD | Li+TBP | 10.98 |
| Eze, V. O. et al., Org. Electron. physics, Mater. Appl. 46, 253–262 (2017) | 2017 | Wox | C60 | MAPbI3 | one-step | spin | no | GBL+NMP | na | na | na | spiro-OMeTAD | Li+TBP | 15.02 |
| Fan, R. et al., J. Mater. Chem. A 5, 12034–12042 (2017) | 2017 | TiO2 | 0 | FAI,MAI,MACl,MABr,PbI2 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.5 |
| Fan, R. et al., J. Mater. Chem. A 5, 12034–12042 (2017) | 2017 | TiO2 | Au@TiO2-nanorod | FAI,MAI,MACl,MABr,PbI2 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.5 |
| Fei, C. et al., Adv. Energy Mater. 7, 1602017 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 90 | 30 | na | spiro-OMeTAD | Li+TBP | 14.3 |
| Fei, C. et al., Adv. Energy Mater. 7, 1602017 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | ethylacetate | DMF+thiourea | 90 | 30 | na | spiro-OMeTAD | Li+TBP | 18.05 |
| Fei, C. et al., Adv. Energy Mater. 7, 1602017 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+thiourea | 90 | 30 | na | spiro-OMeTAD | Li+TBP | 11.32 |
| Gao, X. et al., Phys. Chem. Chem. Phys. 19, 4956–4961 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.1 |
| Gao, X. et al., Phys. Chem. Chem. Phys. 19, 4956–4961 (2017) | 2017 | TiO2 | TiO2-nanotube | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.1 |
| Gao, L.-L. et al., J. Mater. Chem. A 5, 1548–1557 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin-MAK | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 16.44 |
| Gao, C. et al., Chem. Eng. J. 325, 378–385 (2017) | 2017 | cZnO | ZnO-SnO2-ndt | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 60 | na | P3HT | no | 12.1 |
| Guo, Y. et al., Nano Energy 38, 193–200 (2017) | 2017 | Ni-Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 11.6 |
| Guo, Y. et al., Nano Energy 38, 193–200 (2017) | 2017 | Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 9.2 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | 0 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-PMMA | no | 6.5 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-PMMA | no | 5 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-PMMA | TBP | 14.2 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-polycarbonate | TBP | 13.5 |
| Han, F. et al., J. Power Sources 359, 577–584 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14.05 |
| Han, F. et al., J. Power Sources 359, 577–584 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+4MSA | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.72 |
| Han, F. et al., Electrochim. Acta 236, 122–130 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 16.78 |
| Han, F. et al., Electrochim. Acta 236, 122–130 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 14.37 |
| Han, F. et al., Appl. Surf. Sci. 408, 34–37 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | na | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.35 |
| Han, F. et al., Appl. Surf. Sci. 408, 34–37 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | DMSO-CB | na | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.42 |
| He, M. et al., Nat. Commun. 8, 16045 (2017) | 2017 | TiO2 | 0 | FA0.85MA0.15PbI2.55Br0.45 | one-step | MASP | no | DMSO | MS | na | na | PTAA | Li+TBP | 19.9 |
| Hou, Y. et al., Adv. Funct. Mater. 27, 1700878 (2017) | 2017 | TiO2-SnO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.48 |
| Hou, Y. et al., Adv. Funct. Mater. 27, 1700878 (2017) | 2017 | TiO2-SnO2 | 0 | Cs5(MA0.17FA0.83)95Pb(I0.83Br0.17)3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.08 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.3 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | In2S3 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.4 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 6.37 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | α‐Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 10.78 |
| Huckaba, A. J. et al., Small Methods 1, 1700250 (2017) | 2017 | TiO2 | mTiO2-Li | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | TiS2 | no | 12.34 |
| Jiang, X. et al., Sci. Rep. 7, 42564 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | PEDOT | no | 14.6 |
| Jiang, J. et al., J. Mater. Chem. A 5, 9514–9522 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 16.98 |
| Jiang, J. et al., J. Mater. Chem. A 5, 9514–9522 (2017) | 2017 | TiO2 | ITIC | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 19.86 |
| Jin, J. et al., ACS Appl. Mater. Interfaces 9, acsami.7b15310 (2017) | 2017 | TiO2 | 0 | MAI(PbI2)0.97(ZnCl2)0.03 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 18 |
| Jin, J. et al., ACS Appl. Mater. Interfaces 9, acsami.7b15310 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 16.1 |
| Jodlowski, A. D. et al., Nat. Energy 2, 972–979 (2017) | 2017 | TiO2 | mTiO2-Li | MA1–x GuaxPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 45 | na | spiro-OMeTAD | Li+TBP+Co(II)TFSI | 19.21 |
| Ke, W. et al., Sci. Adv. 3, e1701293 (2017) | 2017 | TiO2 | mTiO2 | en-FASnI3 | one-step | spin | no | DMF+DMSO | 120 | 10 | na | PTAA | no | 6.65 |
| Kim, D. H. et al., Adv. Mater. 29, 1606831 (2017) | 2017 | TiO2 | 0 | FA0.6MA0.4PbI(3-y)Cly | one-step | spin 2-3 | diethyl ether | DMF | 130 | 10 | na | spiro-OMeTAD | Li+TBP+FK102 | 19 |
| Kim, D. H. et al., Adv. Mater. 29, 1606831 (2017) | 2017 | TiO2 | 0 | FA0.6MA0.4PbI(3-y)Cly | one-step | spin 2-3 | diethyl ether | DMSO+GBL | 130 | 10 | na | spiro-OMeTAD | Li+TBP+FK102 | 13.4 |
| Lee, W. et al., Org. Electron. 51, 404–409 (2017) | 2017 | 0 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 12.6 |
| Lee, W. et al., Org. Electron. 51, 404–409 (2017) | 2017 | PEIE-LiQ | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Liu, Z. et al., J. Mater. Chem. A 5, 6597–6605 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | NiOx | no | 15.66 |
| Long, M. et al., Adv. Energy Mater. 7, 1601882 (2017) | 2017 | TiO2 | 0 | FAPbI3-xBrx | one-step | spin | no | DMF | 160 | 60 | na | spiro-OMeTAD | Li+TBP | 18.5 |
| Lu, J. et al., Adv. Energy Mater. 7, 1700444 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 16.5 |
| Lu, J. et al., Adv. Energy Mater. 7, 1700444 (2017) | 2017 | TiO2 | 0 | MA1-2xEDAxPbI3 | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 18.1 |
| Lu, H. et al., Small 13, 1701535 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 105 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 16.5 |
| Luo, Q. et al., Adv. Funct. Mater. 27, 1702090 (2017) | 2017 | α‐Fe2O3 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 25 | glovebox | spiro-OMeTAD | Li+TBP | 11.1 |
| Luo, Q. et al., Adv. Funct. Mater. 27, 1702090 (2017) | 2017 | α‐Fe2O3 | m-α‐Fe2O3 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 25 | glovebox | spiro-OMeTAD | Li+TBP | 17.4 |
| Mahmud, M. A. et al., Phys. Chem. Chem. Phys. 19, 21033–21045 (2017) | 2017 | cZnO | 0 | MA0.6FA0.4PbI3 | one-step | spin | no | DMF | 100 | 10 | na | FDT | Li+TBP | 11.87 |
| Mahmud, M. A. et al., Phys. Chem. Chem. Phys. 19, 21033–21045 (2017) | 2017 | cZnO | 0 | MA0.6FA0.4PbI3 | one-step | spin | no | DMF | 100 | 10 | na | FDT | F4TCNQ | 13.33 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 14 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanoflower | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 15.2 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 14.6 |
| Mu, C. et al., Adv. Energy Mater. 7, 1601297 (2017) | 2017 | TiO2 | 0 | FAPbI2.8Cl0.2 | one-step | spin | no | DMF | 100 | 50 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 16.5 |
| Mu, C. et al., Adv. Energy Mater. 7, 1601297 (2017) | 2017 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | 100 | 50 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 15 |
| Nia, N. Y. et al., ChemSusChem 10, 3854–3860 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | Li+TBP | 14.7 |
| Nia, N. Y. et al., ChemSusChem 10, 3854–3860 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.4 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.5 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.9 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.5 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.1 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.4 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 19.3 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.4 |
| Pham, N. D. et al., J. Mater. Chem. A 5, 5195–5203 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 16.2 |
| Pham, N. D. et al., J. Mater. Chem. A 5, 5195–5203 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 17.5 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | FAPbI2.85Br0.15 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16.8 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | FAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16.7 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | Cs0.1FA0.9MA0.34PbI2.865Br0.135 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 18.9 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | Cs0.2FA0.8PbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.4 |
| Qiu, L. et al., J. Phys. Chem. B 122, acs.jpcb.7b03921 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 60 | dry air | spiro-OMeTAD | Li+TBP | 16.4 |
| Ren, Y. K. et al., J. Alloys Compd. 705, 205–210 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 14.8 |
| Sanehira, E. M. et al., Sci. Adv. 3, eaao4204 (2017) | 2017 | TiO2 | 0 | CsPbI3 QD | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 6.1 |
| Sanehira, E. M. et al., Sci. Adv. 3, eaao4204 (2017) | 2017 | TiO2 | 0 | FA-CsPbI3 QD | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 13.43 |
| Sin, D. H. et al., ACS Appl. Mater. Interfaces 9, 18103–18112 (2017) | 2017 | cZnO-PEG | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.1 |
| Sun, M. et al., J. Mater. Chem. A 5, 13448–13456 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 15.6 |
| Sun, M. et al., J. Mater. Chem. A 5, 13448–13456 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO+2-pyridylthiourea | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 18.2 |
| Wang, L.-Y. et al., Nanoscale 9, 17893–17901 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | di-isopropyl ether | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.81 |
| Wang, Z. et al., Nat. Energy 2, 17135 (2017) | 2017 | SnO2 | PCBM-N-DPBI | BA0.05(FA0.83Cs0.17)0.95Pb(I0.8Br0.2)3 | one-step | spin | no | DMF+HI+HBr | 175 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 19.5 |
| Wang, Z. et al., Nat. Energy 2, 17135 (2017) | 2017 | SnO2 | PCBM-N-DPBI | BA0.09(FA0.83Cs0.17)0.91Pb(I0.6Br0.4)3 | one-step | spin | no | DMF+HI+HBr | 175 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 17.3 |
| Wang, Z. et al., Nat. Energy 2, 17135 (2017) | 2017 | SnO2 | PCBM-N-DPBI | FA0.83Cs0.17Pb(I0.6Br0.4)3 | one-step | spin | no | DMF+HI+HBr | 175 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Wang, Z. et al., Adv. Mater. 29, 1604186 (2017) | 2017 | C60-N-DPBI | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 17.9 |
| Wang, Z. et al., Adv. Mater. 29, 1604186 (2017) | 2017 | C60 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 16.2 |
| Wang, H. et al., ACS Appl. Mater. Interfaces 9, 21756–21762 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | no | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 16.12 |
| Wu, T. et al., J. Power Sources 365, 1–6 (2017) | 2017 | TiO2 | 0 | Cs0.05(MA0.17FA0.83)0.95Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO+NMP | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 18.6 |
| Yang, G. et al., J. Mater. Chem. A 5, 1658–1666 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO+Pb(SCN)2 | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.54 |
| Yang, G. et al., Small 13, 1601769 (2017) | 2017 | SnO2-Y | 0 | MAPbI3 | one-step | spin 2-3 | diethyl ether | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 16.25 |
| Yang, G. et al., Small 13, 1601769 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin 2-3 | diethyl ether | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 12.23 |
| Yu, Y. et al., ACS Appl. Mater. Interfaces 9, 23624–23634 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | na | dry air | spiro-OMeTAD | Li+TBP | 13.69 |
| Yu, Y. et al., ACS Appl. Mater. Interfaces 9, 23624–23634 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | n-hexane | DMF+DMSO | 100 | na | dry air | spiro-OMeTAD | Li+TBP | 15.82 |
| Zhang, T. et al., Sci. Adv. 3, e1700841 (2017) | 2017 | TiO2 | 0 | CsPbI3·xEDAI2 | one-step | spin | no | DMF+EDAI2 | 150 | 2 | na | spiro-OMeTAD | Li+TBP | 10.5 |
| Zhang, F. et al., Nano Energy 41, 469–475 (2017) | 2017 | TiO2 | mTiO2 | (FAI)0.81(PbI2)0.85(MABr)0.15(PbBr2)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | Z26 | Li+TBP+FK209 | 19.8 |
| Zhang, F. et al., Nano Energy 41, 469–475 (2017) | 2017 | TiO2 | mTiO2 | (FAI)0.81(PbI2)0.85(MABr)0.15(PbBr2)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | Z25 | Li+TBP+FK209 | 16.7 |
| Zhang, F. et al., Nano Energy 41, 469–475 (2017) | 2017 | TiO2 | mTiO2 | (FAI)0.81(PbI2)0.85(MABr)0.15(PbBr2)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 20.4 |
| Zhang, X. et al., Sol. Energy 148, 70–77 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 10.1 |
| Zhang, X. et al., Sol. Energy 148, 70–77 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+Al | MS | na | na | spiro-OMeTAD | Li+TBP | 13.3 |
| Zhao, P. et al. J. Mater. Chem. A 5, 7905–7911 (2017) | 2017 | TiO2 | mTiO2 | MA1-xKxPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 17.2 |
| Zhao, Y. et al., J. Power Sources 359, 147–156 (2017) | 2017 | TiO2 | mTiO2 | FA0.6MA0.4PbI3 | two-step | spin-drip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | no | 18.9 |
| Zheng, X. et al., Nano Lett. 17, 2496–2505 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 14.76 |
| Zheng, X. et al., Nano Lett. 17, 2496–2505 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 14.089 |
| Zheng, X. et al., Nano Lett. 17, 2496–2505 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 10.385 |
| Zheng, X. et al., Nano Energy 38, 1–11 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 18 |
| Zheng, X. et al., Nano Energy 38, 1–11 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 17.4 |
| Zheng, J. et al., Sol. Energy Mater. Sol. Cells 168, 165–171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | blowdry | no | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.1 |
| Zheng, J. et al., Sol. Energy Mater. Sol. Cells 168, 165–171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 15.1 |
| Zuo, L. et al., Sci. Adv. 3, e1700106 (2017) | 2017 | SnO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.5 |
| Zuo, L. et al., Sci. Adv. 3, e1700106 (2017) | 2017 | SnO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF+PVP | - | - | - | spiro-OMeTAD | Li+TBP | 19.1 |
| Zuo, L. et al., Nano Lett. 17, 269–275 (2017) | 2017 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.8 |
| Zuo, L. et al., Nano Lett. 17, 269–275 (2017) | 2017 | SnO2 | PA-SAM | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.7 |
| Adnan, M. and Lee, J. K., Sci. Rep. 8, 2168 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | two-step | dipping | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 9.828 |
| Bashir, A. et al., Nanoscale 10, 2341–2350 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3-5AVAI | one-step | spin | no | GBL | na | na | na | Co3O4 | no | 11.32 |
| Christians, J. A. et al., Nat. Energy 3, 68–74 (2018) | 2018 | TiO2 | mTiO2 | (FA0.76MA0.21Cs0.03)0.67Pb(I0.89Br0.11)2.56 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 3 | glovebox | spiro-OMeTAD | Li+TBP | 18.5 |
| Christians, J. A. et al., Nat. Energy 3, 68–74 (2018) | 2018 | TiO2 | mTiO2 | (FA0.76MA0.21Cs0.03)0.67Pb(I0.89Br0.11)2.56 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | EH44 | EH44-ox+TBP | 17.5 |
| Domanski, K. et al., Nat. Energy 3, 61–67 (2018) | 2018 | TiO2 | mTiO2-Li | Cs5(FA83MA17)95Pb(I83Br17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | dry air | spiro-OMeTAD | Li+TBP+FK209 | 19.6 |
| Hou, Q. et al., ChemElectroChem 5, 725 (2018) | 2018 | α‐Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 10.3 |
| Hou, Q. et al., ChemElectroChem 5, 725 (2018) | 2018 | α‐Fe2O3 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 12.8 |
| Jiang, H. et al., ACS Appl. Energy Mater. 1, 900–909 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.3 |
| Jiang, H. et al., ACS Appl. Energy Mater. 1, 900–909 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL+HaHc | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.7 |
| Li, F. et al., Adv. Funct. Mater. 28, 1706377 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene-PF1 | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | no | 18.3 |
| Li, B. et al., Nat. Commun. 9, 1076 (2018) | 2018 | TiO2 | mTiO2 | CsPbI3 | one-step | spin | no | DMF+DMSO+PVP | 300 | 5 | glovebox | spiro-OMeTAD | no | 10 |
| Liu, N. et al., J. Mater. Chem. A 6, 6806–6814 (2018) | 2018 | SnO2 | 0 | MAxFA1-xPbI3-yBry | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 18.9 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V885 | Li+TBP+FK209 | 18.6 |
| Mathies, F. et al., ACS Appl. Energy Mater. acsaem.8b00222 (2018). doi:10.1021/acsaem.8b00222 | 2018 | TiO2 | 0 | Cs0.1(FA0.83MA0.17)0.9Pb(Br0.17I0.83)3 | one-step | printed | no | DMF+DMSO | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 12.9 |
| Que, M. et al., J. Power Sources 383, 42–49 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 14.02 |
| Que, M. et al., J. Power Sources 383, 42–49 (2018) | 2018 | TiO2 | mTiO2-Au | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 16.58 |
| Zhang, M. et al., Sol. RRL 2, 1700213 (2018) | 2018 | TiO2 | 0 | FAI, CsI, PbI2, MABr,PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP+FK209 | 18.47 |
| Zhang, M. et al., Sol. RRL 2, 1700213 (2018) | 2018 | TiO2 | 0 | FAI, CsI, PbI2, MABr,PbBr2 | one-step | spin 2-3 | methoxybenzene | DMF+DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP+FK209 | 19.08 |
| Zhao, Y. et al., Nat. Commun. 9, 1607 (2018) | 2018 | TiO2-Cl | 0 | Cs10 (Cs0.1FA0.78MA0.12PbI2.55Br0.45) | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 21.5 |
| Zhu, W. et al., Dalt. Trans. 47, 6404–6411 (2018) | 2018 | Ti-Fe2O3 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.05 |

Table S8. Stabilized efficiencies of inverted cells

| Article | Year | HTL | HTL-2 | Perovskite | Perovskite deposition procedure | Perovskite deposition method | Anti-solvent treatment | Precursor solution | Annealing temperature (°C) | Annealing time (minutes) | Annealing ambience | ETL | ETL interlayer | PCEstabilized (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Chen, W. et al., Energy Environ. Sci. 8, 629–640 (2015) | 2015 | NiOx | mAl2O3 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | glovebox | PCBM | BCP | 13.61 |
| Kaltenbrunner, M. et al. , Nat. Mater. 14, 1032–1039 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 110 | 20 | ambient | PTCDI | no | 12.5 |
| Kuang, C. et al., Nano Lett. 15, 2756–2762 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM-GD-C60 | no | 4.4 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPb(I0.8Br0.2)xCl3-x | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 9.84 |
| Park, I. J. et al, J. Phys. Chem. C 119, 27285–27290 (2015) | 2015 | NiOx | PEDOT:PSS | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | no | 14.8 |
| Qing, J. et al., ACS Appl. Mater. Interfaces 7, 23110–23116 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 5 | glovebox | BCP | no | 13.9 |
| Qiu, W. et al., Org. Electron. 26, 30–35 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | PCBM | ZnO | 12.5 |
| Wang, Q. et al., Nano Energy 15, 275–280 (2015) | 2015 | PTAA-1wtF4-TCNQ | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | BCP | 17.5 |
| Wang, X. et al., Org. Electron. physics, Mater. Appl. 24, 205–211 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | IPA | DMF | 80 | 120 | glovebox | PCBM+C60 | no | 11.8 |
| Wang, X. et al., Org. Electron. physics, Mater. Appl. 24, 205–211 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM+C60 | no | 10.8 |
| Ye, S. et al., Nano Lett. 15, 3723–3728 (2015) | 2015 | CuSCN | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | C60 | BCP | 16 |
| Yeo, J.-S. et al., Nano Energy 12, 96–104 (2015) | 2015 | GO | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 2 | glovebox | PCBM | BCP | 3.4592 |
| Yeo, J.-S. et al., Nano Energy 12, 96–104 (2015) | 2015 | RGO | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 2 | glovebox | PCBM | BCP | 11.703 |
| Yeo, J.-S. et al., Nano Energy 12, 96–104 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 2 | glovebox | PCBM | BCP | 9.266 |
| Yin, X. et al., J. Mater. Chem. A 3, 24495–24503 (2015) | 2015 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 14.03 |
| Adam, G. et al., Sol. Energy Mater. Sol. Cells 157, 318–325 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 110 | 45 | ambient | PCBM | no | 12.6 |
| Bai, Y. et al., Adv. Funct. Mater. 26, 2950–2958 (2016) | 2016 | NiOx | DEA | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | PCBM | no | 15.52 |
| Bai, Y. et al., Adv. Funct. Mater. 26, 2950–2958 (2016) | 2016 | NiOx | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | PCBM | no | 11.36 |
| Fu, W. et al., Sol. Energy Mater. Sol. Cells 155, 331–340 (2016) | 2016 | PTAA | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | ZnO | 16.1 |
| Fu, F. et al., Nat. Energy, 2, 16190 (2016) | 2016 | PTAA | 0 | MAPbI3 | two-step | spin | chlorobenzene | na | - | - | - | PCBM | ZnO | 16.1 |
| Li, B. et al., Org. Electron. 34, 97–103 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM+C60 | no | 13.96 |
| Li, B. et al., Org. Electron. 34, 97–103 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM+C60 | no | 11.6 |
| Liu, X. et al., Nano Energy 30, 417–425 (2016) | 2016 | NiOx-Cu | 0 | MAPbI3 | one-step | spin 2-3 | no | DMSO+GBL+DFC60 | 100 | 10 | na | PCBM+C60 | no | 18 |
| Liu, Z. et al, Nano Energy, 28, 151–157 (2016) | 2016 | P3HT | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | na | PCBM | no | 15.4 |
| Liu, Z. et al, Nano Energy, 28, 151–157 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | na | PCBM | no | 14.2 |
| Qing, J. et al., Org. Electron. physics, Mater. Appl. 38, 144–149 (2016) | 2016 | PEDOT:PSS | 0 | Cs0.15FA0.85PbI3 | one-step | spin | toluene | DMF+DMSO+MACl | 120 | 10 | glovebox | C60 | BCP | 14.5 |
| Rao, H. et al., Nano Energy 27, 51–57 (2016) | 2016 | CuOx | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 10 | glovebox | PCBM+C60 | BCP | 18 |
| Sun, W. et al., Nanoscale 8, 10806–10813 (2016) | 2016 | CuOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | C60 | BCP | 16.3 |
| Xie, J. et al., Nano Energy 28, 330–337 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | ambient | PCBM | PCBDAN | 17 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | HSL2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 16.5 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | HSL2 | MAPb(I0.3Br0.7)xCl3-x | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 10.2 |
| Yin, X. et al., ACS Nano 10, 3630–3636 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 16.21 |
| Yin, X. et al., ACS Nano 10, 3630–3636 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 11.13 |
| Yin, X. et al., J. Power Sources 329, 398–405 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | PCBM | no | 16.49 |
| Mohd Yusoff, A. R. bin et al., Nanoscale 8, 6328–6334 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Zr(acac) | no | 12 |
| Zhou, Z. et al., Sol. Energy 136, 210–216 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF+HI | - | - | - | PCBM | Ca | 18.693 |
| Chen, Q. et al., Nano Lett. 17, 3231–3237 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | TiOx | 15.5 |
| Chen, Q. et al., Nano Lett. 17, 3231–3237 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL+Ag | 100 | 10 | na | PCBM | TiOx | 17.7 |
| Chen, Q. et al., Dye. Pigment., 147, 113–119 (2017) | 2017 | TTA | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | PCBM+C60 | BCP | 15.6 |
| Chen, Z. et al., Nat. Commun., 8, 1890 (2017) | 2017 | PTAA | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 60 | na | PCBM+C60 | BCP | 17.7 |
| Fu, G. et al., Sol. Energy Mater. Sol. Cells 165, 36–44 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | na | na | na | PCBM | TIPD | 17.8 |
| He, M. et al., Nat. Commun. 8, 16045 (2017) | 2017 | PTAA-Li:TBP | 0 | FA0.85MA0.15PbI2.55Br0.45 | one-step | MASP | no | DMSO | na | na | na | PCBM | BCP | 19.1 |
| Hong, S. C. et al., ACS Appl. Mater. Interfaces 9, 7879–7884 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | electrospray | no | DMSO | 100 | 5 | na | C60 | BCP | 13 |
| Jošt, M. et al., ACS Photonics 4, 1232–1239 (2017) | 2017 | PTAA | 0 | MAPbI3 | one-step | spin | no | DMF+HPA | 80 | 5 | glovebox | PCBM | BCP | 16.1 |
| Kim, H.-S. et al., ACS Omega 2, 9074–9079 (2017) | 2017 | NiOx | 0 | FAPbI3, MAPbBr3, CsI | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 50 | glovebox | PCBM | BCP | 15.3 |
| Kim, H.-S. et al., ACS Omega 2, 9074–9079 (2017) | 2017 | NiOx-Cs | 0 | FAPbI3, MAPbBr3, CsI | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 50 | glovebox | PCBM | BCP | 17.2 |
| Lin, Y. et al., Adv. Mater., 29, 1700607 (2017) | 2017 | PTAA | 0 | (FA0.83MA0.17)0.95Cs0.05Pb(I0.6Br0.4)3 | one-step | spin 2-3 | toluene | DMF+DMSO | MS | na | glovebox | ICBA+tran3+C60 | BCP | 18.2 |
| Liu, J. et al., ChemPhysChem 18, 617–625 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | glovebox | PCBM | BCP | 13.167 |
| Luo, D. et al., Adv. Mater. 29, 1604758 (2017) | 2017 | PTAA-F4-TCNQ | 0 | MA0.6FA0.4PbI3 | one-step | spin | no | DMF | 140 | 10 | glovebox | PCBM+C60 | BCP | 19.8 |
| Wang, K. et al., ACS Omega, 2, 6250–6258 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 15 | glovebox | PCBM | BCP | 14.3 |
| Wang, N. et al., Adv. Energy Mater. 7, 1700522 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 100 | 5 | glovebox | HATNT | LiF | 18 |
| Xue, Q. et al., Adv. Energy Mater. 7, 1602333 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 15 | glovebox | C60(CH2) | no | 17.9 |
| Xue, Q. et al., Adv. Energy Mater. 7, 1602333 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 15 | glovebox | PCBM | no | 16.1 |
| Yao, K. et al., Nano Energy, 40, 155–162 (2017) | 2017 | NiOx-Cu | mNiOx-Cu | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | PCBM+C60 | no | 19.5 |
| Yoon, J. et al., Energy Environ. Sci. 10, 337–345 (2017) | 2017 | PEDOT:PSS-F4-TCNQ | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | C60 | BCP/LiF | 16.6 |
| Zhang, H. et al., Adv. Mater. 29, 1604695 (2017) | 2017 | NiOx | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | C60 | no | 17.07 |
| Zhao, D. et al., Nat. Energy 2, 17018 (2017) | 2017 | PEDOT:PSS | 0 | (FASnI3)0.6(MAPbI3)0.4 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 7 | glovebox | C60 | BCP | 17 |
| Zhao, J. et al., Adv. Energy Mater., 7, 1602599 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 90 | glovebox | PCBM | AZO | 11 |
| Zheng, X. et al., Nat. Energy, 2, 17102 (2017) | 2017 | PTAA | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | choline chloride+C60 | BCP | 19.6 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS-Na | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF | 100 | 30 | glovebox | PCBM | no | 15.4 |
| Chen, W. et al., Org. Electron., 58, 283–289 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | toluene | DMSO+GBL+ASCl | 100 | 20 | glovebox | PCBM | no | 14.26 |
| Han, C. et al., J. Mater. Chem. C (2018). doi:10.1039/C8TC01033A | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 5 | na | PCBM | PEI | 15.048 |
| Han, C. et al., J. Mater. Chem. C (2018). doi:10.1039/C8TC01033A | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene-ITIC | DMSO+GBL | 100 | 5 | na | PCBM | PEI | 16.544 |
| Han, C. et al., J. Mater. Chem. C (2018). doi:10.1039/C8TC01033A | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL+ITIC | 100 | 5 | na | PCBM | PEI | 15.928 |
| Lee, H. et al., Sci. Rep. 8, 5590 (2018) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | na | PCBM | BCP | 11.8 |
| Li, W. et al., Energy Environ. Sci., 11, 286–293 (2018) | 2018 | NiOx | 0 | CsxFA1-xPbI3–[GaAA3]4 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 30 | dry air | PCBM | BCP | 18 |
| Liu, C. et al., J. Am. Chem. Soc., 140, 3825–3828 (2018) | 2018 | NiOx | 0 | CsPbI2Br | one-step | spin 2-3 | no | DMSO | MS | na | na | ZnO-C60 | no | 12 |
| Niu, G. et al., J. Mater. Chem. A , 6, 4721–4728 (2018) | 2018 | NiMgLiO | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 90 | 10 | na | PCBM | BCP | 17.14 |
| Niu, G. et al., J. Mater. Chem. A , 6, 4721–4728 (2018) | 2018 | NiMgLiO | 0 | Cs0.05FA0.15MA0.8PbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 90 | 10 | na | PCBM | BCP | 19.15 |
| Shao, S. et al., Adv. Energy Mater., 8, 1702019 (2018) | 2018 | PEDOT:PSS | 0 | PEA2FAn-1SnnI3n+1 | one-step | spin | diethyl ether | DMF+DMSO | 65 | 20 | glovebox | C60 | BCP | 8.5 |
| Wu, W.-Q. et al., Nat. Commun., 9, 1625 (2018) | 2018 | no | no | MAPbI3 | one-step | spin | no | DMF+F4TCNQ | 100 | 30 | glovebox | C60 | BCP | 19.9 |
| Yu, J. C. et al., Sci. Rep. 8, 1070 (2018) | 2018 | PEDOT:GO | 0 | MAPbI3-xBrx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 20 | glovebox | PCBM | ZnO | 17.68 |
| Zhang, J. et al., Adv. Energy Mater., 8, 1701981 (2017) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 95 | na | na | PCBM | no | 13.3 |
| Zhang, J. et al., Adv. Energy Mater., 8, 1701981 (2017) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO+LiI | 95 | na | na | PCBM | no | 18.1 |

Table S9. Best efficiencies of entire regular cells

| Article | Year | ETL | ETL-2 | Perovskite | Perovskite deposition procedure | Perovskite deposition method | Anti-solvent treatment | Precursor solution | Annealing temperature (°C) | Annealing time (minutes) | Annealing ambience | HTL | HTL additive | PCEbest (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | PCPDTBT | no | 6.8 |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | PCPDTBT | no | 0.6 |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | P3HT | no | 6.7 |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | P3HT | no | 3.8 |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 11.8 |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 11.7 |
| Abrusci, A. et al., Nano Lett. 13, 3124–3128 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 10.2 |
| Ball, J. M. et al., Energy Environ. Sci. 6, 1739 (2013) | 2013 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 12.3 |
| Bi, D. et al., J. Phys. Chem. Lett. 4, 1532–1536 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | ambient | DEH | Li+TBP | 1.6 |
| Bi, D. et al., J. Phys. Chem. Lett. 4, 1532–1536 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | ambient | P3HT | Li+TBP | 4.5 |
| Bi, D. et al., J. Phys. Chem. Lett. 4, 1532–1536 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | ambient | spiro-OMeTAD | Li+TBP | 8.5 |
| Bi, D. et al., Nanoscale 5, 11686 (2013) | 2013 | ZnO | ZnO-nanorod | MAPbI3 | one-step | spin | no | GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 5 |
| Burschka, J. et al., Nature 499, 316–319 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15 |
| Cai, B. et al., Energy Environ. Sci. 6, 1480 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | na | PCBTDPP | no | 5.6 |
| Cai, B. et al., Energy Environ. Sci. 6, 1480 (2013) | 2013 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin | no | GBL | 100 | 15 | na | PCBTDPP | no | 3 |
| Cai, B. et al., Energy Environ. Sci. 6, 1480 (2013) | 2013 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin | no | GBL | 100 | 15 | na | P3HT | no | 0.8 |
| Chen, H. et al., Chem. Commun. 49, 7277 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | glovebox | P3HT | Li+TBP | 6.5 |
| Chen, H. et al., Chem. Commun. 49, 7277 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | glovebox | P3HT | Li+TBP | 4.1 |
| Colella, S. et al., Chem. Mater. 25, 4613–4618 (2013) | 2013 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 7.4 |
| Colella, S. et al., Chem. Mater. 25, 4613–4618 (2013) | 2013 | TiO2 | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 4.8 |
| Dharani, S. et al., Nanoscale 6, 1675–1679 (2014) | 2013 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3.1 |
| Dharani, S. et al., Nanoscale 6, 1675–1679 (2014) | 2013 | TiO2 | TiO2-nanofiber | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.8 |
| Edri, E. et al., J. Phys. Chem. Lett. 4, 897–902 (2013) | 2013 | TiO2 | mAl2O3 | MAPbBr3 | one-step | spin | no | DMF | 100 | 45 | na | PCBM | no | 0.7 |
| Edri, E. et al., J. Phys. Chem. Lett. 4, 897–902 (2013) | 2013 | TiO2 | mAl2O3 | MAPbBr3 | one-step | spin | no | DMF | 100 | 45 | na | TPD | no | 0.7 |
| Edri, E. et al., J. Phys. Chem. Lett. 4, 897–902 (2013) | 2013 | TiO2 | mAl2O3 | MAPbBr3 | one-step | spin | no | DMF | 100 | 45 | na | PDI | no | 0.6 |
| Edri, E. et al., J. Phys. Chem. Lett. 4, 897–902 (2013) | 2013 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin | no | DMF | 100 | 45 | na | PDI | no | 0.5 |
| Edri, E. et al., J. Phys. Chem. Lett. 4, 897–902 (2013) | 2013 | TiO2 | mAl2O3 | MAPbBr3 | one-step | spin | no | DMF | 100 | 45 | na | P3HT | no | 0.5 |
| Heo, J. H. et al., Nat. Photonics 7, 486–491 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | glovebox | no | no | 2.5 |
| Heo, J. H. et al., Nat. Photonics 7, 486–491 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | glovebox | PCPDTBT | no | 5.3 |
| Heo, J. H. et al., Nat. Photonics 7, 486–491 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | glovebox | PCDTBT | no | 4.2 |
| Heo, J. H. et al., Nat. Photonics 7, 486–491 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | glovebox | PTAA | no | 12 |
| Heo, J. H. et al., Nat. Photonics 7, 486–491 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | glovebox | P3HT | Li+TBP | 6.7 |
| Heo, J. H. et al., Nat. Photonics 7, 486–491 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | glovebox | spiro-OMeTAD | Li+TBP | 8.4 |
| Jeon, N. J. et al., J. Am. Chem. Soc. 135, 19087–19090 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | no | no | 8 |
| Jeon, N. J. et al., J. Am. Chem. Soc. 135, 19087–19090 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | Py-C | Li+TBP+FK269 | 12.4 |
| Jeon, N. J. et al., J. Am. Chem. Soc. 135, 19087–19090 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | spiro-OMeTAD | Li+TBP+FK269 | 12.7 |
| Shi, J. J. et al., Chinese Phys. Lett. 30, 128402 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | na | na | no | no | 5.1 |
| Shi, J. J. et al., Chinese Phys. Lett. 30, 128402 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | na | na | no | no | 3.3 |
| Kim, H. S. et al., Nano Lett. 13, 2412–2417 (2013) | 2013 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin | no | GBL | na | na | na | spiro-OMeTAD | Li+TBP | 9.4 |
| Kumar, M. H. et al., Chem. Commun. 49, 11089 (2013) | 2013 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 5.5 |
| Kumar, M. H. et al., Chem. Commun. 49, 11089 (2013) | 2013 | ZnO | ZnO-nanorod | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 8.9 |
| Laban, W. A. and Etgar, L., Energy Environ. Sci. 6, 3249 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 15 | glovebox | no | no | 8 |
| Bi, D. et al., RSC Adv. 3, 18762 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.5 |
| Bi, D. et al., RSC Adv. 3, 18762 (2013) | 2013 | TiO2 | mZrO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.8 |
| Liu, M. et al., Nature 501, 395–398 (2013) | 2013 | TiO2 | 0 | MAPbI3-xClx | one-step | CVD | no | na | na | na | na | spiro-OMeTAD | Li+TBP | 15.4 |
| Liu, M. et al., Nature 501, 395–398 (2013) | 2013 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | na | na | na | na | spiro-OMeTAD | Li+TBP | 8.6 |
| Liu, D. and Kelly, T. L., Nat. Photonics 8, 133–138 (2013) | 2013 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.7 |
| Noh, J. H. et al., Nano Lett. 13, 1764–1769 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3-xBrx | one-step | spin 2-3 | no | DMF+GBL | 100 | 5 | na | PTAA | Li+TBP | 12.3 |
| Noh, J. H. et al., J. Mater. Chem. A 1, 11842 (2013) | 2013 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | spiro-OMeTAD | Li+TBP+FK209 | 10.4 |
| Qiu, J. et al., Nanoscale 5, 3245 (2013) | 2013 | TiO2 | TiO2-nanowire | MAPbI3 | one-step | spin | no | DMF | 100 | 30 | ambient | spiro-OMeTAD | Li+TBP | 4.3 |
| Qiu, J. et al., Nanoscale 5, 3245 (2013) | 2013 | TiO2 | TiO2-nanowire | MAPbI2Br | one-step | spin | no | DMF | 100 | 30 | ambient | spiro-OMeTAD | Li+TBP | 4.9 |
| Zhang, W. et al., Nano Lett. 13, 4505–4510 (2013) | 2013 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 10.7 |
| Zhang, W. et al., Nano Lett. 13, 4505–4510 (2013) | 2013 | TiO2 | Au@SiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 11.4 |
| Abate, A. et al., Nano Lett. 14, 3247–3254 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 15.7 |
| Abate, A. et al., Nano Lett. 14, 3247–3254 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 13 |
| Abate, A. et al., Nano Lett. 14, 3247–3254 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 6.1 |
| Abate, A. et al., Nano Lett. 14, 3247–3254 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 3.8 |
| Aharon, S. et al., Phys. Chem. Chem. Phys. 16, 10512–10518 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | no | no | 10.9 |
| Aharon, S. et al., J. Phys. Chem. C 118, 17160–17165 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 1.7 |
| Aharon, S. et al., J. Phys. Chem. C 118, 17160–17165 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 7.2 |
| Aharon, S. et al., J. Phys. Chem. C 118, 17160–17165 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xBrx | two-step | spin-dip | no | DMF | - | - | - | no | no | 8.5 |
| Badia, L. et al., APL Mater. 2, 081507 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 9.2 |
| Badia, L. et al., APL Mater. 2, 081507 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP+Ir | 10.8 |
| Bera, A. et al., J. Phys. Chem. C 118, 28494–28501 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 7.8 |
| Bera, A. et al., J. Phys. Chem. C 118, 28494–28501 (2014) | 2014 | TiO2 | Msto | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 7.6 |
| Chandiran, A. K. et al., Adv. Mater. 26, 4309–4312 (2014) | 2014 | 0 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.5 |
| Chandiran, A. K. et al., Adv. Mater. 26, 4309–4312 (2014) | 2014 | 0 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 7.2 |
| Chavhan, S. et al., J. Mater. Chem. A 2, 12754–12760 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 110 | 180 | glovebox | CuSCN | no | 6.4 |
| Chen, Q. et al., Nano Lett. 14, 4158–4163 (2014) | 2014 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12 |
| Chen, Q. et al., J. Am. Chem. Soc. 136, 622–625 (2014) | 2014 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.1 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 6.9 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | OMeTPA-FA | no | 11.1 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | OMeTPA-FA | Li+TBP | 12.4 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | OMeTPA-TPA | Li+TBP | 11 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | OMeTPA-FA | Li+TBP+FK209 | 13.6 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | OMeTPA-TPA | Li+TBP+FK209 | 12.3 |
| Choi, H. et al., Chem. - A Eur. J. 20, 10894–10899 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 14.7 |
| Christians, J. A. et al., J. Am. Chem. Soc. 136, 758–764 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 80 | 45 | na | spiro-OMeTAD | Li+TBP | 7.9 |
| Christians, J. A. et al., J. Am. Chem. Soc. 136, 758–764 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 80 | 45 | na | CuI | no | 6 |
| Colella, S. et al., J. Phys. Chem. Lett. 5, 3532–3538 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 9.2 |
| Conings, B. et al., APL Mater. 2, 081505 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMSO | 100 | 60 | glovebox | P3HT | no | 13.6 |
| Conings, B. et al., Adv. Mater. 26, 2041–2046 (2014) | 2014 | TiO2 | 0 | MAPbI2Cl | one-step | spin | no | DMF | 100 | 50 | glovebox | P3HT | no | 11.4 |
| Ding, Y. et al., J. Power Sources 272, Ahead of Print (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 140 | 50 | na | spiro-OMeTAD | Li+TBP | 4.5 |
| Ding, Y. et al., J. Power Sources 272, Ahead of Print (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF+PVP | 140 | 50 | na | spiro-OMeTAD | Li+TBP | 8.7 |
| Do, K. et al., Chem. Commun. 50, 10971–10974 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Triazine-Th-OMeTPA | Li+TBP+FK102 | 12.5 |
| Do, K. et al., Chem. Commun. 50, 10971–10974 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Triazine-Ph-OMeTPA | Li+TBP+FK102 | 10.9 |
| Do, K. et al., Chem. Commun. 50, 10971–10974 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 13.5 |
| Edri, E. et al., J. Phys. Chem. Lett. 5, 429–433 (2014) | 2014 | TiO2 | mAl2O3 | MAPbBr3 | one-step | spin 2-3 | no | DMF | 150 | 60 | ambient | CBP | Li+TBP | 0.4 |
| Edri, E. et al., J. Phys. Chem. Lett. 5, 429–433 (2014) | 2014 | TiO2 | mAl2O3 | MAPbBr3-xClx | one-step | spin 2-3 | no | DMF | 150 | 60 | ambient | CBP | Li+TBP | 2.7 |
| Edri, E. et al., J. Phys. Chem. Lett. 5, 429–433 (2014) | 2014 | TiO2 | mAl2O3 | MAPbBr3-xClx | one-step | spin 2-3 | no | DMF | 150 | 60 | ambient | CBP | TBP | 0.4 |
| Eperon, G. E. et al., Energy Environ. Sci. 7, 982 (2014) | 2014 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | 100 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 14.2 |
| Etgar, L. et al., J. Mater. Chem. A 2, 11586–11590 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | no | no | 3 |
| Etgar, L. et al., J. Mater. Chem. A 2, 11586–11590 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | PbS QDs | no | 3.6 |
| Di Giacomo, F. et al., J. Power Sources 251, 152–156 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 120 | 60 | ambient | P3HT | Li+TBP | 9.3 |
| Di Giacomo, F. et al., J. Power Sources 251, 152–156 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 120 | 60 | ambient | spiro-OMeTAD | Li+TBP | 8.6 |
| Guo, Y. et al., J. Mater. Chem. A 2, 13827–13830 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 95 | glovebox | P3HT | no | 9.2 |
| Guo, Y. et al., J. Mater. Chem. A 2, 13827–13830 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 95 | glovebox | P3HT | Li | 11.2 |
| Guo, Y. et al., J. Mater. Chem. A 2, 13827–13830 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 95 | glovebox | P3HT | Li+D-TBP | 12.4 |
| Guo, Y. et al., J. Mater. Chem. A 2, 13827–13830 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 95 | glovebox | P3HT | D-TBP | 9.1 |
| Hanusch, F. C. et al., J. Phys. Chem. Lett. 5, 2791–2795 (2014) | 2014 | TiO2 | 0 | MAPbBr3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 0.4 |
| Hanusch, F. C. et al., J. Phys. Chem. Lett. 5, 2791–2795 (2014) | 2014 | TiO2 | 0 | FAPbBr3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.5 |
| Hao, F. et al., Nat. Photonics 8, 489–494 (2014) | 2014 | TiO2 | mTiO2 | MASnIBr2 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 6 |
| Hao, F. et al., Nat. Photonics 8, 489–494 (2014) | 2014 | TiO2 | mTiO2 | MASnI2Br | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 5.6 |
| Hao, F. et al., Nat. Photonics 8, 489–494 (2014) | 2014 | TiO2 | mTiO2 | MASnI3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 5.4 |
| Hao, F. et al., Nat. Photonics 8, 489–494 (2014) | 2014 | TiO2 | mTiO2 | MASnBr3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 4.5 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 8094–8099 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 8.3 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 8094–8099 (2014) | 2014 | TiO2 | mTiO2 | MASn0.25Pb0.75I3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 7.4 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 8094–8099 (2014) | 2014 | TiO2 | mTiO2 | MASn0.5Pb0.5I3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 7.3 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 8094–8099 (2014) | 2014 | TiO2 | mTiO2 | MASn0.75Pb0.25I3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 3.7 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 8094–8099 (2014) | 2014 | TiO2 | mTiO2 | MASnI3 | one-step | spin | no | DMF | 125 | 30 | na | spiro-OMeTAD | Li+2,6lutidiene | 5.4 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 16411–16419 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | no | no | 6.4 |
| Hao, F. et al., J. Am. Chem. Soc. 136, 16411–16419 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | no | no | 10.6 |
| Hu, Q. et al., ACS Nano 8, 10161–10167 (2014) | 2014 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.2 |
| Hu, Q. et al., ACS Nano 8, 10161–10167 (2014) | 2014 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.6 |
| Hu, Q. et al., ACS Nano 8, 10161–10167 (2014) | 2014 | Cs2CO3 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Huang, F. et al., Nano Energy 10, 10–18 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17 |
| Huang, F. et al., Nano Energy 10, 10–18 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 5.7 |
| Huang, F. et al., Nano Energy 10, 10–18 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 75 | 10 | na | spiro-OMeTAD | Li+TBP | 13.4 |
| Huang, F. et al., Nano Energy 10, 10–18 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 60 | 10 | na | spiro-OMeTAD | Li+TBP | 8.6 |
| Huang, F. et al., Nano Energy 10, 10–18 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 35 | 10 | na | spiro-OMeTAD | Li+TBP | 4.3 |
| Ito, S. et al., ChemPhysChem 15, 1194–1200 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | ambient | no | no | 1.4 |
| Ito, S. et al., ChemPhysChem 15, 1194–1200 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | ambient | no | no | 0.8 |
| Ito, S. et al., ChemPhysChem 15, 1194–1200 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | ambient | CuSCN | no | 4.9 |
| Ito, S. et al., ChemPhysChem 15, 1194–1200 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | ambient | CuSCN | no | 1.8 |
| Ito, S. et al., J. Phys. Chem. C 118, 16995–17000 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | ambient | CuSCN | no | 5.1 |
| Ito, S. et al., J. Phys. Chem. C 118, 16995–17000 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | ambient | CuSCN | no | 4.8 |
| Jeon, N. J. et al., Nat. Mater. 13, 897–903 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18 |
| Jeon, N. J. et al., J. Am. Chem. Soc. 136, 7837–7840 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 15.2 |
| Jeon, N. J. et al., J. Am. Chem. Soc. 136, 7837–7840 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14.9 |
| Jeon, N. J. et al., J. Am. Chem. Soc. 136, 7837–7840 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.9 |
| Jeon, N. J. et al., Nat. Mater. 13, 897–903 (2014) | 2014 | TiO2 | 0 | MAPbI3-xBrx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PTAA | no | 15.8 |
| Jeon, N. J. et al., Nat. Mater. 13, 897–903 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xBrx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PTAA | no | 16.7 |
| Juarez-Perez, E. J. et al., J. Phys. Chem. Lett. 5, 680–685 (2014) | 2014 | 0 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 0.1 |
| Juarez-Perez, E. J. et al., J. Phys. Chem. Lett. 5, 680–685 (2014) | 2014 | ZnO | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 1.8 |
| Juarez-Perez, E. J. et al., J. Phys. Chem. Lett. 5, 680–685 (2014) | 2014 | CdS | mAl2O3 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 1.5 |
| Juarez-Perez, E. J. et al., J. Phys. Chem. Lett. 5, 680–685 (2014) | 2014 | 0 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5 |
| Juarez-Perez, E. J. et al., J. Phys. Chem. Lett. 5, 680–685 (2014) | 2014 | ZnO | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.1 |
| Juarez-Perez, E. J. et al., J. Phys. Chem. Lett. 5, 680–685 (2014) | 2014 | ZnO | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 7.9 |
| Ke, W. et al., ACS Appl. Mater. Interfaces 6, 15959–15965 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Koh, T. M. et al., ChemSusChem 7, 1909–1914 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 11 |
| Koh, T. M. et al., ChemSusChem 7, 1909–1914 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+MY11 | 11.9 |
| Krishna, A. et al., Chem. Sci. 5, 2702–2709 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 4.7 |
| Krishna, A. et al., Chem. Sci. 5, 2702–2709 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | T1no3 | Li+TBP+FK102 | 12.4 |
| Krishna, A. et al., Chem. Sci. 5, 2702–2709 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | T1no2 | Li+TBP+FK102 | 12.2 |
| Krishna, A. et al., Chem. Sci. 5, 2702–2709 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | T1no1 | Li+TBP+FK102 | 8.4 |
| Krishna, A. et al., Chem. Sci. 5, 2702–2709 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 12.9 |
| Krishnamoorthy, T. et al., J. Mater. Chem. A 2, 6305–6309 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | KTM3 | no | 7.3 |
| Krishnamoorthy, T. et al., J. Mater. Chem. A 2, 6305–6309 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | KTM3 | Li+TBP+FK102 | 8.7 |
| Krishnamoorthy, T. et al., J. Mater. Chem. A 2, 6305–6309 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | KTM3 | Li+TBP+FK209 | 11 |
| Krishnamoorthy, T. et al., J. Mater. Chem. A 2, 6305–6309 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 11.4 |
| Kwon, Y. S. et al., Energy Environ. Sci. 7, 1454 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | PDPPDBTE | no | 9.2 |
| Kwon, Y. S. et al., Energy Environ. Sci. 7, 1454 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | P3HT | Li+TBP | 6.3 |
| Kwon, Y. S. et al., Energy Environ. Sci. 7, 1454 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 7.6 |
| Lee, J.-W. et al., ChemPhysChem 15, 2595–2603 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMA | 100 | 15 | na | PTB-DCB21 | no | 8.7 |
| Lee, J.-W. et al., ChemPhysChem 15, 2595–2603 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMA | 100 | 15 | na | PTB-BO | no | 7.4 |
| Lee, J.-W. et al., ChemPhysChem 15, 2595–2603 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMA | 100 | 15 | na | spiro-OMeTAD | no | 7 |
| Lee, J.-W. et al., ChemPhysChem 15, 2595–2603 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMA | 100 | 15 | na | PTB-DCB21 | Li+TBP | 9.5 |
| Lee, J.-W. et al., ChemPhysChem 15, 2595–2603 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMA | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 11.6 |
| Lee, J. W. et al., Adv. Mater. 26, 4991–4998 (2014) | 2014 | TiO2 | mTiO2 | FAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16 |
| Lee, J.-W. et al., J. Mater. Chem. A 2, 9251 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMA | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 9 |
| Lee, J.-W. et al., J. Mater. Chem. A 2, 9251 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMA | - | - | - | spiro-OMeTAD | Li+TBP | 14.5 |
| Leijtens, T. et al., J. Phys. Chem. Lett. 5, 1096–1102 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 8.6 |
| Li, H. et al., Angew. Chemie - Int. Ed. 53, 4085–4088 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | H1no1 | Li+TBP | 11.1 |
| Li, H. et al., Angew. Chemie - Int. Ed. 53, 4085–4088 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | H1no1 | Li+TBP+FK102 | 13.8 |
| Li, H. et al., Angew. Chemie - Int. Ed. 53, 4085–4088 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 13.7 |
| Li, Z. et al., ACS Nano 8, 6797–6804 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 6.9 |
| Li, Z. et al., ACS Nano 8, 6797–6804 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 5.1 |
| Li, Z. et al., ACS Nano 8, 6797–6804 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 9.9 |
| Li, W. et al., J. Mater. Chem. A 2, 13587–13592 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.9 |
| Li, W. et al., J. Mater. Chem. A 2, 13587–13592 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9 |
| Liang, L. et al., ACS Appl. Mater. Interfaces 6, 20585–20589 (2014) | 2014 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.4 |
| Liang, L. et al., ACS Appl. Mater. Interfaces 6, 20585–20589 (2014) | 2014 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 7 |
| Liu, J. et al., Energy Environ. Sci. 7, 2963–2967 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | TTF-1 | no | 11 |
| Liu, J. et al., Energy Environ. Sci. 7, 2963–2967 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 6.2 |
| Liu, J. et al., Energy Environ. Sci. 7, 2963–2967 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 6.2 |
| Liu, J. et al., Energy Environ. Sci. 7, 2963–2967 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | TTF-1 | Li+TBP | 4.4 |
| Liu, J. et al., Energy Environ. Sci. 7, 2963–2967 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | Li+TBP | 6.7 |
| Liu, J. et al., Energy Environ. Sci. 7, 2963–2967 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.4 |
| Liu, D., Yang, J. and Kelly, T. L., J. Am. Chem. Soc. 136, 17116–17122 (2014) | 2014 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | Li+TBP | 11.7 |
| Liu, D., Yang, J. and Kelly, T. L., J. Am. Chem. Soc. 136, 17116–17122 (2014) | 2014 | no | no | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | Li+TBP | 11.6 |
| Liu, D., Yang, J. and Kelly, T. L., J. Am. Chem. Soc. 136, 17116–17122 (2014) | 2014 | ZnO | no | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.7 |
| Liu, D., Yang, J. and Kelly, T. L., J. Am. Chem. Soc. 136, 17116–17122 (2014) | 2014 | no | no | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Lv, S. et al., Chem. Commun. 50, 6931 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | HTM2 | no | 11.6 |
| Lv, S. et al., Chem. Commun. 50, 6931 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | HTM1 | no | 11.3 |
| Mahmood, K. et al., Nanoscale 6, 9127 (2014) | 2014 | ZnO | mZnO | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.9 |
| Mahmood, K. et al., Nanoscale 6, 9127 (2014) | 2014 | ZnO-Al | m-Al-ZnO | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.2 |
| Manseki, K. et al., RSC Adv. 4, 9652–9655 (2014) | 2014 | TiO2 | Mg-TiO2-nanorod | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | P3HT | Li+TBP | 4.2 |
| Manseki, K. et al., RSC Adv. 4, 9652–9655 (2014) | 2014 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | P3HT | Li+TBP | 3.1 |
| Moehl, T. et al., J. Phys. Chem. Lett. 5, 3931–3936 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.1 |
| Moehl, T. et al., J. Phys. Chem. Lett. 5, 3931–3936 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.6 |
| Nagarjuna, P. et al., Electrochim. Acta 151, 21–26 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 45 | na | no | no | 2.7 |
| Nagarjuna, P. et al., Electrochim. Acta 151, 21–26 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 45 | na | copolymerP | no | 6.6 |
| Nagarjuna, P. et al., Electrochim. Acta 151, 21–26 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 45 | na | P3HT | no | 4.2 |
| Nguyen, W. H. et al., J. Am. Chem. Soc. 136, 10996–11001 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.5 |
| Nguyen, W. H. et al., J. Am. Chem. Soc. 136, 10996–11001 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | spiro(TFSI)2+TBP | 10.6 |
| Niu, G. et al., J. Mater. Chem. A 2, 705–710 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 4.7 |
| Niu, G. et al., J. Mater. Chem. A 2, 705–710 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 4.6 |
| Noel, N. K. et al., ACS Nano 8, 9815–9821 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 16.5 |
| Noel, N. K. et al., ACS Nano 8, 9815–9821 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.3 |
| Noel, N. K. et al., ACS Nano 8, 9815–9821 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 13.1 |
| Noel, N. K. et al., Energy Environ. Sci. 7, 3061–3068 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | glovebox | spiro-OMeTAD | H+TBP | 15 |
| Noel, N. K. et al., Energy Environ. Sci. 7, 3061–3068 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | glovebox | spiro-OMeTAD | H+TBP | 11.5 |
| Noel, N. K. et al., Energy Environ. Sci. 7, 3061–3068 (2014) | 2014 | TiO2 | mTiO2 | MASnI3 | one-step | spin | no | DMF | na | na | glovebox | spiro-OMeTAD | H+TBP | 6.4 |
| Ogomi, Y. et al., J. Phys. Chem. Lett. 5, 1004–1011 (2014) | 2014 | TiO2 | mTiO2 | MASn1-xPbxI3 | one-step | spin | no | DMF | 70 | 30 | glovebox | P3HT | no | 4.2 |
| Ogomi, Y. et al., J. Phys. Chem. Lett. 5, 1004–1011 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 70 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 12 |
| Ogomi, Y. et al., in ChemPhysChem 15, 1062–1069 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 7.5 |
| Ogomi, Y. et al., in ChemPhysChem 15, 1062–1069 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 7 |
| Ogomi, Y. et al., in ChemPhysChem 15, 1062–1069 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 6.6 |
| Pang, S. et al., Chem. Mater. 26, 1485–1491 (2014) | 2014 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | P3HT | no | 3.7 |
| Pang, S. et al., Chem. Mater. 26, 1485–1491 (2014) | 2014 | TiO2 | mTiO2 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 7.5 |
| Pathak, S. K. et al., Adv. Funct. Mater. 24, 6046–6055 (2014) | 2014 | TiO2-Al | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 13.8 |
| Pathak, S. K. et al., Adv. Funct. Mater. 24, 6046–6055 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 11.1 |
| Pellet, N. et al., Angew. Chemie - Int. Ed. 53, 3151–3157 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.5 |
| Pellet, N. et al., Angew. Chemie - Int. Ed. 53, 3151–3157 (2014) | 2014 | TiO2 | mTiO2 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11 |
| Pellet, N. et al., Angew. Chemie - Int. Ed. 53, 3151–3157 (2014) | 2014 | TiO2 | mTiO2 | (MA)0.6(FA)0.4PbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.9 |
| Qin, P. et al., Nat. Commun. 5, 3834 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | no | no | 6.7 |
| Qin, P. et al., Nat. Commun. 5, 3834 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 3.8 |
| Qin, P. et al., Nat. Commun. 5, 3834 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | CuSCN | no | 12.4 |
| Qin, P. et al., Nat. Commun. 5, 3834 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | CuSCN | no | 11.2 |
| Qin, P. et al., J. Am. Chem. Soc. 136, 8516–8519 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 7.7 |
| Qin, P. et al., J. Am. Chem. Soc. 136, 8516–8519 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Fused-F | no | 12.8 |
| Qin, P. et al., J. Am. Chem. Soc. 136, 8516–8519 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.7 |
| Qin, P. et al., Nanoscale 6, 1508–1514 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 10 | dry air | spiro-OMeTAD | Li+TBP | 10.6 |
| Qin, P. et al., Nanoscale 6, 1508–1514 (2014) | 2014 | TiO2 | m-Y0.5-TiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 10 | dry air | spiro-OMeTAD | Li+TBP | 11.4 |
| Ramos, F. J. et al., ChemPhysChem 15, 1148–1153 (2014) | 2014 | TiO2 | ZnO-nanocolumn | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PTAA | Li+TBP | 1.3 |
| Ramos, F. J. et al., ChemPhysChem 15, 1148–1153 (2014) | 2014 | TiO2 | ZnO-nanocolumn | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 4.8 |
| Ryu, S. et al., Energy Environ. Sci. 7, 2614–2618 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin 2-3 | toluene | DMF+GBL | na | na | na | PIF8-TAA | Li+TBP | 6.7 |
| Ryu, S. et al., Energy Environ. Sci. 7, 2614–2618 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin 2-3 | toluene | DMF+GBL | na | na | na | PF8-TAA | Li+TBP | 6 |
| Ryu, S. et al., Energy Environ. Sci. 7, 2614–2618 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+GBL | na | na | na | PIF8-TAA | Li+TBP | 9.1 |
| Ryu, S. et al., Energy Environ. Sci. 7, 2614–2618 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+GBL | na | na | na | PF8-TAA | Li+TBP | 4.6 |
| Ryu, S. et al., Energy Environ. Sci. 7, 2614–2618 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin 2-3 | toluene | DMF+GBL | na | na | na | PTAA | Li+TBP | 5.9 |
| Ryu, S. et al., Energy Environ. Sci. 7, 2614–2618 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+GBL | na | na | na | PTAA | Li+TBP | 16.2 |
| Sarkar, A. et al., J. Phys. Chem. C 118, 16688–16693 (2014) | 2014 | TiO2 | mTiO2 | MAPb(I0.9Br0.1)3 | one-step | spin 2-3 | no | GBL | 100 | 10 | na | PTAA | no | 12.8 |
| Shi, J. et al., Appl. Phys. Lett. 104, 063901 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 10.5 |
| Shi, J. et al., ACS Appl. Mater. Interfaces 6, 9711–9718 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | no | no | 10.5 |
| Son, D.-Y. et al., J. Phys. Chem. C 118, 16567–16573 (2014) | 2014 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10 |
| Son, D.-Y. et al., J. Phys. Chem. C 118, 16567–16573 (2014) | 2014 | ZnO | ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.1 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 1.4 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mAl2O3 | MAPbBr3-xClx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 3.2 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3-xClx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 2.9 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 6.5 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xBrx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 4.5 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xBrx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 2.9 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 11.1 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 12.5 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 10.9 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | 0 | MAPb(I1-xBrx)3-yCly | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 3.9 |
| Suarez, B. et al., J. Phys. Chem. Lett. 5, 1628–1635 (2014) | 2014 | TiO2 | mTiO2 | MAPb(I1-xBrx)3-yCly | one-step | spin | no | GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 9.1 |
| Wang, J. T. W. et al., Nano Lett. 14, 724–730 (2014) | 2014 | 0 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 3.7 |
| Wang, J. T. W. et al., Nano Lett. 14, 724–730 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 14.1 |
| Wang, J. T. W. et al., Nano Lett. 14, 724–730 (2014) | 2014 | TiO2-graphene | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 15.6 |
| Wang, J. T. W. et al., Nano Lett. 14, 724–730 (2014) | 2014 | graphene | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 5.9 |
| Wang, X. et al., Mater. Sci. Semicond. Process. 27, 569–576 (2014) | 2014 | 0 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | na | P3HT | Li+TBP | 1.3 |
| Wang, X. et al., Mater. Sci. Semicond. Process. 27, 569–576 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | na | P3HT | Li+TBP | 3.2 |
| Wang, J. et al., Chem. Commun. 50, 5829 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 30 | na | 2TPA-2-DP | no | 9.1 |
| Wang, J. et al., Chem. Commun. 50, 5829 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 10.2 |
| Wojciechowski, K. et al., Energy Environ. Sci. 7, 1142–1147 (2014) | 2014 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 15.9 |
| Wu, Y. et al., Appl. Phys. Express 7, 052301 (2014) | 2014 | 0 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 0.3 |
| Wu, Y. et al., Appl. Phys. Express 7, 052301 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.6 |
| Xiao, M. et al., Angew. Chemie 126, 10056–10061 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 16.2 |
| Xiao, M. et al., Angew. Chemie 126, 10056–10061 (2014) | 2014 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 1.8 |
| Xiao, J. et al., RSC Adv. 4, 32918 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PNBA | no | 11.4 |
| Xu, Y. et al., ACS Appl. Mater. Interfaces 6, 5651–5656 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | no | no | 6.7 |
| Xu, Y. et al., ACS Appl. Mater. Interfaces 6, 5651–5656 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | no | no | 5.7 |
| Yella, A. et al., Nano Lett. 14, 2591–2596 (2014) | 2014 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.7 |
| Zhang, H. et al., Chem. Commun. 50, 5020 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | no | 4 |
| Zhang, H. et al., Chem. Commun. 50, 5020 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 8.4 |
| Zhang, H. et al., Chem. Commun. 50, 5020 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | BuPyIm-TFSI | 8.2 |
| Zhang, F. et al., ACS Appl. Mater. Interfaces 6, 16140–16146 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | na | no | no | 8.3 |
| Zhao, Y. et al., Appl. Phys. Lett. 104, 213906 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | no | no | 0 |
| Zhao, Y. et al., Appl. Phys. Lett. 104, 213906 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 12.4 |
| Zhao, Y. et al., Appl. Phys. Lett. 104, 213906 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 12 |
| Zhao, Y. et al., Appl. Phys. Lett. 104, 213906 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 11.4 |
| Zhao, Y. et al., Appl. Phys. Lett. 104, 213906 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 0 |
| Zhao, Y. et al., Faraday Discuss. 176, 301–312 (2014) | 2014 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin | no | DMF | 100 | 5 | ambient | spiro-OMeTAD | Li+TBP | 4.1 |
| Zhao, Y. et al., Faraday Discuss. 176, 301–312 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 5 | ambient | spiro-OMeTAD | Li+TBP | 9.2 |
| Zhao, Y. et al., Faraday Discuss. 176, 301–312 (2014) | 2014 | TiO2 | mTiO2 | MAPbI2Br | one-step | spin | no | DMF | 100 | 5 | ambient | spiro-OMeTAD | Li+TBP | 6.8 |
| Zhao, Y. et al., Faraday Discuss. 176, 301–312 (2014) | 2014 | TiO2 | mTiO2 | MAPbIBr2 | one-step | spin | no | DMF | 100 | 5 | ambient | spiro-OMeTAD | Li+TBP | 4.7 |
| Zheng, L. et al., Chem. Commun. 50, 11196–11199 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | DR3TBDTT-PDMS | no | 8.8 |
| Zheng, L. et al., Chem. Commun. 50, 11196–11199 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | DR3TBDTT | no | 4.9 |
| Zheng, L. et al., Chem. Commun. 50, 11196–11199 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | DR3TBDTT | Li+TBP | 3.7 |
| Zheng, L. et al., Chem. Commun. 50, 11196–11199 (2014) | 2014 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.9 |
| Zhou, H. et al., J. Phys. Chem. Lett. 5, 3241–3246 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 9.1 |
| Zhou, H. et al., Science 345, 542-546 (2014) | 2014 | TiO2-Y | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | ambient | spiro-OMeTAD | Li+TBP | 19.3 |
| Zhu, Z. et al., J. Am. Chem. Soc. 136, 3760–3763 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 8.8 |
| Zhu, Z. et al., J. Am. Chem. Soc. 136, 3760–3763 (2014) | 2014 | TiO2 | mTiO2-GQDs | MAPbI3 | one-step | spin | no | GBL | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 10.2 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 20 | na | TFB | Li+TBP | 10.9 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 20 | na | PFB | Li+TBP | 8 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 20 | na | PFO | Li+TBP | 1.2 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | TFB | Li+TBP | 12.8 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PFB | Li+TBP | 8.8 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PFO | Li+TBP | 1.6 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 9.8 |
| Zhu, Z. et al., Adv. Funct. Mater. 24, 7357–7365 (2014) | 2014 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.6 |
| Adli, H. K. et al., J. Phys. Chem. C 119, 22304–22309 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.8 |
| Aharon, S. et al., J. Mater. Chem. A 3, 9171–9178 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 7.7 |
| Aharon, S. et al., J. Mater. Chem. A 3, 9171–9178 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 3.9 |
| Ahn, N. et al., J. Am. Chem. Soc. 137, 8696–8699 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 19.7 |
| Bansode, U. et al., J. Phys. Chem. C 119, 9177–9185 (2015) | 2015 | ZnO | 0 | MAPbI3-xClx | one-step | PLD | no | na | na | na | na | spiro-OMeTAD | Li+TBP | 7.7 |
| Bera, A. et al., ACS Appl. Mater. Interfaces 7, 12404–12411 (2015) | 2015 | Zn2SnO4 | mZn2SnO4 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 13.3 |
| Bera, A. et al., ACS Appl. Mater. Interfaces 7, 12404–12411 (2015) | 2015 | TiO2 | mZn2SnO4 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 7.1 |
| Bi, H. and Zhang, Y., Mater. Lett. 161, 767–769 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 30 | glovebox | PCBM | no | 5.1 |
| Bi, H. and Zhang, Y., Mater. Lett. 161, 767–769 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 30 | glovebox | PCBM | Li+TBP | 9.7 |
| Bi, D. et al., ACS Photonics 2, 589–594 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.9 |
| Bu, L. et al., ACS Appl. Mater. Interfaces 7, 17776–17781 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.4 |
| Bu, L. et al., ACS Appl. Mater. Interfaces 7, 17776–17781 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.1 |
| Cai, B. et al., Chinese J. Catal. 36, 1183–1190 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 7.9 |
| Cai, B. et al., Cuihua Xuebao/Chinese J. Catal. 36, 1183–1190 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 16.5 |
| Cai, B. et al., Chinese J. Catal. 36, 1183–1190 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 15.1 |
| Cai, B. et al., Chinese J. Catal. 36, 1183–1190 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 14.1 |
| Cai, B. et al., Chinese J. Catal. 36, 1183–1190 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 9 |
| Cao, D. H. et al., J. Am. Chem. Soc. 137, 7843–7850 (2015) | 2015 | TiO2 | mTiO2 | (CH3(CH2)3NH3)2(MA)2Pb3I10 | one-step | spin | no | DMF | 70 | 30 | na | no | no | 3.5 |
| Cao, D. H. et al., J. Am. Chem. Soc. 137, 7843–7850 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 2.4 |
| Cao, D. H. et al., J. Am. Chem. Soc. 137, 7843–7850 (2015) | 2015 | TiO2 | mTiO2 | (CH3(CH2)3NH3)2(MA)2Pb3I10 | one-step | spin | no | DMF | 70 | 30 | na | spiro-OMeTAD | Li+TBP | 4 |
| Cao, K. et al., Nano Energy 17, 171–179 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3 | two-step | infiltration-dip | no | DMF | - | - | - | no | no | 15 |
| Cao, K. et al., Nano Energy 17, 171–179 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3 | two-step | infiltration-dip | no | DMF | - | - | - | no | no | 11.2 |
| Cao, J. et al., J. Am. Chem. Soc. 137, 10914–10917 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | TSHBC | no | 12.8 |
| Cao, J. et al., J. Am. Chem. Soc. 137, 10914–10917 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | TSHBC | graphene | 14 |
| Casaluci, S. et al., J. Power Sources 297, 504–510 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.7 |
| Casaluci, S. et al., J. Power Sources 297, 504–510 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10 |
| Casaluci, S. et al., J. Power Sources 297, 504–510 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 11 |
| Chang, C. Y. et al., ACS Appl. Mater. Interfaces 7, 4955–4961 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 10.6 |
| Chang, C. Y. et al., ACS Appl. Mater. Interfaces 7, 4955–4961 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+PEG | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 13.2 |
| Chen, H. et al., Nano Energy 15, 216–226 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 10.4 |
| Chen, H. et al., Nano Energy 15, 216–226 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | electrodeposition-dip | no | na | - | - | - | no | no | 10.2 |
| Chen, B. et al., Nano Energy 13, 582–591 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 0.3 |
| Chen, B. et al., Nano Energy 13, 582–591 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 13.5 |
| Chen, B. et al., Nano Energy 13, 582–591 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 13 |
| Cheng, Y. et al., ACS Appl. Mater. Interfaces 7, 19986–19993 (2015) | 2015 | ZnO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 2.9 |
| Cheng, Y. et al., ACS Appl. Mater. Interfaces 7, 19986–19993 (2015) | 2015 | ZnO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5.4 |
| Cheng, Y. et al., ACS Appl. Mater. Interfaces 7, 19986–19993 (2015) | 2015 | ZnO | PEI | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| Cheng, Y. et al., ACS Appl. Mater. Interfaces 7, 19986–19993 (2015) | 2015 | ZnO | PCBM | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.4 |
| Cheng, M. et al., Chem. Mater. 27, 1808–1814 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | POZ2 | no | 12.8 |
| Cheng, M. et al., Chem. Mater. 27, 1808–1814 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | POZ3 | no | 11.5 |
| Cheng, M. et al., Chem. Mater. 27, 1808–1814 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.8 |
| Dao, V. D. et al., Thin Solid Films 593, 10–16 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 2.3 |
| Dao, V. D. et al., Thin Solid Films 593, 10–16 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 5.2 |
| Das, S. et al., ACS Photonics 2, 680–686 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 13 |
| Das, S. et al., ACS Photonics 2, 680–686 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spray | no | DMF | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 13 |
| Dong, Q. et al., J. Phys. Chem. C 119, 10212–10217 (2015) | 2015 | SnO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 7.3 |
| Dong, Q. et al., J. Phys. Chem. C 119, 10212–10217 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 13.9 |
| Du, T. et al., ACS Appl. Mater. Interfaces 7, 3382–3388 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5.8 |
| Du, T. et al., ACS Appl. Mater. Interfaces 7, 3382–3388 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.1 |
| Fakharuddin, A. et al., J. Power Sources 283, 61–67 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 12.1 |
| Fakharuddin, A. et al., J. Power Sources 283, 61–67 (2015) | 2015 | TiO2 | TiO2-nanorod | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 12.2 |
| Fakharuddin, A. et al., ACS Nano 9, 8420–8429 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 5.8 |
| Fakharuddin, A. et al., ACS Nano 9, 8420–8429 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 7.9 |
| Fakharuddin, A. et al., ACS Nano 9, 8420–8429 (2015) | 2015 | 0 | TiO2-nanorod | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 10.5 |
| Gamliel, S. et al., J. Phys. Chem. C 119, 19722–19728 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spray | no | DMF | 80 | 40 | glovebox | no | no | 6.9 |
| Della Gaspera, E. et al., Nano Energy 13, 249–257 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.6 |
| Della Gaspera, E. et al., Nano Energy 13, 249–257 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 1.2 |
| Di Giacomo, F. et al., Adv. Energy Mater. 5, 1401808 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 7 |
| Di Giacomo, F. et al., Adv. Energy Mater. 5, 1401808 (2015) | 2015 | 0 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 2.2 |
| Di Giacomo, F. et al., Adv. Energy Mater. 5, 1401808 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 9.9 |
| Gu, Z. et al., Sol. Energy Mater. Sol. Cells 140, 396–404 (2015) | 2015 | 0 | CdS-nanorod | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | no | no | 0 |
| Gu, Z. et al., Sol. Energy Mater. Sol. Cells 140, 396–404 (2015) | 2015 | 0 | CdS-nanorod | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | P3HT | no | 1 |
| Gu, Z. et al., Sol. Energy Mater. Sol. Cells 140, 396–404 (2015) | 2015 | 0 | CdS-nanorod | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 8.4 |
| Guarnera, S. et al., J. Phys. Chem. Lett. 6, 432–437 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | H-TFSI+Et4N-TFSI | 10.3 |
| Guarnera, S. et al., J. Phys. Chem. Lett. 6, 432–437 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | H-TFSI+Et4N-TFSI+Al2o3 | 13.1 |
| Han, G. S. et al., ACS Appl. Mater. Interfaces 7, 23521–23526 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Han, G. S. et al., ACS Appl. Mater. Interfaces 7, 23521–23526 (2015) | 2015 | TiO2 | mTiO2-Rgo | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.5 |
| Han, G. S. et al., J. Mater. Chem. A 3, 9160–9164 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.7 |
| Han, G. S. et al., J. Mater. Chem. A 3, 9160–9164 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.4 |
| Hao, F. et al., J. Am. Chem. Soc. 137, 11445–11452 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 5.8 |
| Hao, F. et al., J. Am. Chem. Soc. 137, 11445–11452 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMSO+SnF2 | 100 | 15 | glovebox | no | no | 3.2 |
| Heo, J. H. et al., Nano Energy 15, 530–539 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | PTAA | Li+TBP | 5.7 |
| Heo, J. H. et al., Nano Energy 15, 530–539 (2015) | 2015 | TiO2-Li | 0 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | PTAA | Li+TBP | 5 |
| Heo, J. H. et al., Nano Energy 15, 530–539 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | PTAA | Li+TBP | 3.2 |
| Heo, J. H. et al., Nano Energy 15, 530–539 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | PTAA | Li+TBP | 15.7 |
| Heo, J. H. et al., Nano Energy 15, 530–539 (2015) | 2015 | TiO2 | mTiO2-Li | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 2 | na | PTAA | Li+TBP | 17.2 |
| Hong, S. et al., Curr. Appl. Phys. 15, 574–579 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.8 |
| Hou, Y. et al., Adv. Energy Mater. 5, 1500543 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | ambient | PEDOT | no | 14.2 |
| Hou, Y. et al., Adv. Energy Mater. 5, 1500543 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 16.4 |
| Hou, Y. et al., Adv. Energy Mater. 5, 1500543 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 10 | ambient | PEDOT | no | 11.2 |
| Huang, W. et al., Adv. Funct. Mater. 25, 5529–5536 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14.3 |
| Huang, W. et al., Adv. Funct. Mater. 25, 5529–5536 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 12 |
| Huang, L. et al., Sol. Energy Mater. Sol. Cells 141, 377–382 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 13.6 |
| Huang, L. et al., Sol. Energy Mater. Sol. Cells 141, 377–382 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 8.7 |
| Huangfu, M. et al., Appl. Surf. Sci. 357, 2234–2240 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 30 | glovebox | CuI | no | 5.8 |
| Hwang, K. et al., Adv. Mater. 27, 1241–1247 (2015) | 2015 | ZnO | 0 | MAPbI3 | two-step | slot-die | no | DMF | - | - | - | P3HT | Li+TBP | 12 |
| Hwang, I. et al., ACS Appl. Mater. Interfaces 7, 17330–17336 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.8 |
| Hwang, I. et al., ACS Appl. Mater. Interfaces 7, 17330–17336 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.3 |
| Ito, S. et al., J. Phys. Chem. Lett. 6, 881–886 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | CuSCN | no | 7.2 |
| Ito, S. et al., J. Phys. Chem. Lett. 6, 881–886 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | CuSCN | no | 12 |
| Ito, S. et al., J. Phys. Chem. Lett. 6, 881–886 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | CuSCN | no | 0.1 |
| Ito, S. et al., J. Phys. Chem. Lett. 6, 881–886 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | CuSCN | no | 9.9 |
| Jeon, N. J. et al., Nature 517, 476–480 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PTAA | Li+TBP | 19 |
| Jeong, I. et al., Nano Energy 17, 131–139 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Jiang, C. et al., ACS Appl. Mater. Interfaces 7, 24726–24732 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.8 |
| Jiang, C. et al., ACS Appl. Mater. Interfaces 7, 24726–24732 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.6 |
| Jin, Y. and Chumanov, G., ACS Appl. Mater. Interfaces 7, 12015–12021 (2015) | 2015 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 10.2 |
| Kang, M. S. et al., ACS Appl. Mater. Interfaces 7, 22213–22217 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | SGT-411 | Li+TBP+FK209 | 13 |
| Kang, M. S. et al., ACS Appl. Mater. Interfaces 7, 22213–22217 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | SGT-41no | Li+TBP+FK209 | 12.6 |
| Kang, M. S. et al., ACS Appl. Mater. Interfaces 7, 22213–22217 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | SGT-4no9 | Li+TBP+FK209 | 11 |
| Kang, M. S. et al., ACS Appl. Mater. Interfaces 7, 22213–22217 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 13.8 |
| Ke, W. et al., J. Am. Chem. Soc. 137, 6730–6733 (2015) | 2015 | SnO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 17.2 |
| Ke, W. et al., J. Am. Chem. Soc. 137, 6730–6733 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 15.2 |
| Kim, G. Y. et al., J. Phys. Chem. Lett. 6, 2355–2362 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 10.6 |
| Kim, G. Y. et al., J. Phys. Chem. Lett. 6, 2355–2362 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xBrx | one-step | spin | no | DMSO+GBL | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 13.6 |
| Lee, J. W. et al., Adv. Energy Mater. 5, 1501310 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 17.4 |
| Lee, J. W. et al., Adv. Energy Mater. 5, 1501310 (2015) | 2015 | TiO2 | 0 | FA0.9Cs0.1PbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 19 |
| Li, F. et al., Mater. Lett. 157, 38–41 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| Li, F. et al., Mater. Lett. 157, 38–41 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.5 |
| Li, W. et al., J. Am. Chem. Soc. 137, 10399–10405 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.6 |
| Li, W. et al., J. Am. Chem. Soc. 137, 10399–10405 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.2 |
| Li, Y. et al., J. Phys. Chem. Lett. 6, 493–499 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.8 |
| Li, Y. et al., J. Phys. Chem. Lett. 6, 493–499 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.1 |
| Li, Y. et al., J. Phys. Chem. Lett. 6, 493–499 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.8 |
| Li, Y. et al., J. Phys. Chem. Lett. 6, 493–499 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3.4 |
| Li, Y. et al., RSC Adv. 5, 28424–28429 (2015) | 2015 | SnO2 | mSnO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.8 |
| Li, Y. et al., J. Am. Chem. Soc. 137, 15540–15547 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.4 |
| Li, Y. et al., J. Am. Chem. Soc. 137, 15540–15547 (2015) | 2015 | TiO2 | PCBB-2CN-2C8 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.4 |
| Li, C. et al., ACS Appl. Mater. Interfaces 7, 15117–15122 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 10.7 |
| Li, C. et al., ACS Appl. Mater. Interfaces 7, 15117–15122 (2015) | 2015 | TiO2-NS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 10.7 |
| Listorti, A. et al., J. Phys. Chem. Lett. 6, 1628–1637 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | na | ambient | spiro-OMeTAD | Li+TBP | 9.3 |
| Listorti, A. et al., J. Phys. Chem. Lett. 6, 1628–1637 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | na | ambient | spiro-OMeTAD | Li+TBP | 9.8 |
| Listorti, A. et al., J. Phys. Chem. Lett. 6, 1628–1637 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | na | ambient | spiro-OMeTAD | Li+TBP | 8.7 |
| Liu, D. et al., ACS Appl. Mater. Interfaces 7, 16330–16337 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin-TSA | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 14.1 |
| Liu, D. et al., ACS Appl. Mater. Interfaces 7, 16330–16337 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin-OTA | no | DMF | 90 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 9 |
| Liu, D. et al., ACS Appl. Mater. Interfaces 7, 16330–16337 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin-OSA | no | DMF | 90 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 10.2 |
| Liu, J. et al., J. Phys. Chem. Lett. 6, 1666–1673 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | no | no | 6.5 |
| Liu, J. et al., J. Phys. Chem. Lett. 6, 1666–1673 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | PEDOT | no | 14.5 |
| Liu, J. et al., J. Phys. Chem. Lett. 6, 1666–1673 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 12.6 |
| Liu, C. et al., ACS Appl. Mater. Interfaces 7, 1153–1159 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | P3HT | no | 7.1 |
| Liu, C. et al., ACS Appl. Mater. Interfaces 7, 1153–1159 (2015) | 2015 | TiO2 | PCBM | MAPbI3 | two-step | spin | no | DMF | - | - | - | P3HT | no | 14.6 |
| Liu, C. et al., ACS Appl. Mater. Interfaces 7, 1153–1159 (2015) | 2015 | TiO2 | PCBM | MAPbI3 | two-step | spin | no | DMF | - | - | - | P3HT | no | 13.2 |
| Liu, C. et al., ACS Appl. Mater. Interfaces 7, 9066–9071 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| Liu, C. et al., ACS Appl. Mater. Interfaces 7, 9066–9071 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 7.7 |
| Liu, J. et al., J. Mater. Chem. A 3, 11750–11755 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 12.8 |
| Liu, J. et al., J. Mater. Chem. A 3, 11750–11755 (2015) | 2015 | CdS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 11.2 |
| Liu, J. et al., J. Mater. Chem. A 3, 11750–11755 (2015) | 2015 | ZnS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 1 |
| Liu, J. et al., J. Mater. Chem. A 3, 11750–11755 (2015) | 2015 | no | no | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 3.6 |
| Liu, Z. et al., Dalt. Trans. 44, 3967–3973 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | mNiO | no | 11.4 |
| Liu, Z. et al., Dalt. Trans. 44, 3967–3973 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | ZrO2 | no | 8.2 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | RGO-1 | no | 9.3 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | RGO-2 | no | 8.3 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | RGO-3 | no | 7 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | GO | no | 5.5 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 5.9 |
| Luo, Q. et al., J. Mater. Chem. A 3, 15996–16004 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.3 |
| Luo, P. et al., ACS Appl. Mater. Interfaces 7, 2708–2714 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3.6 |
| Luo, P. et al., ACS Appl. Mater. Interfaces 7, 2708–2714 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.5 |
| Luo, P. et al., ACS Appl. Mater. Interfaces 7, 2708–2714 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.7 |
| Lv, M. et al., ACS Appl. Mater. Interfaces 7, 17482–17488 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 5.7 |
| Lv, M. et al., ACS Appl. Mater. Interfaces 7, 17482–17488 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | CuInS2/ZnS | no | 8.4 |
| Lv, M. et al., ACS Appl. Mater. Interfaces 7, 17482–17488 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | CuInS2 | no | 6.6 |
| Lv, M. et al., ACS Appl. Mater. Interfaces 7, 17482–17488 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.9 |
| Ma, Y. et al., ACS Appl. Mater. Interfaces 7, 6406–6411 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | no | no | 3.4 |
| Ma, Y. et al., ACS Appl. Mater. Interfaces 7, 6406–6411 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | TPD | no | 7.1 |
| Ma, Y. et al., ACS Appl. Mater. Interfaces 7, 6406–6411 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF | - | - | - | TPD | no | 3.2 |
| Mahmood, K. et al., Adv. Energy Mater. 5, 1500568 (2015) | 2015 | ZnO | N-ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.2 |
| Mahmood, K. et al., Adv. Energy Mater. 5, 1500568 (2015) | 2015 | ZnO | ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Mali, S. S. et al., Chem. Mater. 27, 1541–1551 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | spiro-OMeTAD | Li+TBP | 10 |
| Mali, S. S. et al., Chem. Mater. 27, 1541–1551 (2015) | 2015 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | spiro-OMeTAD | Li+TBP | 13.8 |
| Mali, S. S. et al., Chem. Mater. 27, 1541–1551 (2015) | 2015 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | spiro-OMeTAD | Li+TBP | 10 |
| Matteocci, F. et al., ACS Appl. Mater. Interfaces 7, 26176–26183 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 7.4 |
| Matteocci, F. et al., ACS Appl. Mater. Interfaces 7, 26176–26183 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | blade-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.9 |
| Matteocci, F. et al., ACS Appl. Mater. Interfaces 7, 26176–26183 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.3 |
| Matteocci, F. et al., ACS Appl. Mater. Interfaces 7, 26176–26183 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.7 |
| Nejand, B. A. et al., ACS Appl. Mater. Interfaces 7, 21807–21818 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | NiOx | no | 1.3 |
| Nejand, B. A. et al., ACS Appl. Mater. Interfaces 7, 21807–21818 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | spiro-OMeTAD | Li+TBP | 8.2 |
| Peng, Y. et al., J. Mater. Chem. A 3, 12436–12442 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.1 |
| Raga, S. R. et al., Chem. Mater. 27, 1597–1603 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 115 | 45 | ambient | spiro-OMeTAD | Li+TBP | 12.5 |
| Raga, S. R. et al., Chem. Mater. 27, 1597–1603 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 45 | ambient | spiro-OMeTAD | Li+TBP | 9 |
| Raga, S. R. et al., Chem. Mater. 27, 1597–1603 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 125 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 8.7 |
| Raga, S. R. et al., Chem. Mater. 27, 1597–1603 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 115 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 12.1 |
| Raga, S. R. et al., Chem. Mater. 27, 1597–1603 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 8.3 |
| Rakstys, K. et al., J. Am. Chem. Soc. 137, 16172–16178 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3) | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | KR131 | Li+TBP+FK209 | 18.3 |
| Rakstys, K. et al., J. Am. Chem. Soc. 137, 16172–16178 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3) | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | KR133 | Li+TBP+FK209 | 16.8 |
| Rakstys, K. et al., J. Am. Chem. Soc. 137, 16172–16178 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3) | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | KR145 | Li+TBP+FK209 | 11.9 |
| Rakstys, K. et al., J. Am. Chem. Soc. 137, 16172–16178 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3) | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | KR122 | Li+TBP+FK209 | 9 |
| Rakstys, K. et al., J. Am. Chem. Soc. 137, 16172–16178 (2015) | 2015 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3) | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.9 |
| Razza, S. et al., J. Power Sources 277, 286–291 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | blade-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.3 |
| Razza, S. et al., J. Power Sources 277, 286–291 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13 |
| Sabba, D. et al., J. Phys. Chem. C 119, 1763–1767 (2015) | 2015 | TiO2 | mTiO2 | CsSnI2.9Br0.1 | one-step | spin | no | DMSO+SnF2 | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 1.8 |
| Sabba, D. et al., J. Phys. Chem. C 119, 1763–1767 (2015) | 2015 | TiO2 | mTiO2 | CsSnI3 | one-step | spin | no | DMSO+SnF2 | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 1.7 |
| Sabba, D. et al., J. Phys. Chem. C 119, 1763–1767 (2015) | 2015 | TiO2 | mTiO2 | CsSnBr3 | one-step | spin | no | DMSO+SnF2 | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 1 |
| Seol, D. J. et al., ChemSusChem 8, 2414–2419 (2015) | 2015 | TiO2 | 0 | FAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.2 |
| Sepalage, G. A. et al., Adv. Funct. Mater. 25, 5650–5661 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | CuI | no | 7.5 |
| Sepalage, G. A. et al., Adv. Funct. Mater. 25, 5650–5661 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | CuI | no | 1.1 |
| Sepalage, G. A. et al., Adv. Funct. Mater. 25, 5650–5661 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 15.8 |
| Sepalage, G. A. et al., Adv. Funct. Mater. 25, 5650–5661 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 10.1 |
| Sfyri, G. et al., Sol. Energy Mater. Sol. Cells 134, 60–63 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 30 | ambient | spiro-OMeTAD | no | 2.8 |
| Shen, P. S. et al., Sol. Energy 120, 345–356 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 110 | 10 | na | spiro-OMeTAD | Li+TBP | 11.8 |
| Shi, Y. et al., J. Phys. Chem. C 119, 15868–15873 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 12.7 |
| Shi, Y. et al., J. Phys. Chem. C 119, 15868–15873 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 100 | 45 | na | spiro-OMeTAD | Li+TBP | 7.9 |
| Shi, Y. et al., J. Phys. Chem. C 119, 15868–15873 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.8 |
| Shi, Y. et al., J. Phys. Chem. C 119, 15868–15873 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.1 |
| Son, D. Y. et al., J. Phys. Chem. C 119, 10321–10328 (2015) | 2015 | 0 | ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.4 |
| Son, D. Y. et al., J. Phys. Chem. C 119, 10321–10328 (2015) | 2015 | 0 | ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.7 |
| Song, D. et al., J. Phys. Chem. C 119, 22812–22819 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16.4 |
| Song, D. et al., J. Phys. Chem. C 119, 22812–22819 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.5 |
| Song, D. et al., J. Phys. Chem. C 119, 22812–22819 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16 |
| Song, D. et al., J. Phys. Chem. C 119, 22812–22819 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 15.4 |
| Song, D. et al., J. Phys. Chem. C 119, 22812–22819 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 6 |
| Song, T. B. et al., Nano Energy 12, 494–500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 110 | dry air | spiro-OMeTAD | Li+TBP | 12.9 |
| Song, T. B. et al., Nano Energy 12, 494–500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | dry air | spiro-OMeTAD | Li+TBP | 13.9 |
| Song, T. B. et al., Nano Energy 12, 494–500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 70 | dry air | spiro-OMeTAD | Li+TBP | 14.1 |
| Song, T. B. et al., Nano Energy 12, 494–500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 55 | dry air | spiro-OMeTAD | Li+TBP | 14 |
| Song, T. B. et al., Nano Energy 12, 494–500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 40 | dry air | spiro-OMeTAD | Li+TBP | 13 |
| Sun, H. et al, Solid State Sci. 40, 60–66 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 30 | na | no | no | 3.5 |
| Sun, H. et al, Solid State Sci. 40, 60–66 (2015) | 2015 | TiO2 | S@STiO2 | MAPbI3 | one-step | spin | no | GBL | 100 | 30 | na | no | no | 4.3 |
| Sun, C. et al., Sol. Energy Mater. Sol. Cells 143, 360–368 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.9 |
| Sung, S. et al., Nanoscale 7, 8898–8906 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.2 |
| Tao, H. et al., J. Power Sources 290, 144–152 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.6 |
| Tao, H. et al., J. Power Sources 290, 144–152 (2015) | 2015 | 0 | TiO2-nanowire | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.8 |
| Tripathi, B. et al.,Sol. Energy Mater. Sol. Cells 132, 615–622 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | na | ambient | no | no | 1.1 |
| Tripathi, B. et al.,Sol. Energy Mater. Sol. Cells 132, 615–622 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | na | ambient | no | no | 0.9 |
| Tripathi, B. et al.,Sol. Energy Mater. Sol. Cells 132, 615–622 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | na | ambient | no | no | 0.3 |
| Wang, Z. et al., Chem. Mater. 27, 7149–7155 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 + FACl | one-step | spin | no | DMF | 140 | na | na | spiro-OMeTAD | Li+TBP | 13.7 |
| Wang, Z. et al., Chem. Mater. 27, 7149–7155 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | no | DMF | 140 | na | na | spiro-OMeTAD | Li+TBP | 0.2 |
| Wang, Z. et al., Chem. Mater. 27, 7149–7155 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | no | DMF+MACl | 140 | na | na | spiro-OMeTAD | Li+TBP | 7 |
| Wang, Z. et al., Chem. Mater. 27, 7149–7155 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | no | DMF+NH4Cl | 140 | na | na | spiro-OMeTAD | Li+TBP | 0.6 |
| Wang, M. et al., Chem. Phys. Lett. 639, 283–288 (2015) | 2015 | ZnO | ZnO-nanorod | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 6.6 |
| Wang, M. et al., Chem. Phys. Lett. 639, 283–288 (2015) | 2015 | ZnO | ZnO-nanorod | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 4.3 |
| Wang, J. Y. et al., ACS Appl. Mater. Interfaces 7, 27676–27684 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | P3HT | no | 10.7 |
| Wang, J. Y. et al., ACS Appl. Mater. Interfaces 7, 27676–27684 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | P3HT | no | 8.7 |
| Wang, H. et al., ACS Photonics 2, 849–855 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | Rno1 | Li+TBP | 7.5 |
| Wang, H. et al., ACS Photonics 2, 849–855 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 7.7 |
| Wang, H. et al., ACS Photonics 2, 849–855 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | Rno1 | Li+TBP+MY11 | 12 |
| Wang, H. et al., ACS Photonics 2, 849–855 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | spiro-OMeTAD | Li+TBP+MY11 | 12.2 |
| Wang, F. et al., Adv. Funct. Mater. 25, 1120–1126 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 6.1 |
| Wang, F. et al., Adv. Funct. Mater. 25, 1120–1126 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+HCl | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 17.5 |
| Wang, F. et al., Adv. Funct. Mater. 25, 1120–1126 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+HI | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 12.4 |
| Wang, K. et al., J. Phys. Chem. Lett. 6, 755–759 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 9.6 |
| Wang, K. et al., J. Phys. Chem. Lett. 6, 755–759 (2015) | 2015 | Wox | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 9.4 |
| Wei, H. et al., Carbon 93, 861–868 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | no | no | 13.5 |
| Wei, H. et al., Carbon 93, 861–868 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | DMF | - | - | - | no | no | 10.7 |
| Werner, J. et al., Sol. Energy Mater. Sol. Cells 141, 407–413 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 12.2 |
| Werner, J. et al., Sol. Energy Mater. Sol. Cells 141, 407–413 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 10.4 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | C60 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 13.5 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 13.9 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | C60 | 0 | MAPbI3-xClx | two-step | evap-spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.5 |
| Wojciechowski, K. et al., J. Phys. Chem. Lett. 6, 2399–2405 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | evap-spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.6 |
| Wozny, S. et al., Chem. Mater. 27, 4814–4820 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | toluene | DMF | 170 | 10 | ambient | spiro-OMeTAD | Li+TBP | 13.5 |
| Wozny, S. et al., Chem. Mater. 27, 4814–4820 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | toluene | DMF | 170 | 10 | ambient | spiro-OMeTAD | Li+TBP | 13 |
| Wozny, S. et al., Chem. Mater. 27, 4814–4820 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | toluene | DMF | 170 | 10 | ambient | spiro-OMeTAD | Li+TBP | 10.3 |
| Wozny, S. et al., Chem. Mater. 27, 4814–4820 (2015) | 2015 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | toluene | DMF | 170 | 10 | dry air | spiro-OMeTAD | Li+TBP | 16.6 |
| Wu, Y. et al., ACS Appl. Mater. Interfaces 7, 20707–20713 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 16 |
| Wu, N. et al., Appl. Surf. Sci. 357, 2372–2377 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.1 |
| Xia, X. et al., ACS Appl. Mater. Interfaces 7, 16907–16912 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.2 |
| Xie, Y. et al., ACS Appl. Mater. Interfaces 7, 12937–12942 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.4 |
| Xie, Y. et al., ACS Appl. Mater. Interfaces 7, 12937–12942 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.1 |
| Xu, X. et al., Nano Lett. 15, 6514–6520 (2015) | 2015 | TiO2 | 0 | Cl-FAPbI3 | two-step | spin | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15.3 |
| Xu, X. et al., Nano Lett. 15, 6514–6520 (2015) | 2015 | no | no | Cl-FAPbI3 | two-step | spin | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15.5 |
| Yang, Z. et al., Nano Energy 15, 670–678 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-contact | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16 |
| Yang, Y. and Wang, W., J. Power Sources 293, 577–584 (2015) | 2015 | 0 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | glovebox | P3HT | Li+TBP | 4.9 |
| Yang, Y. and Wang, W., J. Power Sources 293, 577–584 (2015) | 2015 | 0 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | glovebox | P3HT | Li+TBP | 1.9 |
| Yang, D. et al.,Energy Environ. Sci. 8, 3208–3214 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 16.2 |
| Yang, W. S. et al., Science 348, 1234–1237 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 | two-step | spin | no | DMF | - | - | - | PTAA | Li+TBP | 15.6 |
| Yang, W. S. et al., Science 348, 1234–1237 (2015) | 2015 | TiO2 | mTiO2 | FAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | PTAA | Li+TBP | 20.1 |
| Yang, L. et al., ACS Appl. Mater. Interfaces 7, 14614–14619 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.4 |
| Yang, L. et al., ACS Appl. Mater. Interfaces 7, 14614–14619 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF+HCl | - | - | - | spiro-OMeTAD | Li+TBP | 15.2 |
| Yang, L. et al., ACS Appl. Mater. Interfaces 7, 14614–14619 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF+HI | - | - | - | spiro-OMeTAD | Li+TBP | 12.2 |
| You, P. et al., Adv. Mater. 27, 3632–3638 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 14.6 |
| You, P. et al., Adv. Mater. 27, 3632–3638 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 12.4 |
| Yu, J. C. et al., Adv. Mater. 27, 3492–3500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 16.3 |
| Yu, J. C. et al., Adv. Mater. 27, 3492–3500 (2015) | 2015 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 12.8 |
| Yue, Y. et al., J. Phys. Chem. C 119, 22847–22854 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 13.1 |
| Yue, Y. et al., J. Phys. Chem. C 119, 22847–22854 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 5.3 |
| Yue, Y. et al., J. Phys. Chem. C 119, 22847–22854 (2015) | 2015 | TiO2 | mTiO2-PMMA | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 14 |
| Yue, Y. et al., J. Phys. Chem. C 119, 22847–22854 (2015) | 2015 | TiO2 | mTiO2-PS | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 8 |
| Zhang, T. et al., Nano Lett. 15, 3959–3963 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.2 |
| Zhang, T. et al., Nano Lett. 15, 3959–3963 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.4 |
| Zhang, J. and Pauporté, T., J. Phys. Chem. C 119, 14919–14928 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | 100 | na | na | spiro-OMeTAD | Li+TBP | 6.7 |
| Zhang, J. and Pauporté, T., J. Phys. Chem. C 119, 14919–14928 (2015) | 2015 | ZnO | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | 100 | na | na | spiro-OMeTAD | Li+TBP | 15 |
| Zhang, J. and Pauporté, T., J. Phys. Chem. C 119, 14919–14928 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | 100 | na | na | spiro-OMeTAD | Li+TBP | 9.4 |
| Zhang, J. and Pauporté, T., J. Phys. Chem. C 119, 14919–14928 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3.8 |
| Zhang, J. and Pauporté, T., J. Phys. Chem. C 119, 14919–14928 (2015) | 2015 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.9 |
| Zhang, J. and Pauporté, T., J. Phys. Chem. C 119, 14919–14928 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.3 |
| Zhang, H. et al., J. Energy Chem. 24, 729–735 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.1 |
| Zhang, M. et al., Chem. Commun. 51, 10038–10041 (2015) | 2015 | TiO2 | 0 | MAPbBr3 | one-step | blowdry | no | DMF | 100 | 10 | ambient | P3HT | no | 10.2 |
| Zhang, M. et al., Chem. Commun. 51, 10038–10041 (2015) | 2015 | TiO2 | 0 | MAPbBr3 | one-step | spin | no | DMF | 100 | 10 | na | P3HT | no | 4.8 |
| Zhang, Z. et al., Sol. Energy 122, 97–103 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+IPA | - | - | - | spiro-OMeTAD | Li+TBP | 12.2 |
| Zhang, Z. et al., Sol. Energy 122, 97–103 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+IPA | - | - | - | spiro-OMeTAD | Li+TBP | 12.5 |
| Zhang, Y. et al., J. Power Sources 274, 1224–1230 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 120 | 30 | glovebox | no | no | 3.5 |
| Zhang, Y. et al., J. Power Sources 274, 1224–1230 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 120 | 30 | glovebox | P3HT | no | 6.1 |
| Zheng, X. et al., Nano Energy 17, 269–278 (2015) | 2015 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin 2-3 | toluene | DMF+DMSO | na | 30 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 8.3 |
| Zheng, Y. C. et al., Chem. Mater. 27, 5116–5121 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | spiro-OMeTAD | Li+TBP | 13.1 |
| Zheng, Y. C. et al., Chem. Mater. 27, 5116–5121 (2015) | 2015 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 1.6 |
| Zhong, D. et al., Nano Energy 11, 409–418 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11 |
| Zhong, D. et al., Nano Energy 11, 409–418 (2015) | 2015 | TiO2 | TiO2-nanocone | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.9 |
| Zhong, D. et al., Nano Energy 11, 409–418 (2015) | 2015 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.1 |
| Zhou, Y. et al., J. Phys. Chem. Lett. 6, 2292–2297 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.1 |
| Zhou, Y. et al., J. Phys. Chem. Lett. 6, 2292–2297 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.8 |
| Zhou, H. et al., J. Phys. Chem. C 119, 4600–4605 (2015) | 2015 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 8.7 |
| Zhu, L. et al., Nano Energy 15, 540–548 (2015) | 2015 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 14 |
| Zhu, L. et al., Nano Energy 15, 540–548 (2015) | 2015 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 17.4 |
| Zuo, L. et al., J. Am. Chem. Soc. 137, 2674–2679 (2015) | 2015 | ZnO | 0 | MAPbI3 | one-step | spin | no | DMF | 80 | 4 | glovebox | spiro-OMeTAD | Li | 12 |
| Zuo, L. et al., J. Am. Chem. Soc. 137, 2674–2679 (2015) | 2015 | ZnO | C3-SAM | MAPbI3 | one-step | spin | no | DMF | 80 | 4 | glovebox | spiro-OMeTAD | Li | 15.7 |
| Adhikari, N. et al., Nanoscale 8, 2693–2703 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.3 |
| Adhikari, N. et al., Nanoscale 8, 2693–2703 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+H2O | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Bae, S. et al., J. Phys. Chem. Lett. 7, 3091–3096 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | na | na | na | spiro-OMeTAD | Li+TBP | 14.3 |
| Bai, S. et al., Electrochim. Acta 190, 775–779 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 12.5 |
| Bai, S. et al., Electrochim. Acta 190, 775–779 (2016) | 2016 | TiO2 | mTiO2 | FAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 7.4 |
| Bai, S. et al., Electrochim. Acta 190, 775–779 (2016) | 2016 | TiO2 | mTiO2 | FAxMA1-xPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 13 |
| Bai, Y. et al., ChemSusChem 9, 2686–2691 (2016) | 2016 | SnO2-Sb | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 17.7 |
| Bai, Y. et al., ChemSusChem 9, 2686–2691 (2016) | 2016 | SnO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 15.7 |
| Behrouznejad, F. et al., J. Mater. Chem. A 4, 13488–13498 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | no | no | 3.1 |
| Behrouznejad, F. et al., J. Mater. Chem. A 4, 13488–13498 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | no | no | 2.6 |
| Behrouznejad, F. et al., J. Mater. Chem. A 4, 13488–13498 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | no | no | 0.2 |
| Behrouznejad, F. et al., J. Mater. Chem. A 4, 13488–13498 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 16.5 |
| Behrouznejad, F. et al., J. Mater. Chem. A 4, 13488–13498 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 16.4 |
| Behrouznejad, F. et al., J. Mater. Chem. A 4, 13488–13498 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 14.7 |
| Besleaga, C. et al., J. Phys. Chem. Lett. 7, 5168–5175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | no | no | 5.9 |
| Besleaga, C. et al., J. Phys. Chem. Lett. 7, 5168–5175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 12 |
| Besleaga, C. et al., J. Phys. Chem. Lett. 7, 5168–5175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 11.6 |
| Bi, D. et al., Sci. Adv. 2, e1501170–e1501170 (2016) | 2016 | TiO2 | mTiO2 | FAI, PbI2, MABr, and PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 90 | na | spiro-OMeTAD | Li+TBP+FK209 | 20.8 |
| Chang, S. et al., ACS Appl. Mater. Interfaces 8, 8511–8519 (2016) | 2016 | IBF-Ep | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 6.9 |
| Chang, S. et al., ACS Appl. Mater. Interfaces 8, 8511–8519 (2016) | 2016 | PCBM | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 2.5 |
| Chaudhary, D. K. et al., RSC Adv. 6, 94731–94738 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 50 | ambient | P3HT | no | 8.1 |
| Chaudhary, D. K. et al., RSC Adv. 6, 94731–94738 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 50 | ambient | P3HT | no | 5.5 |
| Chen, H. N. et al., Adv. Energy Mater. 6, 1502087 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 8.7 |
| Chen, H. N. et al., Adv. Energy Mater. 6, 1502087 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+CYHEX | - | - | - | no | no | 14.4 |
| Chen, X. et al., J. Mater. Chem. A 4, 6521–6526 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.3 |
| Chen, X. et al., J. Mater. Chem. A 4, 6521–6526 (2016) | 2016 | TiO2 | TiO2 flower like | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.7 |
| Chen, L.-C. et al., Mater. Sci. Semicond. Process. 56, 179–182 (2016) | 2016 | graphene | mTiO2 | MAPbI3 | one-step | spin | no | DMSO+GBL | 70 | 30 | na | spiro-OMeTAD | Li+TBP | 6.9 |
| Chen, H. W. et al., Sci. Rep. 6, 34319 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 90 | glovebox | MEH-PPV | no | 9.7 |
| Chen, H. W. et al., Sci. Rep. 6, 34319 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 13.3 |
| Chen, H. W. et al., Sci. Rep. 6, 34319 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 12.3 |
| Chen, H. W. et al., Sci. Rep. 6, 34319 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.4 |
| Chen, B.-X. et al., J. Mater. Chem. A 4, 15662–15669 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | toluene | DMSO | 150 | 10 | na | spiro-OMeTAD | Li+TBP | 5.6 |
| Chen, B.-X. et al., J. Mater. Chem. A 4, 15662–15669 (2016) | 2016 | TiO2 | PS | MAPbI3 | one-step | spin | toluene | DMSO | 150 | 10 | na | spiro-OMeTAD | Li+TBP | 11.7 |
| Cheng, N. et al., J. Power Sources 321, 71–75 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 12.7 |
| Cheng, N. et al., J. Power Sources 321, 71–75 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 9.9 |
| Cheng, N. et al., J. Power Sources 319, 111–115 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin | chlorobenzene | DMF | - | - | - | spiro-OMeTAD | no | 11.6 |
| Cheng, N. et al., J. Power Sources 319, 111–115 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin | ethanol | DMF | - | - | - | spiro-OMeTAD | no | 12.1 |
| Cheng, N. et al., J. Power Sources 319, 111–115 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 10.3 |
| Cheng, N. et al., J. Power Sources 319, 111–115 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin | IPA | DMF | - | - | - | spiro-OMeTAD | no | 11.2 |
| Chiang, Y.-H. et al., ChemSusChem 9, 2620–2627 (2016) | 2016 | TiO2 | mTiO2 | MAPb(SCN)xI3-x | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.7 |
| Chiang, Y.-H. et al., ChemSusChem 9, 2620–2627 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.3 |
| Cohen, B. El et al., J. Phys. Chem. C 120, 142–147 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 10.3 |
| Cohen, B. El et al., J. Phys. Chem. C 120, 142–147 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | toluene | DMF | - | - | - | no | no | 11.8 |
| Cui, D. et al., J. Phys. Chem. C 120, 42–47 (2016) | 2016 | TiO2 | 0 | MAPbBr3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3.5 |
| Cui, D. et al., J. Phys. Chem. C 120, 42–47 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.8 |
| Cui, D. et al., J. Phys. Chem. C 120, 42–47 (2016) | 2016 | TiO2 | 0 | MAPbI3-xBrx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.8 |
| Cui, D. et al., J. Phys. Chem. C 120, 42–47 (2016) | 2016 | TiO2 | 0 | MAPbI3-xBrx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 4.1 |
| Du, Y. et al., RSC Adv. 6, 83264–83272 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | CVD | no | na | - | - | - | P3HT | Li+TBP | 11.2 |
| Du, Y. et al., RSC Adv. 6, 101250–101258 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.4 |
| Du, Y. et al., RSC Adv. 6, 101250–101258 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 12.7 |
| Duan, J. et al., Int. J. Energy Res. 40, 806–813 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | dipping | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 10.5 |
| Duan, J. et al., Int. J. Energy Res. 40, 806–813 (2016) | 2016 | ZnO | mTiO2 | MAPbI3 | two-step | dipping | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 8 |
| Duan, J. et al., Int. J. Energy Res. 40, 806–813 (2016) | 2016 | TiO2/ZnO/TiO2 | mTiO2 | MAPbI3 | two-step | dipping | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 12.8 |
| Dubey, A. et al, Sol. Energy Mater. Sol. Cells 145, 193–199 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PDPP3T | no | 12.3 |
| Dubey, A. et al, Sol. Energy Mater. Sol. Cells 145, 193–199 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.3 |
| Fei, C. et al., Nano Energy 27, 17–26 (2016) | 2016 | SnO2 | 0 | MAPbI3 | one-step | spin | ethylacetate | DMF | 100 | 90 | na | spiro-OMeTAD | Li+TBP | 14 |
| Fei, C. et al., Nano Energy 27, 17–26 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | one-step | spin | ethylacetate | DMF | 100 | 90 | na | spiro-OMeTAD | Li+TBP | 17.2 |
| Fernandes, S. L. et al., Mater. Lett. 181, 103–107 (2016) | 2016 | Nb2O5 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 12.3 |
| Fu, K. et al., Nanoscale 8, 4181–4193 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 14.6 |
| Gong, G. et al., J. Mater. Chem. A 4, 3661–3666 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | DEPT-SC | no | 9.7 |
| Gong, G. et al., J. Mater. Chem. A 4, 3661–3666 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | DOPT-SC | no | 8.7 |
| Gong, G. et al., J. Mater. Chem. A 4, 3661–3666 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | DHPT-SC | no | 8.4 |
| Gong, G. et al., J. Mater. Chem. A 4, 3661–3666 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 5.4 |
| Gong, G. et al., Org. Electron. physics, Mater. Appl. 35, 171–175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | DEPT-SC | no | 9.7 |
| Gong, G. et al., Org. Electron. physics, Mater. Appl. 35, 171–175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | DEPT-SC | Li+TBP | 5.2 |
| Gong, G. et al., Org. Electron. physics, Mater. Appl. 35, 171–175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.2 |
| Gong, G. et al., Org. Electron. physics, Mater. Appl. 35, 171–175 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | DEPT-SC | F4TCNQ | 11.5 |
| Guerrero, A. et al., J. Phys. Chem. C 120, 8023–8032 (2016) | 2016 | SnO2 | 0 | FA0.85MA0.15Pb(I0.85Br0.15)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 16.9 |
| Guerrero, A. et al., J. Phys. Chem. C 120, 8023–8032 (2016) | 2016 | TiO2 | 0 | FA0.85MA0.15Pb(I0.85Br0.15)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 9.8 |
| Guerrero, A. et al., J. Phys. Chem. C 120, 8023–8032 (2016) | 2016 | Nb2O5 | 0 | FA0.85MA0.15Pb(I0.85Br0.15)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 0.1 |
| Guo, J. J. et al., Synth. Met. 220, 462–468 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | CoPcNO2-Oph | no | 8.2 |
| Guo, J. J. et al., Synth. Met. 220, 462–468 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.8 |
| Guo, Y. et al., RSC Adv. 6, 62522–62528 (2016) | 2016 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.4 |
| Hao, Q. et al., J. Alloys Compd. 671, 11–16 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | NEP | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| He, X. et al., J. Power Sources 332, 366–371 (2016) | 2016 | TiO2-nanorod(used as compact layer) | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 17.6 |
| He, X. et al., J. Power Sources 332, 366–371 (2016) | 2016 | TiO2-QD | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 15.2 |
| He, X. et al., J. Power Sources 332, 366–371 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 13.5 |
| Heo, J. H. and Im, S. H., Nanoscale 8, 2554–2560 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+HI | 100 | 2 | ambient | PTAA | Li+TBP | 18.9 |
| Hou, Y. et al., Sol. Energy Mater. Sol. Cells 155, 101–107 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14 |
| Hou, Y. et al., Sol. Energy Mater. Sol. Cells 155, 101–107 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.8 |
| Hou, X. et al., Sol. Energy Mater. Sol. Cells 149, 121–127 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12 |
| Hou, X. et al., Sol. Energy Mater. Sol. Cells 149, 121–127 (2016) | 2016 | TiO2 | ZGO | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.3 |
| Hu, Y. et al., J. Alloys Compd. 679, 32–38 (2016) | 2016 | TiO2 | TiO2-nanorod/SrTiO3 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| Hu, Y. et al., J. Alloys Compd. 679, 32–38 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8 |
| Huang, L. et al., Sol. Energy Mater. Sol. Cells 149, 1–8 (2016) | 2016 | TiO2 | no | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 12.3 |
| Huang, L. et al., Sol. Energy Mater. Sol. Cells 149, 1–8 (2016) | 2016 | no | no | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 10.7 |
| Huang, F. et al., Nano Energy 27, 509–514 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.8 |
| Huang, Y. et al., Thin Solid Films 598, 1–5 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.3 |
| Huang, J. et al., RSC Adv. 6, 55720–55725 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 5 | na | spiro-OMeTAD | TFSI+TBP | 12.1 |
| Huang, J. et al., RSC Adv. 6, 55720–55725 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+H2O | 100 | 5 | na | spiro-OMeTAD | TFSI+TBP | 12.7 |
| Huang, J. et al., RSC Adv. 6, 55720–55725 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+HBr | 100 | 5 | na | spiro-OMeTAD | TFSI+TBP | 15.8 |
| Huang, J. et al., RSC Adv. 6, 55720–55725 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+HCl | 100 | 5 | na | spiro-OMeTAD | TFSI+TBP | 13.7 |
| Huang, J. et al., RSC Adv. 6, 55720–55725 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+HI | 100 | 5 | na | spiro-OMeTAD | TFSI+TBP | 14.4 |
| Huang, J. et al., Sol. Energy 133, 331–338 (2016) | 2016 | ZnO | 0 | MAPbI3 | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | no | 8.3 |
| Huang, J. et al., Sol. Energy 133, 331–338 (2016) | 2016 | FPDI | 0 | MAPbI3 | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | no | 7.9 |
| Huang, H. et al., Nano Energy 27, 352–358 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spray | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 16 |
| Jain, S. M. et al., Energy Environ. Sci. 9, 3770–3782 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 18.5 |
| Jain, S. M. et al., Energy Environ. Sci. 9, 3770–3782 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 9.5 |
| Jeon, S. et al., Org. Electron. physics, Mater. Appl. 37, 134–140 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | DPIO | no | 10.1 |
| Jeon, S. et al., Org. Electron. physics, Mater. Appl. 37, 134–140 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | DPIE | no | 5.4 |
| Jeon, S. et al., Org. Electron. physics, Mater. Appl. 37, 134–140 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 12 |
| Jeon, S. et al., Org. Electron. physics, Mater. Appl. 37, 134–140 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 7.9 |
| Jeong, I. et al., Nano Energy 28, 380–389 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 19.6 |
| Jeong, I. et al., Nano Energy 28, 380–389 (2016) | 2016 | UV-Nb-TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 15.5 |
| Jiang, X. et al., J. Phys. Chem. Lett. 7, 4142–4146 (2016) | 2016 | 0 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 50 | na | na | no | no | 12.3 |
| Jiang, X. et al., J. Phys. Chem. Lett. 7, 4142–4146 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | 50 | na | na | no | no | 12.7 |
| Jiang, X. et al., J. Phys. Chem. Lett. 7, 4142–4146 (2016) | 2016 | 0 | mTiO2 | (5-AVA)x(MA)1-xPbI3 | one-step | spin | no | GBL | 50 | na | na | no | no | 12.9 |
| Jiang, X. et al., J. Phys. Chem. Lett. 7, 4142–4146 (2016) | 2016 | TiO2 | mTiO2 | (5-AVA)x(MA)1-xPbI3 | one-step | spin | no | GBL | 50 | na | na | no | no | 13.3 |
| Ke, W. et al., Adv. Mater. 28, 5214–5221 (2016) | 2016 | SnO2 | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 17.8 |
| Ke, W. et al., Adv. Mater. 28, 5214–5221 (2016) | 2016 | SnO2 | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 16.4 |
| Ke, W. et al., J. Mater. Chem. A 4, 14276–14283 (2016) | 2016 | SnO2 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 16.9 |
| Ke, W. et al., J. Mater. Chem. A 4, 14276–14283 (2016) | 2016 | SnO2 | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 19.1 |
| Kim, I. S. et al., ACS Appl. Mater. Interfaces 8, 24310–24314 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 14.3 |
| Kim, A. et al., Nanoscale 8, 6308–6316 (2016) | 2016 | ZnO | mAl2O3 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11 |
| Kim, J. et al., J. Phys. Chem. C 120, 11262–11267 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | 160 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 4 |
| Kim, J. et al., J. Phys. Chem. C 120, 11262–11267 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+HI | 160 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 16 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 6, 2452–2456 (2015) | 2016 | TiO2 | mAl2O3 | CsPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 1.1 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 6, 2452–2456 (2015) | 2016 | TiO2 | mTiO2 | CsPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 5.5 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 6, 2452–2456 (2015) | 2016 | TiO2 | mTiO2 | CsPbI3 | two-step | spin-dip | no | DMF | - | - | - | CBP | no | 4.9 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 7, 167–172 (2016) | 2016 | TiO2 | mTiO2 | MAPbBr3 | two-step | spin-dip | no | DMF | - | - | - | PTAA | no | 6.6 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 6, 2452–2456 (2015) | 2016 | TiO2 | mTiO2 | CsPbI3 | two-step | spin-dip | no | DMF | - | - | - | PTAA | no | 6 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 7, 167–172 (2016) | 2016 | TiO2 | mTiO2 | CsPbBr3 | two-step | spin-dip | no | DMF | - | - | - | PTAA | no | 6.2 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 6, 2452–2456 (2015) | 2016 | TiO2 | mAl2O3 | CsPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 1.9 |
| Kulbak, M. et al., J. Phys. Chem. Lett. 6, 2452–2456 (2015) | 2016 | TiO2 | mTiO2 | CsPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5 |
| Kumar, Y. et al., Sol. Energy Mater. Sol. Cells 157, 10–17 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | na | na | ambient | spiro-OMeTAD | Li+TBP | 4.9 |
| Kumar, Y. et al., Sol. Energy Mater. Sol. Cells 157, 10–17 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | MS | na | ambient | spiro-OMeTAD | Li+TBP | 6.8 |
| Kumar, Y. et al., Sol. Energy Mater. Sol. Cells 157, 10–17 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 3.1 |
| Lan, C. et al., CrystEngComm 18, 9243–9251 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.5 |
| Lee, S. J. et al., J. Am. Chem. Soc. 138, 3974–3977 (2016) | 2016 | TiO2 | mTiO2 | FASnI3 | one-step | spin 2-3 | toluene | DMF+DMSO+SnF2 | 60 | 60 | glovebox | spiro-OMeTAD | lutidiene+TBP | 2.8 |
| Lee, S. J. et al., J. Am. Chem. Soc. 138, 3974–3977 (2016) | 2016 | TiO2 | mTiO2 | FASnI3 | one-step | spin 2-3 | toluene | DMF+DMSO+SnF2+pyrazine | 60 | 60 | glovebox | spiro-OMeTAD | lutidiene+TBP | 4.8 |
| Lee, J. W. et al., Acc. Chem. Res. 49, 311–319 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 11.5 |
| Lee, J. W. et al., Acc. Chem. Res. 49, 311–319 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO+thiourea | MS | na | na | spiro-OMeTAD | Li+TBP | 14.3 |
| Lei, Y. et al., J. Mater. Chem. A 4, 5474–5481 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5 |
| Lei, Y. et al., J. Mater. Chem. A 4, 5474–5481 (2016) | 2016 | ZnO | mZnO | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.8 |
| Leyden, M. R. et al., J. Mater. Chem. A 4, 13125–13132 (2016) | 2016 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 18.3 |
| Leyden, M. R. et al., J. Mater. Chem. A 4, 13125–13132 (2016) | 2016 | TiO2 | mTiO2 | FAPbI3 | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15.6 |
| Li, H. et al., Nanoscale 8, 6379–6385 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 14.7 |
| Li, H. et al., Nanoscale 8, 6379–6385 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 9.9 |
| Li, H. et al., Nanoscale 8, 6379–6385 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.3 |
| Li, H. et al., Sol. Energy 126, 243–251 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.9 |
| Li, M. et al, Adv. Energy Mater. 6, 1601156 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | no | 14.8 |
| Li, M. et al, Adv. Energy Mater. 6, 1601156 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | CuSCN | 18 |
| Li, M. et al, Adv. Energy Mater. 6, 1601156 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | CuI | 16.7 |
| Li, M. et al., ChemSusChem 9, 2862–2869 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMF | 100 | 60 | na | Chl-1 | no | 11.5 |
| Li, M. et al., ChemSusChem 9, 2862–2869 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMF | 100 | 60 | na | Chl-2 | no | 8.1 |
| Li, M. et al., ChemSusChem 9, 2862–2869 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMF | 100 | 60 | na | P3HT | Li+TBP | 8.9 |
| Li, X. et al., ACS Appl. Mater. Interfaces 8, 21358–21365 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.4 |
| Li, X. et al., ACS Appl. Mater. Interfaces 8, 21358–21365 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.2 |
| Li, J. et al., Nanoscale 8, 14163–14170 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 12.3 |
| Li, J. et al., Nanoscale 8, 14163–14170 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 9.7 |
| Li, F. et al., Chem. Commun. 52, 5394–5397 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | na | na | na | spiro-OMeTAD | Li+TBP | 17.8 |
| Li, F. et al., Chem. Commun. 52, 5394–5397 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 16.5 |
| Li, F. et al., J. Mater. Chem. A 4, 11372–11380 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.8 |
| Li, F. et al., J. Mater. Chem. A 4, 11372–11380 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.5 |
| Li, F. et al., J. Mater. Chem. A 4, 11372–11380 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 7.6 |
| Li, Y. et al., J. Power Sources 320, 204–211 (2016) | 2016 | ZnO | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 30 | ambient | spiro-OMeTAD | Li+TBP | 15.5 |
| Liu, L. et al., Electrochim. Acta 222, 933–937 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.6 |
| Liu, L. et al., Electrochim. Acta 222, 933–937 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.5 |
| Liu, D. et al., RSC Adv. 6, 51279–51285 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 75 | na | spiro-OMeTAD | Li+TBP | 14.3 |
| Liu, Z. et al., Nanoscale 8, 7017–7023 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | GBL | - | - | - | no | no | 6.9 |
| Liu, J. et al., Electrochim. Acta 195, 143–149 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.9 |
| Liu, J. et al., Electrochim. Acta 195, 143–149 (2016) | 2016 | TiO2-W | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.9 |
| Luo, S. et al., Mater. Lett. 169, 236–240 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5.4 |
| Luo, S. et al., Mater. Lett. 169, 236–240 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11 |
| Mali, S. S. et al., Nanoscale 8, 2664–2677 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | GBL | 95 | 10 | na | spiro-OMeTAD | Li+TBP | 9.7 |
| Mali, S. S. et al., Nanoscale 8, 2664–2677 (2016) | 2016 | TiO2 | mTiO2-Au | MAPbI3 | one-step | spin 2-3 | no | GBL | 95 | 10 | na | spiro-OMeTAD | Li+TBP | 11.1 |
| Mali, S. S. et al., Nanoscale 8, 2664–2677 (2016) | 2016 | TiO2 | TiO2-Au-nanofiber | MAPbI3 | one-step | spin 2-3 | no | GBL | 95 | 10 | na | spiro-OMeTAD | Li+TBP | 14.9 |
| Mali, S. S. et al., Nanoscale 8, 2664–2677 (2016) | 2016 | TiO2 | TiO2-nanofiber | MAPbI3 | one-step | spin 2-3 | no | GBL | 95 | 10 | na | spiro-OMeTAD | Li+TBP | 11.2 |
| Marco, N. De et al., Nano Lett. 16, 1009–1016 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.4 |
| Marco, N. De et al., Nano Lett. 16, 1009–1016 (2016) | 2016 | TiO2 | 0 | GA:MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.1 |
| McMeekin, D. P. et al., Science 351, 151–5 (2016) | 2016 | SnO2 | PCBM | FA0.83Cs0.17Pb(I0.6Br0.4)3 | one-step | spin | no | DMF | 185 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 17.1 |
| Murugadoss, G. et al., J. Power Sources 307, 891–897 (2016) | 2016 | SnO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | CuSCN | no | 8.4 |
| Nejand, B. A. et al., ChemSusChem 9, 302–313 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | ambient | Cu2O | no | 4 |
| Nejand, B. A. et al., ChemSusChem 9, 302–313 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | Cu2O | no | 8.9 |
| Nejand, B. A. et al., ChemSusChem 9, 302–313 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.5 |
| Nejand, B. A. et al., J. Phys. Chem. C 120, 2520–2528 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | sprayroll | no | DMF | 180 | na | na | spiro-OMeTAD | Li+TBP | 13.2 |
| Nejand, B. A. et al., J. Phys. Chem. C 120, 2520–2528 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spray | no | DMF | 180 | na | glovebox | spiro-OMeTAD | Li+TBP | 8.2 |
| Nejand, B. A. et al., Sci. Rep. 6, 33649 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 5 | ambient | spiro-OMeTAD | Li+TBP | 11.3 |
| Nejand, B. A. et al., Sci. Rep. 6, 33649 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spray | no | na | 120 | 180 | glovebox | spiro-OMeTAD | Li+TBP | 9.1 |
| Niu, G. et al., Nano Energy 27, 87–94 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | MS | na | na | spiro-OMeTAD | Li+TBP | 15.1 |
| Niu, G. et al., Nano Energy 27, 87–94 (2016) | 2016 | TiO2 | mTiO2 | (MAPbI3)0.9(CsPbBr3)0.1 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | MS | na | na | spiro-OMeTAD | Li+TBP | 17.6 |
| Nourolahi, H. et al., Sol. Energy 139, 475–483 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 4.6 |
| Nourolahi, H. et al., Sol. Energy 139, 475–483 (2016) | 2016 | TiO2-Ag | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 6.2 |
| Pascoe, A. R. et al., Adv. Funct. Mater. 26, 1278–1285 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.3 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 85 | 10 | na | spiro-OMeTAD | Li+TBP | 14.2 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 85 | 10 | na | spiro-OMeTAD | Li+TBP | 8.8 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3 | one-step | spin | no | DMSO+GBL | 85 | 10 | na | spiro-OMeTAD | Li+TBP | 10.6 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3 | one-step | spin | no | DMSO+GBL | 80 | 10 | na | spiro-OMeTAD | Li+TBP | 4.9 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMSO+GBL | 85 | 30 | na | spiro-OMeTAD | Li+TBP | 16 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 85 | 10 | na | spiro-OMeTAD | Li+TBP | 14 |
| Pascoe, A. R. et al., Nano Energy 22, 439–452 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 85 | 10 | na | spiro-OMeTAD | Li+TBP | 10.2 |
| Pearson, A. J. et al., Adv. Energy Mater. 6, 1600014 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | ambient | spiro-OMeTAD | Li+TBP | 11.1 |
| Peng, G. et al., J. Mater. Chem. A 4, 1520–1530 (2016) | 2016 | 0 | TiO2-nanocone | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 12 |
| Peng, G. et al., J. Mater. Chem. A 4, 1520–1530 (2016) | 2016 | 0 | TiO2-nanorod | MAPbI3 | one-step | spin 2-3 | no | GBL | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 10 |
| Ramirez, D. et al., J. Phys. Chem. C 120, 8559–8567 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 10.9 |
| Rapsomanikis, A. et al., Sol. Energy Mater. Sol. Cells 151, 36–43 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 100 | 30 | ambient | P3HT | Li+TBP | 13.7 |
| Ren, X. et al., Nanoscale 8, 3816–3822 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.9 |
| Reyna, Y. et al., Nano Energy 30, 570–579 (2016) | 2016 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 14.6 |
| Saliba, M. et al., Energy Environ. Sci. 9, 1989–1997 (2016) | 2016 | TiO2 | mTiO2-Li | Cs5(MA0.17FA0.83)95Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 21.2 |
| Saliba, M. et al., Energy Environ. Sci. 9, 1989–1997 (2016) | 2016 | TiO2 | mTiO2-Li | Cs10(MA0.17FA0.83)90Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 21 |
| Saliba, M. et al., Energy Environ. Sci. 9, 1989–1997 (2016) | 2016 | TiO2 | mTiO2-Li | (MA0.17FA0.83)100Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.4 |
| Saliba, M. et al., Science 354, 206–209 (2016) | 2016 | TiO2 | mTiO2-Li | Rb/Cs/MA/FA cations | one-step | spin 2-3 | no | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 21.8 |
| Sedighi, R. et al., ChemPhysChem 17, 2382–2388 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Sedighi, R. et al., ChemPhysChem 17, 2382–2388 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xBrx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.5 |
| Sedighi, R. et al., ChemPhysChem 17, 2382–2388 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.6 |
| Seo, M.-S. et al, Nanoscale 8, 11472–11479 (2016) | 2016 | TiO2 | TiO2-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.5 |
| Seo, M.-S. et al, Nanoscale 8, 11472–11479 (2016) | 2016 | TiO2 | TiO2-nanowire | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.6 |
| Sfyri, G. et al., Appl. Surf. Sci. 360, 767–771 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 30 | dry air | CuMePc | no | 5 |
| Shaikh, S. F. et al., J. Mater. Chem. A 4, 15478–15485 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 2 | na | spiro-OMeTAD | Li+TBP | 15.8 |
| Shaikh, S. F. et al., J. Mater. Chem. A 4, 15478–15485 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 2 | na | spiro-OMeTAD | Li+TBP | 11.1 |
| Shin, S. S. et al., J. Phys. Chem. Lett. 7, 1845–1851 (2016) | 2016 | Zn2SnO4 | 0 | MAPbI3 | two-step | spin | toluene | DMF | - | - | - | PTAA | no | 17.6 |
| Song, J. et al., J. Mater. Chem. A 4, 8435–8443 (2016) | 2016 | ZnO | 0 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.1 |
| Song, J. et al., J. Mater. Chem. A 4, 8435–8443 (2016) | 2016 | ZnO | 0 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.1 |
| Song, J. et al., J. Mater. Chem. A 4, 8435–8443 (2016) | 2016 | ZnO | 0 | FAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | PEIE | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 11.5 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | 0 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 7.4 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 11 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | PEIE | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 14.1 |
| Song, S. et al., Nano Energy 28, 269–276 (2016) | 2016 | no | no | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | spiro-OMeTAD | Li+TBP | 4.7 |
| Song, J. et al., Sol. Energy Mater. Sol. Cells 144, 623–630 (2016) | 2016 | SnO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Song, J. et al., Sol. Energy Mater. Sol. Cells 144, 623–630 (2016) | 2016 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.9 |
| Song, J. et al., Sol. Energy Mater. Sol. Cells 144, 623–630 (2016) | 2016 | ZnO-SnO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.3 |
| Song, D. H. et al., J. Power Sources 310, 130–136 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMSO | 100 | 40 | ambient | PTAA | Li+TBP | 11.6 |
| Song, D. H. et al., J. Power Sources 310, 130–136 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMSO | 100 | 2 | ambient | PTAA | Li+TBP | 15.6 |
| Su, P. Y. et al., Electrochim. Acta 209, 529–540 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 120 | na | SP-no1-Co | no | 13.9 |
| Su, P. Y. et al., Electrochim. Acta 209, 529–540 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 120 | na | SP-no1 | no | 12.4 |
| Su, P. Y. et al., Electrochim. Acta 209, 529–540 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 120 | na | H1no1 | no | 11.6 |
| Su, P. Y. et al., Electrochim. Acta 209, 529–540 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 120 | na | SP-no2 | no | 6.5 |
| Su, P. Y. et al., Electrochim. Acta 209, 529–540 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 120 | na | spiro-OMeTAD | Li+TBP+FK102 | 14.7 |
| Su, P. Y. et al., Electrochim. Acta 209, 529–540 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 120 | na | spiro-OMeTAD | Li+TBP+FK102 | 13 |
| Supasai, T. et al., Sol. Energy 136, 515–524 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 6.5 |
| Tai, Q. et al., Nat. Commun. 7, 11105 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.3 |
| Tai, Q. et al., Nat. Commun. 7, 11105 (2016) | 2016 | TiO2 | mTiO2 | MAPb(SCN)xI3-x | two-step | spin | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Tai, Q. et al., Nat. Commun. 7, 11105 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 8.8 |
| Tai, Q. et al., Nat. Commun. 7, 11105 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Tang, J. F. et al., Sol. Energy Mater. Sol. Cells 154, 18–22 (2016) | 2016 | ZnO | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 11.3 |
| Tang, J. F. et al., Sol. Energy Mater. Sol. Cells 154, 18–22 (2016) | 2016 | 0 | cZnO-nanowire | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 13.6 |
| Tavakoli, M. M. et al., J. Phys. Chem. C 120, 19531–19536 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Tavakoli, M. M. et al., J. Phys. Chem. C 120, 19531–19536 (2016) | 2016 | TiO2 | Rgs | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.2 |
| Tavakoli, M. M. et al., J. Phys. Chem. C 120, 19531–19536 (2016) | 2016 | TiO2 | 2D-graphene | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.3 |
| Tseng, Z.-L. et al., Nano Energy 28, 311–318 (2016) | 2016 | ZnO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Tseng, Z.-L. et al., Nano Energy 28, 311–318 (2016) | 2016 | AZO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.6 |
| Wang, J. et al., Electrochim. Acta 210, 673–680 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | na | HBZ-7no | no | 4.5 |
| Wang, J. et al., Electrochim. Acta 210, 673–680 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 5.1 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | PDTSTTz-4 | Li+TBP | 13.9 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | PDTSTTz | Li+TBP | 13.3 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | C60 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | PDTSTTz-4 | Li+TBP | 15.8 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | C60 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | PDTSTTz | Li+TBP | 14.4 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | P3HT | Li+TBP | 12.5 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | C60 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | P3HT | Li+TBP | 14.3 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 11.9 |
| Wang, Z. et al., Org. Electron. physics, Mater. Appl. 33, 142–149 (2016) | 2016 | TiO2 | C60 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 13.6 |
| Wang, S. et al., Nanoscale 8, 6600–6608 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 12 |
| Wang, S. et al., Nanoscale 8, 6600–6608 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 14.6 |
| Wang, S. et al., Nanoscale 8, 6600–6608 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 12.2 |
| Wang, S. et al., Nanoscale 8, 6600–6608 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 10.1 |
| Wang, S. et al., Nanoscale 8, 6600–6608 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 7.3 |
| Wang, S. et al., Nanoscale 8, 6600–6608 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK102 | 6.8 |
| Wang, W. et al., Nanoscale Res. Lett. 11, 316 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | glovebox | spiro-OMeTAD | no | 12.4 |
| Wang, W. et al., Nanoscale Res. Lett. 11, 316 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 45 | glovebox | spiro-OMeTAD | no | 10.6 |
| Wang, F. et al., Nanoscale 8, 11882–11888 (2016) | 2016 | TiO2 | no | MAPbI3 | one-step | spin | toluene | DMSO | 100 | 10 | glovebox | SWNT-GO | no | 11.7 |
| Wang, F. et al., Nanoscale 8, 11882–11888 (2016) | 2016 | TiO2 | no | MAPbI3 | one-step | spin | toluene | DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 12.1 |
| Wang, F. et al., Adv. Mater. 28, 9986–9992 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 19.2 |
| Wang, F. et al., Adv. Mater. 28, 9986–9992 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 11.8 |
| Wang, W. et al., J. Mater. Sci. Mater. Electron. 27, 9384–9390 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 11.9 |
| Wang, W. et al., J. Mater. Sci. Mater. Electron. 27, 9384–9390 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF+H3PO2 | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 12.4 |
| Wei, Q. et al., RSC Adv. 6, 56807–56811 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMSO+GBL | 150 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 14.3 |
| Wei, Q. et al., RSC Adv. 6, 56807–56811 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMSO+GBL+CN | 150 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 16.5 |
| Wei, J. et al., Nano Energy 26, 139–147 (2016) | 2016 | TiO2 | no | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 12.5 |
| Wei, J. et al., Nano Energy 26, 139–147 (2016) | 2016 | TiO2 | no | MAPbI3-xClx | one-step | spin | no | DMF+PCBM | MS | na | na | spiro-OMeTAD | Li+TBP | 14.2 |
| Wei, J. et al., Nano Energy 26, 139–147 (2016) | 2016 | TiO2 | no | MAPbI3-xClx | one-step | spin | no | DMF+PCBM+PEG | MS | na | na | spiro-OMeTAD | Li+TBP | 17.1 |
| Wei, J. et al., Nano Energy 26, 139–147 (2016) | 2016 | TiO2 | no | MAPbI3-xClx | one-step | spin | no | DMF+PEG | MS | na | na | spiro-OMeTAD | Li+TBP | 16.3 |
| Wei, Q. et al., Sol. Energy 135, 654–661 (2016) | 2016 | no | no | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 10.2 |
| Wei, Q. et al., Sol. Energy 135, 654–661 (2016) | 2016 | no | no | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 10.1 |
| Wei, Q. et al., Sol. Energy 135, 654–661 (2016) | 2016 | no | no | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 10 |
| Wu, C. et al., J. Phys. Chem. C 120, 26710–26719 (2016) | 2016 | TiO2 | 0 | FAPbI3-xBrx | two-step | spin | no | NMP | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 14 |
| Wu, C. et al., J. Phys. Chem. C 120, 26710–26719 (2016) | 2016 | TiO2 | mTiO2 | FAPbI3-xBrx | two-step | spin | no | NMP | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.5 |
| Wu, W. Q. et al., J. Power Sources 329, 17–22 (2016) | 2016 | no | no | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 2.7 |
| Wu, W. Q. et al., J. Power Sources 329, 17–22 (2016) | 2016 | 0 | TiO2-nanowire | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14.7 |
| Xiao, Y. et al., J. Power Sources 306, 171–177 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin 2-3-dip | no | GBL | - | - | - | PEDOT | no | 12.4 |
| Xiong, H. et al., J. Mater. Chem. C 4, 6848–6854 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 12.4 |
| Xiong, H. et al., J. Mater. Chem. C 4, 6848–6854 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 11.3 |
| Yan, J.-J. et al., Superlattices Microstruct. 94, 196–203 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | Li+TBP | 8.6 |
| Yang, Y. et al., J. Alloys Compd. 684, 84–90 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 6.8 |
| Yang, Y. et al., J. Alloys Compd. 684, 84–90 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+BAI | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 9.1 |
| Yang, Y. et al., J. Alloys Compd. 684, 84–90 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+NH4I | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 9.5 |
| Yang, S. et al., J. Mater. Chem. A 4, 9430–9436 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | 150 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 5.9 |
| Yang, S. et al., J. Mater. Chem. A 4, 9430–9436 (2016) | 2016 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF+NH4SCN | 150 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 11.4 |
| Ahmadian-Yazdi, M. R. et al., Nanoscale Res. Lett. 11, 408 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 3.5 |
| Ahmadian-Yazdi, M. R. et al., Nanoscale Res. Lett. 11, 408 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 7.3 |
| Ye, J. et al., Sol. Energy 136, 505–514 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | DMF+DMSO | 105 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 15.9 |
| Ye, J. et al., Sol. Energy 136, 505–514 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene+acetonitrile | DMF+DMSO | 105 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 18.3 |
| Ye, J. et al., RSC Adv. 6, 36356–36361 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 13.8 |
| Ye, J. et al., RSC Adv. 6, 36356–36361 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 8.2 |
| Yi, Y. et al., RSC Adv. 6, 82759–82762 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | MS | na | na | no | no | 4.4 |
| Yi, Y. et al., RSC Adv. 6, 82759–82762 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | MS | na | na | no | no | 0.1 |
| Yin, X. et al., ACS Appl. Mater. Interfaces 8, 29580–29587 (2016) | 2016 | TiZn2O4 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP | 15.1 |
| Yoon, H. et al., Energy Environ. Sci. 9, 2262–2266 (2016) | 2016 | BCP | C60 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 19.1 |
| Yu, X. et al., J. Power Sources 325, 534–540 (2016) | 2016 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | spiro-OMeTAD | no | 10.5 |
| Yu, X. et al., J. Power Sources 325, 534–540 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | spiro-OMeTAD | no | 10.7 |
| Yu, X. et al., J. Power Sources 325, 534–540 (2016) | 2016 | TiO2 | mSiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | spiro-OMeTAD | no | 15.8 |
| Yu, Y. et al., ChemSusChem 9, 3288–3297 (2016) | 2016 | SnO2 | C60-SAM | FAPbI3 | one-step | spin | no | DMF+DMSO | 150 | 10 | na | spiro-OMeTAD | Li+TBP | 15.2 |
| Yu, Y. et al., ChemSusChem 9, 3288–3297 (2016) | 2016 | SnO2 | C60-SAM | FA0.8Cs0.2PbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 19.6 |
| Yu, Y. et al., ChemSusChem 9, 3288–3297 (2016) | 2016 | SnO2 | C60-SAM | FA0.8Cs0.2PbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.6 |
| Yu, M. et al., Chem. Phys. Lett. 662, 257–262 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 90 | 60 | na | spiro-OMeTAD | Li+TBP | 7.2 |
| Yu, M. et al., Chem. Phys. Lett. 662, 257–262 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 60 | na | spiro-OMeTAD | Li+TBP | 16.4 |
| Yuan, Z. et al., ACS Appl. Mater. Interfaces 8, 34446–34454 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | na | ambient | spiro-OMeTAD | Li+TBP | 13.8 |
| Yuan, Z. et al., ACS Appl. Mater. Interfaces 8, 34446–34454 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 95 | na | ambient | spiro-OMeTAD | Li+TBP | 16.6 |
| Yuan, M. et al., Electrochim. Acta 215, 374–379 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | CZTS-QD | no | 10.7 |
| Yuan, M. et al., Electrochim. Acta 215, 374–379 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | CZTSe-QD | no | 9.7 |
| Yuan, S. et al., RSC Adv. 6, 47459–47467 (2016) | 2016 | TiO2 | PCBM | MAPbI3 | two-step | vasp | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15.6 |
| Zhang, Y. et al., Chem. Commun. 52, 5674–5677 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 12.5 |
| Zhang, Y. et al., Chem. Commun. 52, 5674–5677 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+CNT | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 10.3 |
| Zhang, Y. et al., Chem. Commun. 52, 5674–5677 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+s-CNT | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Zhang, F. et al., Synth. Met. 220, 187–193 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14 |
| Zhang, F. et al., Synth. Met. 220, 187–193 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.6 |
| Zhang, F. et al., Synth. Met. 220, 187–193 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.6 |
| Zhang, F. et al., Chem. Mater. 28, 802–812 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 10.6 |
| Zhang, F. et al., Chem. Mater. 28, 802–812 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 10.6 |
| Zhang, F. et al., Chem. Mater. 28, 802–812 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5.8 |
| Zhang, F. et al., Chem. Mater. 28, 802–812 (2016) | 2016 | TiO2-O2 treated | mTiO2 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5 |
| Zhang, H. et al., J. Mater. Chem. A 4, 8724–8733 (2016) | 2016 | PDI | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 17.7 |
| Zhang, H. et al., J. Mater. Chem. A 4, 8724–8733 (2016) | 2016 | no | no | MAPbI3-xClx | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 12.9 |
| Zhang, X. et al., J. Alloys Compd. 681, 191–196 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 8.6 |
| Zhang, X. et al., J. Alloys Compd. 681, 191–196 (2016) | 2016 | TiO2 | mTiO2-F | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | no | 12.1 |
| Zhang, C. Z. et al., Opt. Quantum Electron. 48, 550 (2016) | 2016 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 105 | 45 | glovebox | spiro-OMeTAD | Li+TBP | 10.4 |
| Zhao, B. G. et al., J. Mater. Sci. Mater. Electron. 27, 10869–10876 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 70 | 30 | na | spiro-OMeTAD | Li+TBP | 13.1 |
| Zhao, B. G. et al., J. Mater. Sci. Mater. Electron. 27, 10869–10876 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 70 | 30 | na | spiro-OMeTAD | Li+TBP | 10.3 |
| Zhao, Q. et al., Sci. Rep. 6, 38670 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 150 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 13 |
| Zhao, Q. et al., Sci. Rep. 6, 38670 (2016) | 2016 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+HAc | 150 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 14.7 |
| Zhou, Z. et al., RSC Adv. 6, 78585–78594 (2016) | 2016 | TiO2 | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 10.6 |
| Zhou, Z. et al., RSC Adv. 6, 78585–78594 (2016) | 2016 | TiO2 | C60 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 16.6 |
| Zhou, Z. et al., Chem. Commun. 52, 3828–3831 (2016) | 2016 | TiO2 | mTiO2 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.8 |
| Zhou, Z. et al., Chem. Commun. 52, 3828–3831 (2016) | 2016 | TiO2 | mTiO2 | FAPbI3 | two-step | vasp | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Zhou, P. et al., Sol. Energy 137, 579–584 (2016) | 2016 | TiO2 | SnO2-ns | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.2 |
| Zuo, L. et al., J. Am. Chem. Soc. 138, 15710–15716 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 19.2 |
| Zuo, L. et al., J. Am. Chem. Soc. 138, 15710–15716 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.2 |
| Zuo, L. et al., J. Am. Chem. Soc. 138, 15710–15716 (2016) | 2016 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.3 |
| Aeineh, N. et al., ACS Appl. Mater. Interfaces 9, 13181–13187 (2017) | 2017 | TiO2 | mTiO2-Au@SiO | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 65 | 3 | na | spiro-OMeTAD | Li+TBP | 16.4 |
| Aeineh, N. et al., ACS Appl. Mater. Interfaces 9, 13181–13187 (2017) | 2017 | TiO2 | mTiO2-Li | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 65 | 3 | na | spiro-OMeTAD | Li+TBP | 16.2 |
| Aeineh, N. et al., ACS Appl. Mater. Interfaces 9, 13181–13187 (2017) | 2017 | TiO2-Au@SiO | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 65 | 3 | na | spiro-OMeTAD | Li+TBP | 17.6 |
| An, Q. et al., Nano Energy 39, 400–408 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | no | DMF+HP | 80 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 6.5 |
| An, Q. et al., Nano Energy 39, 400–408 (2017) | 2017 | ZnO-Li | 0 | MAPbI3 | one-step | spin | no | DMF+HP | 80 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 9.6 |
| An, Q. et al., Nano Energy 39, 400–408 (2017) | 2017 | ZnO-Cs | 0 | MAPbI3 | one-step | spin | no | DMF+HP | 80 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 9.5 |
| An, Q. et al., Nano Energy 39, 400–408 (2017) | 2017 | ZnO | PCBA | MAPbI3 | one-step | spin | no | DMF+HP | 80 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 15.5 |
| An, Q. et al., Nano Energy 39, 400–408 (2017) | 2017 | ZnO-Li | PCBA | MAPbI3 | one-step | spin | no | DMF+HP | 80 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 18.5 |
| An, Q. et al., Nano Energy 39, 400–408 (2017) | 2017 | ZnO-Cs | PCBA | MAPbI3 | one-step | spin | no | DMF+HP | 80 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 17.5 |
| Apostolopoulou, A. et al., Sol. Energy Mater. Sol. Cells 166, 100–107 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 30 | na | P3HT | Li+TBP | 12.9 |
| Apostolopoulou, A. et al., Sol. Energy Mater. Sol. Cells 166, 100–107 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 30 | na | P3HT | Li+TBP | 10 |
| Barbé, J. et al., ACS Appl. Mater. Interfaces 9, 11828–11836 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 80 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 12.8 |
| Barbé, J. et al., ACS Appl. Mater. Interfaces 9, 11828–11836 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 80 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 14.8 |
| Batmunkh, M. et al., ChemSusChem 10, 3750–3753 (2017) | 2017 | TiO2 | mTiO2 | CsI, FAI, PbI2, MABr, PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 45 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 15.2 |
| Batmunkh, M. et al., ChemSusChem 10, 3750–3753 (2017) | 2017 | TiO2 | mTiO2-Au nanostars | CsI, FAI, PbI2, MABr, PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 45 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 17.7 |
| Batmunkh, M. et al., ACS Appl. Mater. Interfaces 9, 19945–19954 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 13.5 |
| Batmunkh, M. et al., ACS Appl. Mater. Interfaces 9, 19945–19954 (2017) | 2017 | TiO2 | TiO2-SWCNTs | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK102 | 16.1 |
| Cai, F. et al., J. Mater. Chem. A 5, 9402–9411 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 17.6 |
| Cai, F. et al., J. Mater. Chem. A 5, 9402–9411 (2017) | 2017 | TiO2-TOPD | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 18.8 |
| Cai, F. et al., J. Mater. Chem. A 5, 9402–9411 (2017) | 2017 | TiO2-TOPD | C60-ETA | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 19.6 |
| Cai, F. et al., J. Mater. Chem. A 5, 9402–9411 (2017) | 2017 | TiO2-TOPD | PCBM | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 20.3 |
| Chaudhary, B. et al., ChemSusChem 10, 2473–2479 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Chaudhary, B. et al., ChemSusChem 10, 2473–2479 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.6 |
| Chen, M. et al., Chem. Eng. J. 313, 791–800 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-drip | no | DMF | - | - | - | no | no | 7.9 |
| Chen, M. et al., Chem. Eng. J. 313, 791–800 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-drip | no | DMF | - | - | - | no | no | 7.3 |
| Chen, Z. et al., J. Power Sources 351, 123–129 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 7.4 |
| Chen, Z. et al., J. Power Sources 351, 123–129 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.3 |
| Chen, C. et al., ACS Energy Letters 2, 497–503 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 14.8 |
| Chen, C. et al., ACS Energy Letters 2, 497–503 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 18.7 |
| Chen, C. et al., ACS Energy Letters 2, 497–503 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | spiro-OMeTAD | Li+TBP+Cu(bpcm) | 18.5 |
| Chen, B.-A. et al., ACS Energy Lett. 2, 342–348 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 80 | 10 | na | spiro-OMeTAD | Li+TBP | 14.4 |
| Chen, J. Y. et al., Sol. Energy Mater. Sol. Cells 164, 47–55 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 13.9 |
| Chen, J. Y. et al., Sol. Energy Mater. Sol. Cells 164, 47–55 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 14.1 |
| Chen, J. Y. et al., Sol. Energy Mater. Sol. Cells 164, 47–55 (2017) | 2017 | TiO2 | C60 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 15.3 |
| Cheng, N. et al., Electrochim. Acta 246, 990–996 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | ethanol | DMF | - | - | - | no | no | 12.8 |
| Cheng, N. et al., Electrochim. Acta 246, 990–996 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | ethanol | DMF | - | - | - | CuPc | no | 16.6 |
| Cheng, N. et al., Electrochim. Acta 246, 990–996 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | ethanol | DMF | - | - | - | CuPc | no | 12.1 |
| Cheng, N. et al., Electrochim. Acta 246, 990–996 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | CuPc | no | 11.7 |
| Cheng, H. et al., Journal of Energy Chemistry (2017), doi:10.1016/j.jechem.2017.08.007 | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | TPADPP-2 | Li+TBP | 9.9 |
| Cheng, H. et al., Journal of Energy Chemistry (2017), doi:10.1016/j.jechem.2017.08.007 | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | PTZDPP-2 | Li+TBP | 8.2 |
| Cheng, H. et al., Journal of Energy Chemistry (2017), doi:10.1016/j.jechem.2017.08.007 | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | TPADPP-1 | Li+TBP | 5.1 |
| Cheng, H. et al., Journal of Energy Chemistry (2017), doi:10.1016/j.jechem.2017.08.007 | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.9 |
| Chiang, Y.-H. et al., ACS Appl. Mater. Interfaces 9, 2403–2409 (2017) | 2017 | TiO2 | mTiO2 | FA1-xCsxPb(SCN)yI3-y | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.4 |
| Chiang, Y.-H. et al., ACS Appl. Mater. Interfaces 9, 2403–2409 (2017) | 2017 | TiO2 | mTiO2 | FA1-xCsxPb(SCN)yI3-y | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 130 | 30 | na | spiro-OMeTAD | Li+TBP | 16.9 |
| Chiang, Y.-H. et al., ACS Appl. Mater. Interfaces 9, 2403–2409 (2017) | 2017 | TiO2 | mTiO2 | FA1-xCsxPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 130 | 30 | na | spiro-OMeTAD | Li+TBP | 14 |
| Cho, A.-N. et al., J. Mater. Chem. A 5, 7603–7611 (2017) | 2017 | TiO2 | PCBM | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | ACR-TPA | Li+TBP | 16.4 |
| Cho, A.-N. et al., J. Mater. Chem. A 5, 7603–7611 (2017) | 2017 | TiO2 | PCBM | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 16.3 |
| Cimaroli, A. J. et al., J. Mater. Chem. C 5, 10152–10157 (2017) | 2017 | C60-SAM | 0 | MA0.7FA0.3PbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | spiro-OMeTAD | Li+TBP | 11.8 |
| Cohen, B.-E. et al., Adv. Funct. Mater. 27, 1604733 (2017) | 2017 | TiO2 | 0 | MAPbBr3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 60 | na | no | no | 6.2 |
| Cohen, B.-E. et al., Adv. Funct. Mater. 27, 1604733 (2017) | 2017 | TiO2 | 0 | (PEA)2(MA)n-1PbnBr3n+1 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 60 | na | no | no | 6.3 |
| Cohen, B.-E. et al., Adv. Funct. Mater. 27, 1604733 (2017) | 2017 | TiO2 | 0 | MAPbBr3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 8.1 |
| Cohen, B.-E. et al., Adv. Funct. Mater. 27, 1604733 (2017) | 2017 | TiO2 | 0 | (PEA)2(MA)n-1PbnBr3n+1 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 8.5 |
| Conings, B. et al., ACS Appl. Mater. Interfaces 9, 8092–8099 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 17.5 |
| Conings, B. et al., ACS Appl. Mater. Interfaces 9, 8092–8099 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 9.1 |
| Kosta, I. et al., Electrochim. Acta 246, 1193–1199 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | electrodeposition-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 7.3 |
| Dao, Q. D. et al., Org. Electron. physics, Mater. Appl. 43, 156–161 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | toluene | DMSO | 120 | 10 | glovebox | C5PcH2 | no | 12.2 |
| Dar, M. I. et al., Adv. Funct. Mater. 27, 1701433 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.3 |
| Dar, M. I. et al., Adv. Funct. Mater. 27, 1701433 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 14.5 |
| Dar, M. I. et al., Adv. Funct. Mater. 27, 1701433 (2017) | 2017 | TiO2 | mTiO2 | FAPbBr3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 5.4 |
| Dar, M. I. et al., Adv. Funct. Mater. 27, 1701433 (2017) | 2017 | TiO2 | mTiO2 | FAPbBr3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 6.8 |
| Dar, M. I. et al., Adv. Funct. Mater. 27, 1701433 (2017) | 2017 | TiO2 | mTiO2 | MAPbBr3 | one-step | spin | no | DMF+HBr | 110 | 15 | na | spiro-OMeTAD | Li+TBP+FK209 | 1.4 |
| Deng, X. et al., J. Phys. Chem. Lett. 8, 3206–3210 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16.3 |
| Ding, B. et al., J. Mater. Chem. A 5, 6840–6848 (2017) | 2017 | TiO2 | 0 | FA0.1MA0.9PbI3 | one-step | spin | no | DMF | 120 | 20 | na | spiro-OMeTAD | Li+TBP | 20.4 |
| Dong, Q. et al., Nano Energy 38, 358–367 (2017) | 2017 | SnO2 | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 18.2 |
| Dong, Q. et al., Nano Energy 38, 358–367 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.3 |
| Dong, Q. et al., Nano Energy 38, 358–367 (2017) | 2017 | no | no | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.3 |
| Eze, V. O. et al., Org. Electron. physics, Mater. Appl. 46, 253–262 (2017) | 2017 | Wox | 0 | MAPbI3 | one-step | spin | no | GBL+NMP | na | na | na | spiro-OMeTAD | Li+TBP | 13.1 |
| Eze, V. O. et al., Org. Electron. physics, Mater. Appl. 46, 253–262 (2017) | 2017 | Wox | C60 | MAPbI3 | one-step | spin | no | GBL+NMP | na | na | na | spiro-OMeTAD | Li+TBP | 16.1 |
| Fan, R. et al., J. Mater. Chem. A 5, 12034–12042 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.5 |
| Fan, R. et al., J. Mater. Chem. A 5, 12034–12042 (2017) | 2017 | TiO2 | Au@TiO2-nanorod | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.8 |
| Fan, R. et al., J. Mater. Chem. A 5, 12034–12042 (2017) | 2017 | TiO2 | 0 | FAI,MAI,MACl,MABr,PbI2 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.2 |
| Fan, R. et al., J. Mater. Chem. A 5, 12034–12042 (2017) | 2017 | TiO2 | Au@TiO2-nanorod | FAI,MAI,MACl,MABr,PbI2 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 20.1 |
| Fei, C. et al., Adv. Energy Mater. 7, 1602017 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 90 | 30 | na | spiro-OMeTAD | Li+TBP | 14.8 |
| Fei, C. et al., Adv. Energy Mater. 7, 1602017 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | ethylacetate | DMF+thiourea | 90 | 30 | na | spiro-OMeTAD | Li+TBP | 18.5 |
| Fei, C. et al., Adv. Energy Mater. 7, 1602017 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+thiourea | 90 | 30 | na | spiro-OMeTAD | Li+TBP | 13.4 |
| Gaml, E. A. et al., Sol. Energy Mater. Sol. Cells 168, 8–13 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 11.6 |
| Gaml, E. A. et al., Sol. Energy Mater. Sol. Cells 168, 8–13 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PBDTT-FTTE | DIO | 11.6 |
| Gao, X. et al., Phys. Chem. Chem. Phys. 19, 4956–4961 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.9 |
| Gao, X. et al., Phys. Chem. Chem. Phys. 19, 4956–4961 (2017) | 2017 | TiO2 | TiO2-nanotube | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.8 |
| Gao, L.-L. et al., J. Mater. Chem. A 5, 1548–1557 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin-MAK | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 17.7 |
| Gao, C. et al., Chem. Eng. J. 325, 378–385 (2017) | 2017 | ZnO | ZnO-SnO2-nanorod | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 60 | na | P3HT | no | 12.3 |
| Grancini, G. et al., Nat. Commun. 8, 15684 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 10 | ambient | spiro-OMeTAD | no | 16 |
| Grancini, G. et al., Nat. Commun. 8, 15684 (2017) | 2017 | TiO2 | mTiO2 | 3% AVAI-MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 10 | ambient | spiro-OMeTAD | no | 14.6 |
| Grisorio, R. et al. ACS Energy Lett. 2, 1029–1034 (2017) | 2017 | TiO2 | mTiO2 | CsI, MAI, MABr, PbI2, PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | PTZ2 | Li+TBP+FK209 | 17.6 |
| Grisorio, R. et al. ACS Energy Lett. 2, 1029–1034 (2017) | 2017 | TiO2 | mTiO2 | CsI, MAI, MABr, PbI2, PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | PTZ1 | Li+TBP+FK209 | 2.1 |
| Grisorio, R. et al. ACS Energy Lett. 2, 1029–1034 (2017) | 2017 | TiO2 | mTiO2 | CsI, MAI, MABr, PbI2, PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.7 |
| Guo, Y. et al., Nano Energy 38, 193–200 (2017) | 2017 | Ni-Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 14.1 |
| Guo, Y. et al., Nano Energy 38, 193–200 (2017) | 2017 | Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 12.3 |
| Guo, J. J. et al., Sol. Energy 155, 121–129 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene+toluene | DMF+DMSO | 100 | 60 | dry air | no | no | 7.8 |
| Guo, J. J. et al., Sol. Energy 155, 121–129 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene+toluene | DMF+DMSO | 100 | 60 | dry air | ZnPcNO2-Oph | no | 14.5 |
| Guo, J. J. et al., Sol. Energy 155, 121–129 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene+toluene | DMF+DMSO | 100 | 60 | dry air | CuPcNO2-Oph | no | 12.8 |
| Guo, J. J. et al., Sol. Energy 155, 121–129 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene+toluene | DMF+DMSO | 100 | 60 | dry air | spiro-OMeTAD | Li+TBP | 18.9 |
| Ha, S.-J. et al., J. Mater. Chem. A 5, 1972–1977 (2017) | 2017 | PS | mTiO2 | MAPbI3 | one-step | spin | toluene | DMSO | 120 | 5 | na | PTAA | Li+TBP | 17.1 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | 0 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-PMMA | no | 6.5 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-PMMA | no | 16.2 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-polycarbonate | no | 12.6 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-PMMA | TBP | 17.3 |
| Habisreutinger, S. N. et al., Adv. Energy Mater. 7, 1601079 (2017) | 2017 | TiO2 | mAl2O3 | MAPbI3-xClx | one-step | spin | no | DMF+H3P | MS | na | na | SWNT-polycarbonate | TBP | 14 |
| Han, F. et al., J. Power Sources 359, 577–584 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 14.1 |
| Han, F. et al., J. Power Sources 359, 577–584 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+4MSA | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 17.6 |
| Han, F. et al., Electrochim. Acta 236, 122–130 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.1 |
| Han, F. et al., Electrochim. Acta 236, 122–130 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 14.4 |
| Han, F. et al., Appl. Surf. Sci. 408, 34–37 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | na | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.8 |
| Han, F. et al., Appl. Surf. Sci. 408, 34–37 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene+DMSO | na | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.8 |
| Hatamvand, M. et al., Optik (Stuttg). 140, 443–450 (2017) | 2017 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 0.3 |
| He, M. et al., Nat. Commun. 8, 16045 (2017) | 2017 | TiO2 | no | FA0.85MA0.15PbI2.55Br0.45 | one-step | MASP | no | DMSO | na | na | na | PTAA | Li+TBP | 20.4 |
| He, M. et al., Nat. Commun. 8, 16045 (2017) | 2017 | TiO2 | no | FA0.85MA0.15PbI2.55Br0.45 | one-step | spin 2-3 | no | DMSO | 150 | 20 | na | PTAA | Li+TBP | 18.3 |
| Hou, Y. et al., Adv. Funct. Mater. 27, 1700878 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12 |
| Hou, Y. et al., Adv. Funct. Mater. 27, 1700878 (2017) | 2017 | TiO2-SnO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.5 |
| Hou, Y. et al., Adv. Funct. Mater. 27, 1700878 (2017) | 2017 | TiO2-SnO2 | 0 | Cs5(MA0.17FA0.83)95Pb(I0.83Br0.17)3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.1 |
| Hou, X. et al., Electrochim. Acta 236, 351–358 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 6.1 |
| Hou, X. et al., Electrochim. Acta 236, 351–358 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 11.3 |
| Hou, X. et al., Electrochim. Acta 236, 351–358 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 7 |
| Hou, X. et al., Electrochim. Acta 236, 351–358 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 12 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.7 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | In2S3 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.2 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 15.3 |
| Hu, W. et al., J. Mater. Chem. A 5, 1434–1441 (2017) | 2017 | α‐Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 14.2 |
| Huang, Z.-L. et al., Superlattices Microstruct. 102, 94–102 (2017) | 2017 | ZnO | Al-ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | P3HT | Li | 10.5 |
| Huang, Z.-L. et al., Superlattices Microstruct. 102, 94–102 (2017) | 2017 | ZnO | ZnO-nanorod | MAPbI3 | two-step | spin | no | DMF | - | - | - | P3HT | Li | 8 |
| Huang, Y. T. et al., Electrochim. Acta 236, 131–139 (2017) | 2017 | 0 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 7.4 |
| Huang, Y. T. et al., Electrochim. Acta 236, 131–139 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 13 |
| Huang, Y. T. et al., Electrochim. Acta 236, 131–139 (2017) | 2017 | Nb2O5 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 14.6 |
| Huckaba, A. J. et al., Small Methods 1, 1700250 (2017) | 2017 | TiO2 | mTiO2-Li | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | no | no | 8.4 |
| Huckaba, A. J. et al., Small Methods 1, 1700250 (2017) | 2017 | TiO2 | mTiO2-Li | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | TiS2 | no | 13.2 |
| Huckaba, A. J. et al., Small Methods 1, 1700250 (2017) | 2017 | TiO2 | mTiO2-Li | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP+Co(II)TFSI | 18.1 |
| Islavath, N. et al., J. Energy Chem. 26, 584–591 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 1.6 |
| Islavath, N. et al., J. Energy Chem. 26, 584–591 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | CuSCN | no | 7.2 |
| Islavath, N. et al., J. Energy Chem. 26, 584–591 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5 |
| Jiang, X. et al., Sci. Rep. 7, 42564 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | no | no | 8.5 |
| Jiang, X. et al., Sci. Rep. 7, 42564 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | PEDOT | no | 17 |
| Jiang, X. et al., Sci. Rep. 7, 42564 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | spiro-OMeTAD | Li+TBP | 18.6 |
| Jiang, X. et al., Sci. Rep. 7, 42564 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Jiang, J. et al., J. Mater. Chem. A 5, 9514–9522 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 17.1 |
| Jiang, J. et al., J. Mater. Chem. A 5, 9514–9522 (2017) | 2017 | ITIC | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | na | na | na | spiro-OMeTAD | Li+TBP | 11.5 |
| Jiang, J. et al., J. Mater. Chem. A 5, 9514–9522 (2017) | 2017 | TiO2 | ITIC | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 15 | na | spiro-OMeTAD | Li+TBP | 20.1 |
| Jin, J. et al., ACS Appl. Mater. Interfaces 9, acsami.7b15310 (2017) | 2017 | TiO2 | no | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 16.4 |
| Jin, J. et al., ACS Appl. Mater. Interfaces 9, acsami.7b15310 (2017) | 2017 | TiO2 | no | MAI(PbI2)0.97(ZnCl2)0.03 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 5 | glovebox | spiro-OMeTAD | Li+TBP | 18.2 |
| Jodlowski, A. D. et al., Nat. Energy 2, 972–979 (2017) | 2017 | TiO2 | mTiO2-Li | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 45 | na | spiro-OMeTAD | Li+TBP+Co(II)TFSI | 18.9 |
| Jodlowski, A. D. et al., Nat. Energy 2, 972–979 (2017) | 2017 | TiO2 | mTiO2-Li | MA1–x GuaxPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO | 100 | 45 | na | spiro-OMeTAD | Li+TBP+Co(II)TFSI | 20.2 |
| Jung, K.-H. et al., J. Mater. Chem. A 5, 24790–24803 (2017) | 2017 | SnO2 | 0 | (FAPbI3)0.875(CsPbBr3)0.125 | one-step | spin | no | DMF | 145 | 40 | glovebox | spiro-OMeTAD | Li+TBP | 18.3 |
| Kavadiya, S. et al., Adv. Energy Mater. 7, 1700210 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-electrospray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12 |
| Kavadiya, S. et al., Adv. Energy Mater. 7, 1700210 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.3 |
| Ke, W. et al., Sci. Adv. 3, e1701293 (2017) | 2017 | TiO2 | mTiO2 | en-FASnI3 | one-step | spin | no | DMF+DMSO | 120 | 10 | na | PTAA | no | 7.1 |
| Kırbıyık, Ç. et al., Appl. Surf. Sci. 423, 521–527 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | toluene | GBL | 85 | 15 | glovebox | P3HT | no | 7.5 |
| Kırbıyık, Ç. et al., Appl. Surf. Sci. 423, 521–527 (2017) | 2017 | TiO2 | SAM | MAPbI3 | one-step | spin | toluene | GBL | 85 | 15 | glovebox | P3HT | no | 11.3 |
| Kim, D. H. et al., Adv. Mater. 29, 1606831 (2017) | 2017 | TiO2 | 0 | FA0.6MA0.4PbI(3-y)Cly | one-step | spin 2-3 | diethyl ether | DMF | 130 | 10 | na | spiro-OMeTAD | Li+TBP+FK102 | 19.7 |
| Kim, D. H. et al., Adv. Mater. 29, 1606831 (2017) | 2017 | TiO2 | 0 | FA0.6MA0.4PbI(3-y)Cly | one-step | spin 2-3 | diethyl ether | DMSO+GBL | 130 | 10 | na | spiro-OMeTAD | Li+TBP+FK102 | 15.7 |
| Kim, C. W. et al., Sci. Rep. 7, 6849 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.2 |
| Kim, N.-K. et al., Sci. Rep. 7, 4645 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.5 |
| Kim, W. et al., Electrochim. Acta 245, 734–741 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 150 | 40 | glovebox | spiro-OMeTAD | Li+TBP | 10.8 |
| Kim, W. et al., Electrochim. Acta 245, 734–741 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | two-step | dip-spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12.1 |
| Lee, W. et al., Org. Electron. 51, 404–409 (2017) | 2017 | 0 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 12.6 |
| Lee, W. et al., Org. Electron. 51, 404–409 (2017) | 2017 | PEIE-LiQ | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Lee, Y. et al., J. Mater. Chem. A 5, 12729–12734 (2017) | 2017 | SnO2 | 0 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | PTAA | Li+TBP | 13 |
| Lee, Y. et al., J. Mater. Chem. A 5, 12729–12734 (2017) | 2017 | TiO2 | 0 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | PTAA | Li+TBP | 17.7 |
| Lee, Y. et al., J. Mater. Chem. A 5, 12729–12734 (2017) | 2017 | TiO2-SnO2 | 0 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | PTAA | Li+TBP | 19.8 |
| Li, D. et al., Chem. Sci. 8, 4587–4594 (2017) | 2017 | PFN-2TNDI | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.2 |
| Li, D. et al., Chem. Sci. 8, 4587–4594 (2017) | 2017 | PFN-2TNDI | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16 |
| Li, D. et al., Chem. Sci. 8, 4587–4594 (2017) | 2017 | no | no | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 12 |
| Li, H. et al., RSC Adv. 7, 30422–30427 (2017) | 2017 | TiO2 | 0 | FA0.9Cs0.1PbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 8.7 |
| Li, H. et al., RSC Adv. 7, 30422–30427 (2017) | 2017 | TiO2 | PCBM | FA0.9Cs0.1PbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.8 |
| Li, B. et al., J. Power Sources 360, 11–20 (2017) | 2017 | TiO2 | mTiO2 | CsPbBr3-Cl | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6.2 |
| Li, B. et al., J. Power Sources 360, 11–20 (2017) | 2017 | TiO2 | mTiO2 | CsPbBr3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 5 |
| Li, H. et al., Sol. Energy Mater. Sol. Cells 168, 85–90 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.3 |
| Li, H. et al., Sol. Energy Mater. Sol. Cells 168, 85–90 (2017) | 2017 | TiO2-La | mTiO2 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.5 |
| Liu, Q. et al., ChemSusChem 10, 3098–3104 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 14.4 |
| Liu, Q. et al., ChemSusChem 10, 3098–3104 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+BPO | 17.5 |
| Liu, D. et al., RSC Adv. 7, 8295–8302 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 75 | na | spiro-OMeTAD | Li+TBP | 15.4 |
| Liu, D. et al., RSC Adv. 7, 8295–8302 (2017) | 2017 | Cd2SnO4 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 75 | na | spiro-OMeTAD | Li+TBP | 18.8 |
| Liu, C. et al., J. Phys. Chem. C 121, 6546–6553 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 6 |
| Liu, C. et al., J. Phys. Chem. C 121, 6546–6553 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+TBP | - | - | - | spiro-OMeTAD | Li+TBP | 12.6 |
| Liu, Y. et al., RSC Adv. 7, 1206–1214 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 8.3 |
| Liu, Y. et al., RSC Adv. 7, 1206–1214 (2017) | 2017 | TiO2-Ag | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 9.1 |
| Liu, Z. et al., J. Mater. Chem. A 5, 6597–6605 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | no | no | 1.8 |
| Liu, Z. et al., J. Mater. Chem. A 5, 6597–6605 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | NiOx | no | 16.7 |
| Liu, X. et al., ChemSusChem 10, 968–975 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | TPA-TPM | Li+TBP | 15.1 |
| Liu, X. et al., ChemSusChem 10, 968–975 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | DPA-TPM | Li+TBP | 9.3 |
| Liu, X. et al., ChemSusChem 10, 968–975 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | Ph-TPM | Li+TBP | 4.6 |
| Liu, X. et al., ChemSusChem 10, 968–975 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | TPA-TPM | Li+TBP | 16.8 |
| Liu, X. et al., ChemSusChem 10, 968–975 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | spiro-OMeTAD | Li+TBP | 15.5 |
| Liu, X. et al., ChemSusChem 10, 968–975 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | na | na | glovebox | spiro-OMeTAD | Li+TBP | 17.4 |
| Long, M. et al., Adv. Energy Mater. 7, 1601882 (2017) | 2017 | TiO2 | 0 | FAPbI3-xBrx | one-step | spin | no | DMF | 160 | 60 | na | spiro-OMeTAD | Li+TBP | 19.2 |
| Long, M. et al., Adv. Energy Mater. 7, 1601882 (2017) | 2017 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | na | na | na | spiro-OMeTAD | Li+TBP | 15.2 |
| Lu, J. et al., Adv. Energy Mater. 7, 1700444 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | na | spiro-OMeTAD | Li+TBP | 17 |
| Lu, J. et al., Adv. Energy Mater. 7, 1700444 (2017) | 2017 | TiO2 | 0 | MA1-2xEDAxPbI3 | one-step | spin | no | DMF | na | na | na | spiro-OMeTAD | Li+TBP | 18.6 |
| Lu, H. et al., Small 13, 1701535 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 105 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 16.9 |
| Luo, H. et al., Energy Technol. 5, 1814–1819 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | no | 16.3 |
| Luo, H. et al., Energy Technol. 5, 1814–1819 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO+LiI | 100 | 10 | na | spiro-OMeTAD | no | 18.3 |
| Luo, Q. et al., Adv. Funct. Mater. 27, 1702090 (2017) | 2017 | α‐Fe2O3 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 25 | glovebox | spiro-OMeTAD | Li+TBP | 15 |
| Luo, Q. et al., Adv. Funct. Mater. 27, 1702090 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 25 | glovebox | spiro-OMeTAD | Li+TBP | 13.9 |
| Luo, Q. et al., Adv. Funct. Mater. 27, 1702090 (2017) | 2017 | α‐Fe2O3 | m-α‐Fe2O3 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 25 | glovebox | spiro-OMeTAD | Li+TBP | 18.1 |
| Mabrouk, S. et al., Sustain. Energy Fuels 1, 2162–2171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 11.3 |
| Mabrouk, S. et al., Sustain. Energy Fuels 1, 2162–2171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+BMImI | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 18 |
| Mabrouk, S. et al., Sustain. Energy Fuels 1, 2162–2171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+Li | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.6 |
| Mabrouk, S. et al., Sustain. Energy Fuels 1, 2162–2171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF+Lil | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 17 |
| Mahmud, M. A. et al., Phys. Chem. Chem. Phys. 19, 21033–21045 (2017) | 2017 | ZnO | 0 | MA0.6FA0.4PbI3 | one-step | spin | no | DMF | 100 | 10 | na | FDT | Li+TBP | 12.9 |
| Mahmud, M. A. et al., Phys. Chem. Chem. Phys. 19, 21033–21045 (2017) | 2017 | ZnO | 0 | MA0.6FA0.4PbI3 | one-step | spin | no | DMF | 100 | 10 | na | FDT | F4TCNQ | 14.7 |
| Mahmud, M. A. et al., Sol. Energy Mater. Sol. Cells 159, 251–264 (2017) | 2017 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF+TBP | - | - | - | P3HT | Li+TBP | 8.8 |
| Mali, S. S. et al., Nanoscale 9, 3095–3104 (2017) | 2017 | TiO2 | 0 | MAPbI3-xBrx | one-step | spin 2-3 | toluene | DMSO+GBL | na | na | na | PTAA | Li+TBP | 16.9 |
| Mali, S. S. et al., Mater. Today Chem. 4, 53–63 (2017). | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | carbon+MAI | no | 13.9 |
| Mali, S. S. et al., Mater. Today Chem. 4, 53–63 (2017). | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 14 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanoflower | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 14.9 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 14.7 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanoflower | MAPbI3-xClx | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 15.9 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanoflower | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin | no | GBL | na | 10 | na | PTAA | Li+TBP | 17.6 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | spiro-OMeTAD | Li+TBP | 11.9 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanoflower | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | spiro-OMeTAD | Li+TBP | 15 |
| Mali, S. S. et al., J. Mater. Chem. A 5, 12340–12353 (2017) | 2017 | TiO2 | TiO2-nanorod | MAPbI3 | one-step | spin | no | GBL | na | 10 | na | spiro-OMeTAD | Li+TBP | 12.5 |
| Mu, C. et al., Adv. Energy Mater. 7, 1601297 (2017) | 2017 | TiO2 | 0 | FAPbI2.8Cl0.2 | one-step | spin | no | DMF | 100 | 50 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.4 |
| Mu, C. et al., Adv. Energy Mater. 7, 1601297 (2017) | 2017 | TiO2 | 0 | FAPbI3 | one-step | spin | no | DMF | 100 | 50 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 15.7 |
| Nia, N. Y. et al., ChemSusChem 10, 3854–3860 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | Li+TBP | 16.9 |
| Nia, N. Y. et al., ChemSusChem 10, 3854–3860 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.8 |
| Paek, S. et al., Adv. Mater. 29, 1606555 (2017) | 2017 | TiO2 | mTiO2-Li | PbI2, FAI, PbBr2, MABr | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | FA-CN | no | 18.9 |
| Paek, S. et al., Adv. Mater. 29, 1606555 (2017) | 2017 | TiO2 | mTiO2-Li | PbI2, FAI, PbBr2, MABr | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | TPA-CN | no | 17.5 |
| Paek, S. et al., Adv. Mater. 29, 1606555 (2017) | 2017 | TiO2 | mTiO2-Li | PbI2, FAI, PbBr2, MABr | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 19.2 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.3 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.1 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.9 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.8 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.8 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2 | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.3 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 20.1 |
| Peng, J. et al., Adv. Energy Mater. 7, 1601768 (2017) | 2017 | TiO2-In | mTiO2 | Cs0.05(MA0.17FA0.83)0.98Pb(I83Br0.17) | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 19.6 |
| Pham, N. D. et al., J. Mater. Chem. A 5, 5195–5203 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 17.1 |
| Pham, N. D. et al., J. Mater. Chem. A 5, 5195–5203 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 18.9 |
| Prathapani, S. et al., Appl. Mater. Today 7, 112–119 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | na | glovebox | spiro-OMeTAD | Li+TBP | 8.1 |
| Pratyusha, T. et al., Mater. Today Proc. 4, 6820–6826 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCDTBT-PCPDTBT | no | 5.1 |
| Pratyusha, T. et al., Mater. Today Proc. 4, 6820–6826 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCDTBT | no | 4.4 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | FAPbI2.85Br0.15 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.6 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | FAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.5 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | Cs0.1FA0.9MA0.34PbI2.865Br0.135 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 19.3 |
| Qiu, W. et al., Adv. Funct. Mater. 27, 1700920 (2017) | 2017 | TiO2 | PCBM | Cs0.2FA0.8PbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.5 |
| Qiu, L. et al., J. Phys. Chem. B 122, acs.jpcb.7b03921 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 60 | dry air | spiro-OMeTAD | Li+TBP | 18.5 |
| Qiu, L. et al., J. Phys. Chem. B 122, acs.jpcb.7b03921 (2017) | 2017 | no | no | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 60 | dry air | spiro-OMeTAD | Li+TBP | 13.5 |
| Qiu, Z. et al., J. Am. Ceram. Soc. 100, 176–184 (2017) | 2017 | ZnO | PCBM | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | P3HT | no | 7.5 |
| Rajmohan, G. D. et al., Thin Solid Films 636, 307–313 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | dry air | spiro-OMeTAD | Li+TBP | 9.3 |
| Ren, Y. K. et al., J. Alloys Compd. 705, 205–210 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 9.6 |
| Ren, Y. K. et al., J. Alloys Compd. 705, 205–210 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 20 | na | spiro-OMeTAD | Li+TBP | 16.4 |
| Sanehira, E. M. et al., Sci. Adv. 3, eaao4204 (2017) | 2017 | TiO2 | 0 | CsPbI3 QD | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 8.5 |
| Sanehira, E. M. et al., Sci. Adv. 3, eaao4204 (2017) | 2017 | TiO2 | 0 | FA-CsPbI3 QD | two-step | spin-dip | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 13.4 |
| Seo, G. et al., ACS Energy Lett. 2, 1705–1710 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.7 |
| Shai, X. et al., Nano Energy 36, 213–222 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.7 |
| Shai, X. et al., Nano Energy 36, 213–222 (2017) | 2017 | TiO2 | 0 | MASr0.05Pb0.95I3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.3 |
| Shi, B. et al., Sol. Energy Mater. Sol. Cells 168, 214–220 (2017) | 2017 | TiO2 | 0 | MAPbI3-xBrx | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 150 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 17.9 |
| Shi, B. et al., Sol. Energy Mater. Sol. Cells 168, 214–220 (2017) | 2017 | TiO2 | 0 | MAPbI3-xBrx | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 150 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 15.3 |
| Shi, B. et al., Sol. Energy Mater. Sol. Cells 168, 214–220 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 13.2 |
| Shi, B. et al., Sol. Energy Mater. Sol. Cells 168, 214–220 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | two-step | CVD | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 13.1 |
| Sidhik, S. et al., J. Phys. Chem. C 121, 4239–4245 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | ethoxyethane | DMF+DMSO | 100 | 3 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 12.3 |
| Sin, D. H. et al., ACS Appl. Mater. Interfaces 9, 18103–18112 (2017) | 2017 | ZnO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3.1 |
| Sin, D. H. et al., ACS Appl. Mater. Interfaces 9, 18103–18112 (2017) | 2017 | ZnO-PEG | no | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.5 |
| Sin, D. H. et al., ACS Appl. Mater. Interfaces 9, 18103–18112 (2017) | 2017 | ZnO-PEG | no | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.1 |
| Sudchanham, J. et al., ChemistrySelect 2, 369–374 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | ambient | spiro-OMeTAD | Li+TBP+FK102 | 11.7 |
| Sun, M. et al., Appl. Surf. Sci. 416, 124–132 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 7.1 |
| Sun, M. et al., Appl. Surf. Sci. 416, 124–132 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Me-QTPA | no | 9.1 |
| Sun, M. et al., Appl. Surf. Sci. 416, 124–132 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Me-BPZTPA | no | 8.2 |
| Sun, M. et al., Appl. Surf. Sci. 416, 124–132 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | no | 5.5 |
| Sun, M. et al., Appl. Surf. Sci. 416, 124–132 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.7 |
| Sun, C. et al., J. Alloys Compd. 722, 196–206 (2017) | 2017 | BaSnO3 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 11 |
| Sun, M. et al., J. Mater. Chem. A 5, 13448–13456 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 15.5 |
| Sun, M. et al., J. Mater. Chem. A 5, 13448–13456 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO+2-pyridylthiourea | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 18.2 |
| Tong, G. et al., RSC Adv. 7, 19457–19463 (2017) | 2017 | CdS | 0 | MAPbI3 | two-step | vasp | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 14.7 |
| Torabi, N. et al., Org. Electron. 48, 211–216 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 5.5 |
| Torabi, N. et al., Org. Electron. 48, 211–216 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | CuPC | no | 14.9 |
| Torabi, N. et al., Org. Electron. 48, 211–216 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.4 |
| Tu, Y. et al., Sci. Rep. 7, 44603 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 15.6 |
| Tu, Y. et al., Sci. Rep. 7, 44603 (2017) | 2017 | TiO2 | mTiO2 | MAPbI2.86Br0.14 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 18 |
| Upama, M. B. et al., Org. Electron. 50, 279–289 (2017) | 2017 | PCBM | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 13.9 |
| Wang, S. et al., Sol. Energy Mater. Sol. Cells 167, 173–177 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 19.6 |
| Wang, L.-Y. et al., Nanoscale 9, 17893–17901 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | di+isopropyl ether | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 19.1 |
| Wang, Z. et al., Nat. Energy 2, 17135 (2017) | 2017 | SnO2 | PCBM-N-DPBI | BA0.05(FA0.83Cs0.17)0.95Pb(I0.8Br0.2)3 | one-step | spin | no | DMF+HI+HBr | 175 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 20.5 |
| Wang, Z. et al., Nat. Energy 2, 17135 (2017) | 2017 | SnO2 | PCBM-N-DPBI | FA0.83Cs0.17Pb(I0.6Br0.4)3 | one-step | spin | no | DMF+HI+HBr | 175 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 16.9 |
| Wang, Z. et al., Nat. Energy 2, 17135 (2017) | 2017 | SnO2 | PCBM-N-DPBI | BA0.09(FA0.83Cs0.17)0.91Pb(I0.6Br0.4)3 | one-step | spin | no | DMF+HI+HBr | 175 | 80 | glovebox | spiro-OMeTAD | Li+TBP | 16.6 |
| Wang, Z. et al., Adv. Mater. 29, 1604186 (2017) | 2017 | C60-N-DPBI | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 18.3 |
| Wang, Z. et al., Adv. Mater. 29, 1604186 (2017) | 2017 | C60 | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 17 |
| Wang, X. et al., Electrochim. Acta 245, 839–845 (2017) | 2017 | TiO2 | TiO2-Er-Yb-nanorod | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 13.4 |
| Wang, X. et al., Electrochim. Acta 245, 839–845 (2017) | 2017 | TiO2 | TiO2-Er-nanorod | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 12.1 |
| Wang, X. et al., Electrochim. Acta 245, 839–845 (2017) | 2017 | TiO2 | TiO2-nanorod | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | spiro-OMeTAD | Li+TBP | 11.1 |
| Wang, X. et al., Optik (Stuttg). 150, 111–116 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| Wang, X. et al., Optik (Stuttg). 150, 111–116 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.2 |
| Wang, M., Sci. Bull. 62, 249–255 (2017) | 2017 | no | no | FAPbI3 | two-step | spin | no | na | - | - | - | spiro-OMeTAD | no | 15.1 |
| Wang, M., Sci. Bull. 62, 249–255 (2017) | 2017 | no | no | FAPbI3 | two-step | spin | no | na | - | - | - | spiro-OMeTAD | no | 10.6 |
| Wang, W.-T. et al., ACS Appl. Mater. Interfaces 9, 10743–10751 (2017) | 2017 | ZnO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 16.3 |
| Wang, W.-T. et al., ACS Appl. Mater. Interfaces 9, 10743–10751 (2017) | 2017 | ZnO | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.1 |
| Wang, F. et al., J. Phys. Chem. C 121, 1562–1568 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | toluene | DMSO | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 16.4 |
| Wang, F. et al., J. Phys. Chem. C 121, 1562–1568 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | toluene | DMSO | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 14.6 |
| Wang, L. et al., Electrochim. Acta 235, 640–645 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 9.2 |
| Wang, H. et al., ACS Appl. Mater. Interfaces 9, 21756–21762 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin 2-3 | no | DMSO+GBL | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 16.7 |
| Wang, L. et al., Energy Storage Mater. 7, 40–47 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16 |
| Wang, L. et al., Energy Storage Mater. 7, 40–47 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Wang, L. et al., Energy Storage Mater. 7, 40–47 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Wang, L. et al., Energy Storage Mater. 7, 40–47 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 12.2 |
| Wang, L. et al., Energy Storage Mater. 7, 40–47 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 11.4 |
| Wei, W. et al., J. Mater. Chem. A 5, 7749–7752 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 10.1 |
| Wei, W. et al., Ind. Eng. Chem. Res. 56, 1803–1809 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 4.7 |
| Wei, W. et al., Ind. Eng. Chem. Res. 56, 1803–1809 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 4.4 |
| Wei, W. et al., Ind. Eng. Chem. Res. 56, 1803–1809 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF+graphene | - | - | - | no | no | 4.7 |
| Wei, W. et al., Ind. Eng. Chem. Res. 56, 1803–1809 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF+MCN | - | - | - | no | no | 10.4 |
| Wu, S. et al., J. Power Sources 359, 303–310 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.3 |
| Wu, S. et al., J. Power Sources 359, 303–310 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+CuPc(tBu)4 | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 17.3 |
| Wu, F. and Zhu, L., Sol. Energy Mater. Sol. Cells 167, 1–6 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | na | glovebox | spiro-OMeTAD | Li+TBP | 12.9 |
| Wu, F. and Zhu, L., Sol. Energy Mater. Sol. Cells 167, 1–6 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+H2O | 100 | na | glovebox | spiro-OMeTAD | Li+TBP | 19.1 |
| Wu, F. et al., Dye. Pigment. 143, 356–360 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | na | JY5 | Li+TBP | 16.9 |
| Wu, F. et al., Dye. Pigment. 143, 356–360 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | na | X51 | Li+TBP | 13.2 |
| Wu, F. et al., Dye. Pigment. 143, 356–360 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | na | spiro-OMeTAD | Li+TBP | 16.2 |
| Wu, T. et al., J. Power Sources 365, 1–6 (2017) | 2017 | TiO2 | 0 | Cs0.05(MA0.17FA0.83)0.95Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 16 |
| Wu, T. et al., J. Power Sources 365, 1–6 (2017) | 2017 | TiO2 | 0 | Cs0.05(MA0.17FA0.83)0.95Pb(I0.83Br0.17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO+NMP | 100 | 60 | na | spiro-OMeTAD | Li+TBP | 19.6 |
| Xiang, W. et al., J. Mater. Chem. A 5, 5486–5494 (2017) | 2017 | TiO2 | no | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 13.3 |
| Xiang, W. et al., J. Mater. Chem. A 5, 5486–5494 (2017) | 2017 | TiO2 | no | MAPbI3 | one-step | spin | chlorobenzene | DMF+PDMSurea | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.4 |
| Xiao, G. et al., Ceram. Int. 43, 12534–12539 (2017) | 2017 | TiO2 | TiO2-nanorod | MAPbI3-xBrx | two-step | spin | no | DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 16.2 |
| Xiao, M. et al., J. Am. Chem. Soc. 139, 3378–3386 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | P3OT | no | 6.9 |
| Xiao, M. et al., J. Am. Chem. Soc. 139, 3378–3386 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | P3DT | no | 6.6 |
| Xiao, M. et al., J. Am. Chem. Soc. 139, 3378–3386 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | P3DDT | no | 3.9 |
| Xiao, M. et al., J. Am. Chem. Soc. 139, 3378–3386 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 60 | glovebox | P3HT | no | 9.6 |
| Xiao, Y. et al., J. Power Sources 342, 489–494 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 10.3 |
| Xiao, Y. et al., J. Power Sources 342, 489–494 (2017) | 2017 | TiO2 | mTiO2-W | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | no | no | 12.1 |
| Xie, X. et al., Org. Electron. 44, 120–125 (2017) | 2017 | PCBM | 0 | MAPbI3 | two-step | evap-spin | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 7.9 |
| Xie, X. et al., Org. Electron. 44, 120–125 (2017) | 2017 | PFN ITO kısmına alsak mı | PCBM | MAPbI3 | two-step | evap-spin | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 12.9 |
| Xu, Z. et al., J. Phys. Chem. C 121, 24389–24396 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | no | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 8.5 |
| Yang, G. et al., J. Mater. Chem. A 5, 1658–1666 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 90 | 60 | ambient | P3HT | no | 11.4 |
| Yang, G. et al., J. Mater. Chem. A 5, 1658–1666 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.3 |
| Yang, G. et al., Small 13, 1601769 (2017) | 2017 | Y-SnO2 | 0 | MAPbI3 | one-step | spin 2-3 | diethyl ether | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 17.3 |
| Yang, G. et al., Small 13, 1601769 (2017) | 2017 | SnO2 | 0 | MAPbI3 | one-step | spin 2-3 | diethyl ether | DMF+DMSO | 100 | 15 | glovebox | spiro-OMeTAD | Li+TBP | 13.4 |
| Ye, J. et al., Appl. Surf. Sci. 407, 427–433 (2017) | 2017 | TiO2 | mTiO2 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 105 | 60 | na | spiro-OMeTAD | Li+TBP | 18.5 |
| Ye, T. et al., ACS Appl. Mater. Interfaces 9, 2358–2368 (2017) | 2017 | TiO2 | mTiO2 | FA0.81MA0.15Pb(I0.836Br0.15)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 20.6 |
| Ye, T. et al., ACS Appl. Mater. Interfaces 9, 2358–2368 (2017) | 2017 | TiO2 | mTiO2 | FA0.81MA0.15Pb(I0.836Br0.15)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 17.1 |
| Yu, Y. et al., ACS Appl. Mater. Interfaces 9, 23624–23634 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | na | dry air | spiro-OMeTAD | Li+TBP | 15.4 |
| Yu, Y. et al., ACS Appl. Mater. Interfaces 9, 23624–23634 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | n+hexane | DMF+DMSO | 100 | na | dry air | spiro-OMeTAD | Li+TBP | 15.7 |
| Yu, M. et al., Phys. Chem. Chem. Phys. 19, 19922–19927 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 15.8 |
| Yu, M. et al., Phys. Chem. Chem. Phys. 19, 19922–19927 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 15.7 |
| Zhang, T. et al., Sci. Adv. 3, e1700841 (2017) | 2017 | TiO2 | no | CsPbI3·xEDAI2 | one-step | spin | no | DMF | 150 | 2 | na | spiro-OMeTAD | Li+TBP | 11.7 |
| Zhang, C. et al., Nanoscale 9, 2852–2864 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 120 | 30 | na | spiro-OMeTAD | Li+TBP+FK209 | 15.1 |
| Zhang, C. et al., Nanoscale 9, 2852–2864 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 120 | 30 | na | spiro-OMeTAD | Li+TBP+FK209 | 12 |
| Zhang, C. et al., Nanoscale 9, 2852–2864 (2017) | 2017 | TiO2 | mTiO2-Au | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 120 | 30 | na | spiro-OMeTAD | Li+TBP+FK209 | 16 |
| Zhang, C. et al., Nanoscale 9, 2852–2864 (2017) | 2017 | TiO2 | mTiO2-Au | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 120 | 30 | na | spiro-OMeTAD | Li+TBP+FK209 | 10.7 |
| Zhang, C. et al., Energy Procedia 105, 793–798 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 13.5 |
| Zhang, F. et al., Nano Energy 41, 469–475 (2017) | 2017 | TiO2 | mTiO2 | (FAI)0.81(PbI2)0.85(MABr)0.15(PbBr2)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | Z26 | Li+TBP+FK209 | 20.1 |
| Zhang, F. et al., Nano Energy 41, 469–475 (2017) | 2017 | TiO2 | mTiO2 | (FAI)0.81(PbI2)0.85(MABr)0.15(PbBr2)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | Z25 | Li+TBP+FK209 | 16.9 |
| Zhang, F. et al., Nano Energy 41, 469–475 (2017) | 2017 | TiO2 | mTiO2 | (FAI)0.81(PbI2)0.85(MABr)0.15(PbBr2)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | Li+TBP+FK209 | 20.6 |
| Zhang, X. et al., Sol. Energy 148, 70–77 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 11.8 |
| Zhang, X. et al., Sol. Energy 148, 70–77 (2017) | 2017 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF+Al | MS | na | na | spiro-OMeTAD | Li+TBP | 13.6 |
| Zhang, W. et al., ACS Appl. Mater. Interfaces 9, 38467–38476 (2017) | 2017 | ZnO | 0 | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 17.5 |
| Zhang, W. et al., ACS Appl. Mater. Interfaces 9, 38467–38476 (2017) | 2017 | ZnO | PCBM | MAPbI3 | two-step | spin-dip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 19.1 |
| Zhang, M.-D. et al., Dye. Pigment. 146, 589–595 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | na | 100 | 10 | glovebox | SYN1 | Li+TBP | 13.1 |
| Zhang, M.-D. et al., Dye. Pigment. 146, 589–595 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | na | 100 | 10 | glovebox | PARA1 | Li+TBP | 11.4 |
| Zhang, M.-D. et al., Dye. Pigment. 146, 589–595 (2017) | 2017 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | na | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP | 12 |
| Zhao, P. et al. J. Mater. Chem. A 5, 7905–7911 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 17.3 |
| Zhao, P. et al. J. Mater. Chem. A 5, 7905–7911 (2017) | 2017 | TiO2 | mTiO2 | MA1-xKxPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 19.3 |
| Zhao, Y. et al., J. Power Sources 359, 147–156 (2017) | 2017 | TiO2 | mTiO2-Li | FAPbI3 | two-step | spin-drip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | no | 17.7 |
| Zhao, Y. et al., J. Power Sources 359, 147–156 (2017) | 2017 | TiO2 | mTiO2-Li | FA0.6MA0.4PbI3 | two-step | spin-drip | no | DMF+DMSO | - | - | - | spiro-OMeTAD | no | 19.3 |
| Zheng, X. et al., Nano Lett. 17, 2496–2505 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 15.2 |
| Zheng, X. et al., Nano Lett. 17, 2496–2505 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 14.6 |
| Zheng, X. et al., Nano Lett. 17, 2496–2505 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 10.7 |
| Zheng, Y.-Z. et al., J. Phys. Chem. Solids 107, 55–61 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | na | na | na | spiro-OMeTAD | Li+TBP | 10.1 |
| Zheng, Y.-Z. et al., J. Phys. Chem. Solids 107, 55–61 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 90 | 20 | na | spiro-OMeTAD | Li+TBP | 6.5 |
| Zheng, Y.-Z. et al., J. Phys. Chem. Solids 107, 55–61 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 80 | 20 | na | spiro-OMeTAD | Li+TBP | 8.9 |
| Zheng, Y.-Z. et al., J. Phys. Chem. Solids 107, 55–61 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 70 | 20 | na | spiro-OMeTAD | Li+TBP | 12.7 |
| Zheng, Y.-Z. et al., J. Phys. Chem. Solids 107, 55–61 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 60 | 20 | na | spiro-OMeTAD | Li+TBP | 11.2 |
| Zheng, Y.-Z. et al., J. Phys. Chem. Solids 107, 55–61 (2017) | 2017 | ZnO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 50 | 20 | na | spiro-OMeTAD | Li+TBP | 10.9 |
| Zheng, X. et al., Nano Energy 38, 1–11 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 19.6 |
| Zheng, X. et al., Nano Energy 38, 1–11 (2017) | 2017 | SnO2 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 18.8 |
| Zheng, L. et al., Energy Procedia 105, 188–193 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.3 |
| Zheng, L. et al., Energy Procedia 105, 188–193 (2017) | 2017 | no | no | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.1 |
| Zheng, J. et al., Sol. Energy Mater. Sol. Cells 168, 165–171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | blowdry | no | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.4 |
| Zheng, J. et al., Sol. Energy Mater. Sol. Cells 168, 165–171 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 15.6 |
| Zheng, L. et al., ACS Appl. Mater. Interfaces 9, 14129–14135 (2017) | 2017 | TiO2 | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.1 |
| Zheng, L. et al., ACS Appl. Mater. Interfaces 9, 14129–14135 (2017) | 2017 | PTEBS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 15.4 |
| Zheng, L. et al., ACS Appl. Mater. Interfaces 9, 14129–14135 (2017) | 2017 | no | no | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 7.8 |
| Zong, X. et al., Tetrahedron 73, 3398–3405 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Q221 | Li+TBP | 10.4 |
| Zong, X. et al., Tetrahedron 73, 3398–3405 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Q222 | Li+TBP | 8.9 |
| Zong, X. et al., Tetrahedron 73, 3398–3405 (2017) | 2017 | TiO2 | mTiO2 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 10.1 |
| Zuo, L. et al., Sci. Adv. 3, e1700106 (2017) | 2017 | SnO2 | no | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18 |
| Zuo, L. et al., Sci. Adv. 3, e1700106 (2017) | 2017 | SnO2 | no | MAPbI3-xClx | two-step | spin | no | DMF+PAA | - | - | - | spiro-OMeTAD | Li+TBP | 19.6 |
| Zuo, L. et al., Sci. Adv. 3, e1700106 (2017) | 2017 | SnO2 | no | MAPbI3-xClx | two-step | spin | no | DMF+PEI | - | - | - | spiro-OMeTAD | Li+TBP | 16.7 |
| Zuo, L. et al., Sci. Adv. 3, e1700106 (2017) | 2017 | SnO2 | no | MAPbI3-xClx | two-step | spin | no | DMF+PVP | - | - | - | spiro-OMeTAD | Li+TBP | 20.2 |
| Zuo, L. et al., Nano Lett. 17, 269–275 (2017) | 2017 | SnO2 | 0 | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 17.2 |
| Zuo, L. et al., Nano Lett. 17, 269–275 (2017) | 2017 | SnO2 | PA-SAM | MAPbI3-xClx | two-step | spin-drip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.8 |
| Adnan, M. and Lee, J. K., Sci. Rep. 8, 2168 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | two-step | dipping | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 12.4 |
| Amini, M. et al., J. Mater. Chem. A 6, 2632–2642 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 15.1 |
| Amini, M. et al., J. Mater. Chem. A 6, 2632–2642 (2018) | 2018 | P123-ib | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | ambient | spiro-OMeTAD | Li+TBP | 16.7 |
| Bashir, A. et al., Nanoscale 10, 2341–2350 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3-5AVAI | one-step | spin | no | GBL | na | na | na | no | no | 11.3 |
| Bashir, A. et al., Nanoscale 10, 2341–2350 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3-5AVAI | one-step | spin | no | GBL | na | na | na | no | no | 9.3 |
| Bashir, A. et al., Nanoscale 10, 2341–2350 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3-5AVAI | one-step | spin | no | GBL | na | na | na | Co3O4 | no | 13.3 |
| Bashir, A. et al., Nanoscale 10, 2341–2350 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3-5AVAI | one-step | spin | no | GBL | na | na | na | Co3O4 | no | 11.7 |
| Chen, T.-P. et al., Adv. Energy Mater. 8, 1701722 (2018) | 2018 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.3 |
| Chen, T.-P. et al., Adv. Energy Mater. 8, 1701722 (2018) | 2018 | 2D titania | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Chen, T.-P. et al., Adv. Energy Mater. 8, 1701722 (2018) | 2018 | no | no | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | spiro-OMeTAD | Li+TBP | 7.2 |
| Chen, R. et al., Energy Fuels 2, 1093–1100 (2018) | 2018 | TiO2 | 0 | MAPb1-xClx | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 13.2 |
| Chen, R. et al., Energy Fuels 2, 1093–1100 (2018) | 2018 | TiO2 | 0 | MAPb1-xZnxI3-yCly | one-step | spin | no | DMF | MS | na | na | spiro-OMeTAD | Li+TBP | 16.9 |
| Christians, J. A. et al., Nat. Energy 3, 68–74 (2018) | 2018 | TiO2 | mTiO2 | (FA0.76MA0.21Cs0.03)0.67Pb(I0.89Br0.11)2.56 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 3 | glovebox | spiro-OMeTAD | Li+TBP | 19.6 |
| Christians, J. A. et al., Nat. Energy 3, 68–74 (2018) | 2018 | TiO2 | mTiO2 | (FA0.76MA0.21Cs0.03)0.67Pb(I0.89Br0.11)2.56 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 3 | glovebox | spiro-OMeTAD | Li+TBP | 14.4 |
| Christians, J. A. et al., Nat. Energy 3, 68–74 (2018) | 2018 | SnO2 | mTiO2 | (FA0.76MA0.21Cs0.03)0.67Pb(I0.89Br0.11)2.56 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | EH44 | EH44-ox+TBP | 12.3 |
| Christians, J. A. et al., Nat. Energy 3, 68–74 (2018) | 2018 | TiO2 | mTiO2 | (FA0.76MA0.21Cs0.03)0.67Pb(I0.89Br0.11)2.56 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | EH44 | EH44-ox+TBP | 16.8 |
| Deng, X. et al., Superlattices Microstruct. 117, 283–287 (2018) | 2018 | TiO2 | Y-TiO2-nanorod | MAPbI3-xBrx | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 18.1 |
| Deng, X. et al., Superlattices Microstruct. 117, 283–287 (2018) | 2018 | TiO2 | TiO2-nanorod | MAPbI3-xBrx | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP+FK209 | 16.4 |
| Domanski, K. et al., Nat. Energy 3, 61–67 (2018) | 2018 | TiO2 | mTiO2-Li | Cs5(FA83MA17)95Pb(I83Br17)3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | dry air | spiro-OMeTAD | Li+TBP+FK209 | 20.2 |
| Draguta, S. et al. Energy Environ. Sci. 11, 960–969 (2018) | 2018 | TiO2 | 0 | FAI, PbI2, MABr, PbBr2,CsI | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 18.8 |
| Draguta, S. et al. Energy Environ. Sci. 11, 960–969 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 3 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.8 |
| Gomez, A. et al., Nano Energy 45, 94–100 (2018) | 2018 | TiO2 | mTiO2-Li | FAI, PbI2, MABr, PbBr2, CsI | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.3 |
| Guo, Y. et al., ACS Appl. Energy Mater. acsaem.8b00094 (2018). doi:10.1021/acsaem.8b00094 | 2018 | IL/PCBM | Nb2O5 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 18.8 |
| Guo, Y. et al., ACS Appl. Energy Mater. acsaem.8b00094 (2018). doi:10.1021/acsaem.8b00094 | 2018 | IL | Nb2O5 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 16.4 |
| Guo, Y. et al., ACS Appl. Energy Mater. acsaem.8b00094 (2018). doi:10.1021/acsaem.8b00094 | 2018 | PCBM | Nb2O5 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 5 | na | spiro-OMeTAD | Li+TBP | 16.6 |
| Guo, Y. et al., Sol. Energy Mater. Sol. Cells 178, 186–192 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF | 90 | 5 | na | spiro-OMeTAD | Li+TBP | 12.7 |
| Guo, Y. et al., Sol. Energy Mater. Sol. Cells 178, 186–192 (2018) | 2018 | TiO2 | CdS | MAPbI3 | one-step | spin | no | DMF | 90 | 5 | na | spiro-OMeTAD | Li+TBP | 16 |
| Hou, Q. et al., ChemElectroChem 5, 725 (2018) | 2018 | α‐Fe2O3 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 12.1 |
| Hou, Q. et al., ChemElectroChem 5, 725 (2018) | 2018 | α‐Fe2O3 | PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 20 | glovebox | spiro-OMeTAD | Li+TBP | 14.2 |
| Jiang, H. et al., ACS Appl. Energy Mater. 1, 900–909 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 16.9 |
| Jiang, H. et al., ACS Appl. Energy Mater. 1, 900–909 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL+HaHc | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 18.7 |
| Kogo, A. et al., ACS Appl. Mater. Interfaces 10, 2224–2229 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 105 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 13.2 |
| Kogo, A. et al., ACS Appl. Mater. Interfaces 10, 2224–2229 (2018) | 2018 | 0 | mTiO2-brookite | MAPbI3 | one-step | spin | no | DMF+DMSO | 105 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 13 |
| Kogo, A. et al., ACS Appl. Mater. Interfaces 10, 2224–2229 (2018) | 2018 | SnO2 | mTiO2-brookite | MAPbI3 | one-step | spin | no | DMF+DMSO | 105 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 18.6 |
| Kogo, A. et al., ACS Appl. Mater. Interfaces 10, 2224–2229 (2018) | 2018 | TiO2 | mTiO2-brookite | MAPbI3 | one-step | spin | no | DMF+DMSO | 105 | 10 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 20.2 |
| Li, F. et al., Adv. Funct. Mater. 28, 1706377 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | no | 17.7 |
| Li, F. et al., Adv. Funct. Mater. 28, 1706377 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene+PF1 | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | no | 18.7 |
| Li, F. et al., Adv. Funct. Mater. 28, 1706377 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene+ F+N2200 | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | no | 18.4 |
| Li, F. et al., Adv. Funct. Mater. 28, 1706377 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene+ PF0 | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | no | 18.1 |
| Li, F. et al., Adv. Funct. Mater. 28, 1706377 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene+N2200 | DMSO+GBL | 100 | 10 | na | spiro-OMeTAD | no | 17.9 |
| Li, K. et al., Sci. Rep. 8, 442 (2018) | 2018 | C60 | 0 | MAPbI3 | two-step | evap-spin | no | na | - | - | - | spiro-OMeTAD | Li+TBP | 15 |
| Li, B. et al., Nat. Commun. 9, 1076 (2018) | 2018 | TiO2 | mTiO2 | CsPbI3 | one-step | spin | no | DMF+DMSO+PVP | 300 | 5 | glovebox | spiro-OMeTAD | no | 10.7 |
| Li, B. et al., Nat. Commun. 9, 1076 (2018) | 2018 | TiO2 | mTiO2 | CsPbI2Br | one-step | spin | no | DMF+DMSO+PVP | 300 | 5 | glovebox | spiro-OMeTAD | no | 8 |
| Liu, N. et al., J. Mater. Chem. A 6, 6806–6814 (2018) | 2018 | SnO2 | 0 | MAxFA1-xPbI3-yBry | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 20.6 |
| Liu, N. et al., J. Mater. Chem. A 6, 6806–6814 (2018) | 2018 | SnO2 | 0 | MAxFA1-xPbI3-yBry | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 18.5 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V885 | Li+TBP+FK209 | 18.9 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V911 | Li+TBP+FK209 | 18.9 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V886 | Li+TBP+FK209 | 18.5 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V1no39 | Li+TBP+FK209 | 17.4 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V946 | Li+TBP+FK209 | 17.1 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V957 | Li+TBP+FK209 | 17.1 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V928 | Li+TBP+FK209 | 16.5 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V9no8 | Li+TBP+FK209 | 16.5 |
| Magomedov, A. et al., Adv. Funct. Mater. 28, 1704351 (2018) | 2018 | TiO2 | mTiO2-Li | Cs0.1(MA0.15FA0.85)0.9Pb(I0.85Br0.15) | one-step | spin | trifluorotoluene | DMF+DMSO | 100 | 90 | glovebox | V931 | Li+TBP+FK209 | 16.3 |
| Mathies, F. et al., ACS Appl. Energy Mater. acsaem.8b00222 (2018). doi:10.1021/acsaem.8b00222 | 2018 | TiO2 | 0 | Cs0.1(FA0.83MA0.17)0.9Pb(Br0.17I0.83)3 | one-step | printed | no | DMF+DMSO | 100 | 60 | ambient | spiro-OMeTAD | Li+TBP | 15.3 |
| Ng, C. H. et al., Sci. Rep. 8, 2482 (2018) | 2018 | TiO2 | mTiO2 | CsPbBr3 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 3.1 |
| Ng, C. H. et al., Sci. Rep. 8, 2482 (2018) | 2018 | TiO2 | mTiO2 | CsPbBr2.9I0.1 | two-step | spin-dip | no | DMF | - | - | - | P3HT | no | 2.5 |
| Ng, C. H. et al., Sci. Rep. 8, 2482 (2018) | 2018 | TiO2 | mTiO2 | CsPbBr2.9I0.1 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 4 |
| Ng, C. H. et al., Sci. Rep. 8, 2482 (2018) | 2018 | TiO2 | mTiO2 | CsPbBr3 | two-step | spin-dip | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 3 |
| Nimens, W. J. et al., ACS Appl. Energy Mater. 1, acsaem.7b00147 (2018) | 2018 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | PTAA | Li+TBP | 13.5 |
| Nimens, W. J. et al., ACS Appl. Energy Mater. 1, acsaem.7b00147 (2018) | 2018 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | PTAA | Li+TBP | 6.3 |
| Nimens, W. J. et al., ACS Appl. Energy Mater. 1, acsaem.7b00147 (2018) | 2018 | 0 | mTiO2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | glovebox | PTAA | Li+TBP | 7.7 |
| Suk, K., Thin Solid Films (2018). doi:10.1016/j.tsf.2018.04.017 | 2018 | ZnO | 0 | FAPbI3-MAPbBr3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP+FK209 | 14.9 |
| Suk, K., Thin Solid Films (2018). doi:10.1016/j.tsf.2018.04.017 | 2018 | ZnO | 0 | FAPbI3-MAPbBr3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 10 | na | spiro-OMeTAD | Li+TBP+FK209 | 13.7 |
| Pelicano, C. M. and Yanagi, H., J. Energy Chem. 27, 455–462 (2018) | 2018 | ZnO | ZnO-nanorod | MAPbI3 | one-step | spin | toluene | DMF | 70 | 10 | glovebox | P3HT | no | 4.9 |
| Pelicano, C. M. and Yanagi, H., J. Energy Chem. 27, 455–462 (2018) | 2018 | ZnO | ZnO-nanorod | MAPbI3 | one-step | spin | toluene | DMF | 70 | 10 | glovebox | P3HT | no | 3.4 |
| Que, M. et al., J. Power Sources 383, 42–49 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 15 |
| Que, M. et al., J. Power Sources 383, 42–49 (2018) | 2018 | TiO2 | mTiO2-Au | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | na | spiro-OMeTAD | Li+TBP | 17.9 |
| Raminafshar, C. et al., Electrochim. Acta 276, 261–267 (2018) | 2018 | TiO2 | mZrO2 | (5-AVA) x (MA) 1-xPbI3 | one-step | drip | no | GBL | 50 | 60 | na | no | no | 10.7 |
| Shao, F. et al., Sci. Rep. 8, 7033 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | trifluorotoluene | DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 16.4 |
| Shao, F. et al., Sci. Rep. 8, 7033 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin 2-3 | trifluorotoluene | DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 8.3 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 17.5 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 14.8 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | FA0.85MA0.1Cs0.05PbI2.7Br0.3 | one-step | spin | diethyl ether | DMF+DMSO | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 18.6 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | FA0.85MA0.15PbI2.55Br0.45 | one-step | spin | diethyl ether | DMF+DMSO | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 17.8 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO+KI | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 17.2 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | FAPbI3 | one-step | spin | diethyl ether | DMF+DMSO+KI | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 10.7 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | FA0.85MA0.1Cs0.05PbI2.7Br0.3 | one-step | spin | diethyl ether | DMF+DMSO+KI | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 18.8 |
| Son, D.-Y. et al., J. Am. Chem. Soc. 140, jacs.7b10430 (2018) | 2018 | TiO2 | mTiO2 | FA0.85MA0.15PbI2.55Br0.45 | one-step | spin | diethyl ether | DMF+DMSO+KI | 145 | 40 | na | spiro-OMeTAD | Li+TBP | 17.9 |
| Sun, K. et al., ACS Appl. Energy Mater. acsaem.8b00160 (2018). doi:10.1021/acsaem.8b00160 | 2018 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 18.5 |
| Sun, K. et al., ACS Appl. Energy Mater. acsaem.8b00160 (2018). doi:10.1021/acsaem.8b00160 | 2018 | TiO2 | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | spiro-OMeTAD | Li+TBP | 14.3 |
| Wang, Q., J. Phys. Chem. C 122, 4822–4827 (2018) | 2018 | TiO2 | 0 | MAPbI2.85Br0.15 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 6.8 |
| Wang, Q., J. Phys. Chem. C 122, 4822–4827 (2018) | 2018 | TiO2 | mTiO2 | MAPbI2.85Br0.15 | one-step | spin | no | DMF | 100 | 10 | na | spiro-OMeTAD | Li+TBP | 6.5 |
| Wang, B. et al., Journal of Energy Chemistry 27, 736–741 (2017) | 2018 | TiO2 | mTiO2 | MAPbI3 | one-step | spin | ethylacetate | DMF+DMSO | 100 | 60 | na | spiro-OMeTAD | no | 16.6 |
| Xu, Z. et al., J. Mater. Chem. C 6, 4746–4752 (2018) | 2018 | TiO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | na | spiro-OMeTAD | Li+TBP | 13.4 |
| Xu, Z. et al., J. Mater. Chem. C 6, 4746–4752 (2018) | 2018 | TiO2-Ru | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | na | spiro-OMeTAD | Li+TBP | 15.7 |
| Ye, Q.-Q. et al., ACS Energy Lett. 3, 875–882 (2018) | 2018 | TiO2 | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | no | 16.3 |
| Ye, Q.-Q. et al., ACS Energy Lett. 3, 875–882 (2018) | 2018 | TiO2 | bis-PCBM-DMC | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | no | 20.1 |
| Ye, Q.-Q. et al., ACS Energy Lett. 3, 875–882 (2018) | 2018 | TiO2 | bis-PCBM | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | spiro-OMeTAD | no | 17.8 |
| Zhang, M. et al., Sol. RRL 2, 1700213 (2018) | 2018 | TiO2 | 0 | FAI, CsI, PbI2, MABr,PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP+FK209 | 19.1 |
| Zhang, M. et al., Sol. RRL 2, 1700213 (2018) | 2018 | TiO2 | 0 | FAI, CsI, PbI2, MABr,PbBr2 | one-step | spin 2-3 | methoxybenzene | DMF+DMSO | 100 | 15 | na | spiro-OMeTAD | Li+TBP+FK209 | 19.4 |
| Zhang, R. et al., Electrochim. Acta 265, 98–106 (2018) | 2018 | TiO2 | mTiO2-Li | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | spiro-OMeTAD | Li+TBP | 16.2 |
| Zhang, R. et al., Electrochim. Acta 265, 98–106 (2018) | 2018 | TiO2 | mTiO2-Li | CsI, FAI, PbI2, MABr, PbBr2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 18.2 |
| Zhao, X. et al., Nano Lett. 18, 2442–2449 (2018) | 2018 | SnO2-5% G | 0 | FA0.75MA0.15Cs0.1PbI2.65Br0.35 | one-step | spin | chlorobenzene | DMF+DMSO | 120 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 20.2 |
| Zhao, X. et al., Nano Lett. 18, 2442–2449 (2018) | 2018 | SnO2 | 0 | FA0.75MA0.15Cs0.1PbI2.65Br0.35 | one-step | spin | chlorobenzene | DMF+DMSO | 120 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 19 |
| Zhao, X. et al., Nano Lett. 18, 2442–2449 (2018) | 2018 | SnO2-5% NDI | 0 | FA0.75MA0.15Cs0.1PbI2.65Br0.35 | one-step | spin | chlorobenzene | DMF+DMSO | 120 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 18.8 |
| Zhao, X. et al., Nano Lett. 18, 2442–2449 (2018) | 2018 | SnO2 | 0 | FA0.83MA0.17PbI2.63Br0.37 | one-step | spin | chlorobenzene | DMF+DMSO | 120 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 15.2 |
| Zhao, X. et al., Nano Lett. 18, 2442–2449 (2018) | 2018 | NDI-graphene | 0 | FA0.83MA0.17PbI2.63Br0.37 | one-step | spin | chlorobenzene | DMF+DMSO | 120 | 30 | glovebox | spiro-OMeTAD | Li+TBP | 9.8 |
| Zhao, Y. et al., Nat. Commun. 9, 1607 (2018) | 2018 | TiO2-Cl | 0 | Cs10 (Cs0.1FA0.78MA0.12PbI2.55Br0.45) | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 21.7 |
| Ng, C. H. et al., Sci. Rep. 8, 2482 (2018) | 2018 | TiO2-Cl | 0 | PbI2/FAI/MABr/MACl | two-step | spin | no | DMF+DMSO | - | - | - | spiro-OMeTAD | Li+TBP | 19.4 |
| Zhu, W. et al., Dalt. Trans. 47, 6404–6411 (2018) | 2018 | Ti-Fe2O3 | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | glovebox | spiro-OMeTAD | Li+TBP+FK209 | 17.9 |

Table S10. Best efficiencies of entire inverted cells

| Article | Year | HTL | HTL-2 | Perovskite | Perovskite deposition procedure | Perovskite deposition method | Anti-solvent treatment | Precursor solution | Annealing temperature (°C) | Annealing time (minutes) | Annealing ambience | ETL | ETL interlayer | PCEbest (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Jeng, J. Y. et al., Adv. Mater. 25, 3727–3732 (2013) | 2013 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | C60 | BCP | 3 |
| Jeng, J. Y. et al., Adv. Mater. 25, 3727–3732 (2013) | 2013 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | ICBA | BCP | 3.4 |
| Jeng, J. Y. et al., Adv. Mater. 25, 3727–3732 (2013) | 2013 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | PCBM | BCP | 3.9 |
| Chiang, Y.-F. et al., Phys. Chem. Chem. Phys. 16, 6033–6040 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | C60 | BCP | 1.9 |
| Chiang, Y.-F. et al., Phys. Chem. Chem. Phys. 16, 6033–6040 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | glovebox | PCBM | BCP | 3.1 |
| Choi, H. et al., Nano Energy 7, 80–85 (2014) | 2014 | PEDOT:PSS | 0 | Cs0.1MA0.9PbI3 | one-step | spin | no | DMF+GBL | 110 | 10 | na | PCBM | no | 7.7 |
| Choi, H. et al., Nano Energy 7, 80–85 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+GBL | 110 | 10 | na | PCBM | no | 5.5 |
| Cui, J. et al., Interfaces 6, 22862–22870 (2014) | 2014 | no | no | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | PCBM | BCP | 0.1 |
| Cui, J. et al., Interfaces 6, 22862–22870 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | na | PCBM | BCP | 6.1 |
| Cui, J. et al., Interfaces 6, 22862–22870 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | na | PCBM | BCP | 4.9 |
| Cui, J. et al., Interfaces 6, 22862–22870 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin | toluene | DMF | na | na | glovebox | PCBM | BCP | 9.8 |
| Cui, J. et al., Interfaces 6, 22862–22870 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin | toluene | DMF | na | na | glovebox | PCBM | BCP | 7.4 |
| Hsu, H.-L. et al., Nanoscale 6, 10281 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 7.5 |
| Hsu, H.-L. et al., Nanoscale 6, 10281 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 5 | glovebox | PCBM | no | 6.8 |
| Hsu, H.-L. et al., Nanoscale 6, 10281 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 30 | glovebox | PCBM | no | 4.7 |
| Hsu, H.-L. et al., Nanoscale 6, 10281 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 60 | glovebox | PCBM | no | 4.5 |
| Hsu, H.-L. et al., Nanoscale 6, 10281 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 110 | 5 | glovebox | PCBM | no | 1.9 |
| Hsu, H.-L. et al., Nanoscale 6, 10281 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 120 | 5 | glovebox | PCBM | no | 0.3 |
| Hu, L. et al., ACS Photonics 1, 547–553 (2014) | 2014 | NiOx | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | no | 7.6 |
| Hu, L. et al., ACS Photonics 1, 547–553 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | no | 5.3 |
| Jeng, J. Y. et al., Adv. Mater. 26, 4107–4113 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | C60 | BCP | 5.7 |
| Jeng, J. Y. et al., Adv. Mater. 26, 4107–4113 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | PCBM | BCP | 7.8 |
| Jeng, J. Y. et al., Adv. Mater. 26, 4107–4113 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | glovebox | PCBM | BCP | 3.9 |
| Jung, J. W. et al., RSC Adv. 4, 62971–62977 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+GBL | 100 | 15 | glovebox | PCBM+C60 | no | 14.1 |
| Jung, J. W. et al., RSC Adv. 4, 62971–62977 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+GBL | 100 | 15 | glovebox | PCBM+C60 | no | 12 |
| Jung, J. W. et al., RSC Adv. 4, 62971–62977 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+GBL | 100 | 15 | glovebox | PCBM+C60 | no | 3.8 |
| Jung, J. W. et al., RSC Adv. 4, 62971–62977 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF+GBL | 100 | 15 | glovebox | PCBM+C60 | no | 11.4 |
| Kim, H.-B. et al., Nanoscale 6, 6679 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | na | PCBM | no | 5 |
| Kim, H.-B. et al., Nanoscale 6, 6679 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL+DMF | 100 | 15 | na | PCBM | no | 6.2 |
| Kim, H.-B. et al., Nanoscale 6, 6679 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 15 | na | PCBM | no | 4.1 |
| Liang, P. W. et al., Adv. Mater. 26, 3748–3754 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | PCBM+C60 | no | 9 |
| Liang, P. W. et al., Adv. Mater. 26, 3748–3754 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | PCBM+C60 | no | 7.9 |
| Liang, P. W. et al., Adv. Mater. 26, 3748–3754 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 11.8 |
| Liang, P. W. et al., Adv. Mater. 26, 3748–3754 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 10.3 |
| Lim, K.-G. et al., Adv. Mater. 26, 6461–6466 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 8.1 |
| Lim, K.-G. et al., Adv. Mater. 26, 6461–6466 (2014) | 2014 | PEDOT:PSS-PFI | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 11.7 |
| Malinkiewicz, O. et al., Adv. Energy Mater. 4, 1400345 (2014) | 2014 | PEDOT:PSS | poly TPD | MAPbI3 | two-step | CVD | no | na | - | - | - | 3TPYMB | no | 5.5 |
| Malinkiewicz, O. et al., Adv. Energy Mater. 4, 1400345 (2014) | 2014 | PEDOT:PSS | poly TPD | MAPbI3 | two-step | CVD | no | na | - | - | - | no | no | 4.6 |
| Malinkiewicz, O. et al., Adv. Energy Mater. 4, 1400345 (2014) | 2014 | PEDOT:PSS | poly TPD | MAPbI3 | two-step | CVD | no | na | - | - | - | PCBM | no | 14.8 |
| Malinkiewicz, O. et al., Nat. Photonics 8, 128–132 (2014) | 2014 | PEDOT:PSS | poly TPD | MAPbI3 | two-step | CVD | no | na | - | - | - | PCBM | no | 12 |
| Momblona, C. et al., APL Mater. 2, 081504 (2014) | 2014 | PEDOT:PSS | poly TPD | MAPbI3 | one-step | CVD | no | na | na | na | na | PCBM | no | 12.7 |
| Seo, J. et al., Energy Environ. Sci. 7, 2642–2646 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | na | na | PCBM | no | 14.1 |
| Seo, J. et al., Energy Environ. Sci. 7, 2642–2646 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | na | na | PCBM | no | 11.5 |
| Subbiah, A. S. et al., J. Phys. Chem. Lett. 5, 1748–1753 (2014) | 2014 | NiOx | 0 | MAPbI3-xClx | two-step | CVD | no | na | - | - | - | PCBM | no | 7.3 |
| Sun, S. et al., Energy Environ. Sci. 7, 399–407 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 0.5 | glovebox | PCBM | no | 7.4 |
| Tian, H. et al., ChemSusChem 7, 2150–2153 (2014) | 2014 | NiOx | mNiOx | MAPbI3 | one-step | spin 2-3 | no | GBL | na | na | na | PCBM | no | 1.5 |
| Tian, H. et al., ChemSusChem 7, 2150–2153 (2014) | 2014 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | no | GBL | na | na | na | PCBM | no | 0.1 |
| Wang, Q. et al., Energy Environ. Sci. 7, 2359–2365 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 60 | na | ICBA+C60 | BCP | 12.2 |
| Wang, Q. et al., Energy Environ. Sci. 7, 2359–2365 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 60 | na | PCBM+C60 | BCP | 10.1 |
| Wang, Q. et al., Energy Environ. Sci. 7, 2359–2365 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 60 | na | C60 | BCP | 2.1 |
| Wang, K.-C. et al., ACS Appl. Mater. Interfaces 6, 11851–11858 (2014) | 2014 | NiOx | mNiOx | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | BCP | 11.6 |
| Wu, Z. et al., Nanoscale 6, 10505–10510 (2014) | 2014 | no | no | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 20 | glovebox | PCBM | ZnO | 2.6 |
| Wu, Z. et al., Nanoscale 6, 10505–10510 (2014) | 2014 | GO | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 20 | glovebox | PCBM | ZnO | 12.4 |
| Wu, Z. et al., Nanoscale 6, 10505–10510 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 20 | glovebox | PCBM | ZnO | 9.3 |
| Xiao, Z. et al., Energy Environ. Sci. 7, 2619–2623 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | BCP | 15.4 |
| Yan, W. et al., RSC Adv. 4, 33039 (2014) | 2014 | polythiophene | 0 | MAPbI3 | one-step | spin | no | DMF | na | na | na | C60 | BCP | 11.8 |
| Yang, Y. et al., ACS Nano 8, 1674–1680 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | na | 90 | 120 | na | PCBM | no | 11.5 |
| Yang, Y. et al., ACS Nano 8, 1674–1680 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | na | 90 | 120 | na | ZnO | no | 10.5 |
| You, J. et al., Appl. Phys. Lett. 105, 183902 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | ambient | PCBM | no | 17.1 |
| You, J. et al., Appl. Phys. Lett. 105, 183902 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | glovebox | PCBM | no | 12.3 |
| Zhang, H. et al., Chem. Mater. 26, 5190–5193 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | na | 110 | 40 | na | PCBM | no | 12.4 |
| Zhang, H. et al., Chem. Mater. 26, 5190–5193 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | na | 110 | 40 | na | PCBM | no | 11.9 |
| Zhang, H. et al., Chem. Mater. 26, 5190–5193 (2014) | 2014 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | na | 110 | 40 | na | PCBM | no | 8.8 |
| Bao, X. et al., J. Power Sources 297, 53–58 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 90 | 20 | glovebox | PCBM | Ca | 2.6 |
| Bao, X. et al., J. Power Sources 297, 53–58 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 90 | 20 | glovebox | PCBM | Ca | 9.9 |
| Bao, X. et al., J. Power Sources 297, 53–58 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL+NMP | 90 | 20 | glovebox | PCBM | Ca | 11.8 |
| Chang, C. Y. et al., Chem. Mater. 27, 7119–7127 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 16.5 |
| Chang, C. Y. et al., Chem. Mater. 27, 7119–7127 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 11 |
| Chang, C. Y. et al., Chem. Mater. 27, 7119–7127 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 8 |
| Chang, C. Y. et al., Chem. Mater. 27, 7119–7127 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 3.7 |
| Chang, C. Y. et al., Chem. Mater. 27, 5122–5130 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | ZnO | 16.5 |
| Chang, C. Y. et al., Chem. Mater. 27, 5122–5130 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | ZnO | 11 |
| Chang, C. Y. et al., Chem. Mater. 27, 5122–5130 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | ZnO | 10.8 |
| Chang, C. Y. et al., Chem. Mater. 27, 5122–5130 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | ZnO | 10.8 |
| Chang, C. Y. et al., Chem. Mater. 27, 5122–5130 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | ZnO | 2.8 |
| Chang, C. Y. et al., Chem. Mater. 27, 5122–5130 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 3.4 |
| Chen, Y. et al., ACS Appl. Mater. Interfaces 7, 4471–4475 (2015) | 2015 | PEDOT:PSS | mTiO2 | MAPbI3 | one-step | spin | no | DMF | 100 | 30 | glovebox | PCBM | no | 9.2 |
| Chen, W. et al., Energy Environ. Sci. 8, 629–640 (2015) | 2015 | NiOx | mAl2O3 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | glovebox | PCBM | BCP | 13.5 |
| Chen, W. et al., Energy Environ. Sci. 8, 629–640 (2015) | 2015 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | glovebox | PCBM | BCP | 11.2 |
| Chen, W. et al., Energy Environ. Sci. 8, 629–640 (2015) | 2015 | NiOx | mAl2O3 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | BCP | 12.7 |
| Chen, W. et al., Energy Environ. Sci. 8, 629–640 (2015) | 2015 | NiOx | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | BCP | 10.4 |
| Chen, Y. et al., Adv. Mater. 27, 1053–1059 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | two-step | evap-dip | no | na | - | - | - | PCBM | no | 15.1 |
| Chen, W.-Y. et al., J. Mater. Chem. A 3, 19353–19359 (2015) | 2015 | no | no | MAPbI3 | two-step | vasp | no | DMF | - | - | - | PCBM | no | 5.6 |
| Chen, W.-Y. et al., J. Mater. Chem. A 3, 19353–19359 (2015) | 2015 | CuI | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | PCBM | no | 13.6 |
| Chen, W.-Y. et al., J. Mater. Chem. A 3, 19353–19359 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | PCBM | no | 13.3 |
| Chen, Y. et al., Chem. Mater. 27, 1448–1451 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+NH4Cl | na | na | glovebox | PCBM | no | 9.3 |
| Chen, Y. et al., Chem. Mater. 27, 1448–1451 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 95 | 10 | glovebox | PCBM | no | 6.3 |
| Dianetti, M. et al., Sol. Energy Mater. Sol. Cells 140, 150–157 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | glovebox | PCBM | TiOx | 9 |
| Gil-Escrig, L. et al., J. Phys. Chem. Lett. 6, 3743–3748 (2015) | 2015 | PEDOT:PSS | polyTPD | MAPbI3 | two-step | CVD | no | na | - | - | - | PCBM | Ba | 12.9 |
| Gil-Escrig, L. et al., J. Phys. Chem. Lett. 6, 3743–3748 (2015) | 2015 | PEDOT:PSS | polyTPD | MAPb(I0.9Br0.1)3 | two-step | CVD | no | na | - | - | - | PCBM | Ba | 10.8 |
| Gil-Escrig, L. et al., J. Phys. Chem. Lett. 6, 3743–3748 (2015) | 2015 | PEDOT:PSS | polyTPD | MAPb(I0.97Br0.03)3 | two-step | CVD | no | na | - | - | - | PCBM | Ba | 10.2 |
| Gil-Escrig, L. et al., J. Phys. Chem. Lett. 6, 3743–3748 (2015) | 2015 | PEDOT:PSS | polyTPD | MAPb(I0.8Br0.2)3 | two-step | CVD | no | na | - | - | - | PCBM | Ba | 9.3 |
| Gil-Escrig, L. et al., J. Phys. Chem. Lett. 6, 3743–3748 (2015) | 2015 | PEDOT:PSS | polyTPD | MAPb(I0.6Br0.4)3 | two-step | CVD | no | na | - | - | - | PCBM | Ba | 2.5 |
| Gil-Escrig, L. et al., J. Phys. Chem. Lett. 6, 3743–3748 (2015) | 2015 | PEDOT:PSS | polyTPD | MAPb(I0.4Br0.6)3 | two-step | CVD | no | na | - | - | - | PCBM | Ba | 1.2 |
| Gong, X. et al., Adv. Funct. Mater. 25, 6671–6678 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | na | PCBM | Bphen | 12.1 |
| Gong, X. et al., Adv. Funct. Mater. 25, 6671–6678 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+H2O | na | na | na | PCBM | Bphen | 16.1 |
| Hsu, H.-L. et al., Sol. Energy Mater. Sol. Cells 140, 224–231 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | glovebox | PCBM | no | 8.5 |
| Hsu, H.-L. et al., Sol. Energy Mater. Sol. Cells 140, 224–231 (2015) | 2015 | PEDOT:PSS-AgNLP | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | glovebox | PCBM | no | 9.6 |
| Hu, Z. et al., Org. Electron. 27, 46–52 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | glovebox | PCBM | no | 13.7 |
| Hu, Z. et al., Org. Electron. 27, 46–52 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 15 | glovebox | PCBM | no | 12.6 |
| Kaltenbrunner, M. et al. , Nat. Mater. 14, 1032–1039 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 110 | 20 | ambient | PTCDI | no | 12.6 |
| Khatiwada, D. et al., J. Phys. Chem. C 119, 25747–25753 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | na | 20 | glovebox | PCBM | rhodamine | 13.2 |
| Khatiwada, D. et al., J. Phys. Chem. C 119, 25747–25753 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | na | 20 | glovebox | PCBM | rhodamine | 10.6 |
| Kim, B. S. et al., Org. Electron. physics, Mater. Appl. 17, 102–106 (2015) | 2015 | MoO3 | NPB | MAPbI3 | one-step | CVD | no | na | na | na | na | C60 | BCP | 13.7 |
| Kim, J. H. et al., Adv. Mater. 27, 695–701 (2015) | 2015 | NiOx | 0 | MAPbI3 | one-step | spin | no | na | na | na | na | PCBM+C60 | no | 8.9 |
| Kim, J. H. et al., Adv. Mater. 27, 695–701 (2015) | 2015 | NiOx-Cu | 0 | MAPbI3 | one-step | spin | no | na | na | na | na | PCBM+C60 | no | 15.4 |
| Kim, J. H. et al., Adv. Mater. 27, 695–701 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | na | na | na | na | PCBM+C60 | no | 11.2 |
| Kuang, C. et al., Nano Lett. 15, 2756–2762 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM-GD-C60 | no | 14.8 |
| Kuang, C. et al., Nano Lett. 15, 2756–2762 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM+C60 | no | 13.6 |
| Li, X. et al., Org. Electron. 18, 107–112 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | glovebox | C60 | no | 8.6 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 3.4 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPb(I0.6Br0.4)3 | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 3.7 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPb(I0.8Br0.2)3 | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 3.6 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 10.5 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPb(I0.8Br0.2)xCl3-x | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 10 |
| Liang, P. W. et al., Adv. Energy Mater. 5, 1400960 (2015) | 2015 | PEDOT:PSS | 0 | MAPb(I0.6Br0.4)xCl3-x | one-step | spin 2-3 | no | DMF+DIO | 90 | 120-180 | glovebox | PCBM+C60 | no | 7.6 |
| Liu, T. et al., Nanoscale 7, 10708–10718 (2015) | 2015 | no | no | MAPbI3-xClx | one-step | spin | no | na | 95 | 15 | na | PCBM | no | 4.4 |
| Liu, T. et al., Nanoscale 7, 10708–10718 (2015) | 2015 | GO | 0 | MAPbI3-xClx | one-step | spin | no | na | 95 | 15 | na | PCBM | no | 5.1 |
| Liu, T. et al., Nanoscale 7, 10708–10718 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | na | 95 | 15 | na | PCBM | no | 10.7 |
| Liu, T. et al., Nanoscale 7, 10708–10718 (2015) | 2015 | PEDOT:PSS-GO-AgOTf | 0 | MAPbI3-xClx | one-step | spin | no | na | 95 | 15 | na | PCBM | no | 11.9 |
| Liu, Z. and Lee, E.-C., Org. Electron. 24, 101–105 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM | no | 13 |
| Liu, Z. and Lee, E.-C., Org. Electron. 24, 101–105 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM | no | 11.3 |
| Liu, X. et al., ACS Appl. Mater. Interfaces 7, 6230–6237 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 105 | 38 | glovebox | PCBM+C60 | LiF | 14.2 |
| Liu, X. et al., ACS Appl. Mater. Interfaces 7, 6230–6237 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 105 | 38 | glovebox | PCBM+C60 | no | 14.7 |
| Liu, X. et al., ACS Appl. Mater. Interfaces 7, 6230–6237 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 105 | 38 | glovebox | PCBM | no | 12.3 |
| Liu, X. et al., ACS Appl. Mater. Interfaces 7, 6230–6237 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 105 | 38 | glovebox | PCBM | no | 11.5 |
| Min, J. et al., Chem. Mater. 27, 227–234 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | ZnO | 11.3 |
| Min, J. et al., Chem. Mater. 27, 227–234 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | PDINO | 14 |
| Min, J. et al., Chem. Mater. 27, 227–234 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 10 |
| Park, M. et al., Adv. Energy Mater. 5, 1501406 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | two-step | spin | no | DMF | - | - | - | no | no | 13.9 |
| Park, I. J. et al, J. Phys. Chem. C 119, 27285–27290 (2015) | 2015 | NiOx | PEDOT:PSS | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | no | 15.1 |
| Park, I. J. et al, J. Phys. Chem. C 119, 27285–27290 (2015) | 2015 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | no | 12.7 |
| Park, I. J. et al, J. Phys. Chem. C 119, 27285–27290 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | no | 11.8 |
| Qing, J. et al., ACS Appl. Mater. Interfaces 7, 23110–23116 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 5 | glovebox | BCP | no | 12.7 |
| Qing, J. et al., ACS Appl. Mater. Interfaces 7, 23110–23116 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 5 | glovebox | BCP | no | 15 |
| Qiu, W. et al., Org. Electron. 26, 30–35 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | PCBM | ZnO | 14.2 |
| Qiu, W. et al., Org. Electron. 26, 30–35 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | no | no | 0.1 |
| Qiu, W. et al., Org. Electron. 26, 30–35 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | PCBM | no | 2.7 |
| Qiu, W. et al., Org. Electron. 26, 30–35 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120-180 | glovebox | ZnO | no | 2.4 |
| Ramesh, M. et al., ACS Appl. Mater. Interfaces 7, 2359–2366 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spray | no | DMF | 100 | 60 | glovebox | PCBM+C60 | BCP | 10.2 |
| Shao, Y. et al., Nano Energy 16, 47–53 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 12.7 |
| Su, Z. et al., Org. Electron. 26, 104–108 (2015) | 2015 | no | no | MAPbI3-xClx | two-step | CVD | no | na | - | - | - | C60 | no | 8.4 |
| Sun, C. et al., Small 11, 3344–3350 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM | TPPI | 11.1 |
| Sun, C. et al., Small 11, 3344–3350 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+TPPI | 100 | 120 | na | PCBM | TPPI | 13 |
| Sun, C. et al., Small 11, 3344–3350 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM | no | 9.6 |
| Sun, C. et al., Small 11, 3344–3350 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+TPPI | 100 | 120 | na | PCBM | no | 11.7 |
| Sun, K. et al., ACS Appl. Mater. Interfaces 7, 15314–15320 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | rhodamine/C60/BCP/rhodamine/LiF | 15.6 |
| Sun, K. et al., ACS Appl. Mater. Interfaces 7, 15314–15320 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | rhodamine/C60/BCP/rhodamine/LiF | 11 |
| Wang, Q. et al., Nano Energy 15, 275–280 (2015) | 2015 | PTAA-1wtF4-TCNQ | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | BCP | 17.5 |
| Wang, Q. et al., Nano Energy 15, 275–280 (2015) | 2015 | PTAA-1wtF4-TCNQ | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | BCP | 14.8 |
| Wang, K. et al., Org. Electron. physics, Mater. Appl. 21, 19–26 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | na | PCBM | no | 12.3 |
| Wang, Z.-K. et al., ACS Appl. Mater. Interfaces 7, 9645–9651 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 11 |
| Wang, Z.-K. et al., ACS Appl. Mater. Interfaces 7, 9645–9651 (2015) | 2015 | PEDOT:PSS-GeO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 15.2 |
| Wang, X. et al., Org. Electron. physics, Mater. Appl. 24, 205–211 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | IPA | DMF | 80 | 120 | glovebox | PCBM+C60 | no | 13.1 |
| Wang, X. et al., Org. Electron. physics, Mater. Appl. 24, 205–211 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM+C60 | no | 12.1 |
| Wang, W. et al., ACS Appl. Mater. Interfaces 7, 3994–3999 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 30 | glovebox | N2200 | ZnO | 8.8 |
| Wang, W. et al., ACS Appl. Mater. Interfaces 7, 3994–3999 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 30 | glovebox | PCBM | ZnO | 9.5 |
| Wang, W. et al., ACS Appl. Mater. Interfaces 7, 3994–3999 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 30 | glovebox | PNDI2OD+TT | ZnO | 6.5 |
| Wang, W. et al., ACS Appl. Mater. Interfaces 7, 3994–3999 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 30 | glovebox | PNVT+8 | ZnO | 7.7 |
| Wu, R. et al., Org. Electron. 26, 265–272 (2015) | 2015 | no | no | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM | no | 11.3 |
| Wu, R. et al., Org. Electron. 26, 265–272 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM | no | 12.9 |
| Wu, C.-G. et al., Energy Environ. Sci. 8, 2725–2733 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 0 |
| Wu, C.-G. et al., Energy Environ. Sci. 8, 2725–2733 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF+H2O | - | - | - | PCBM | no | 18 |
| Xia, F. et al., ACS Appl. Mater. Interfaces 7, 13659–13665 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMSO+GBL | MS | na | glovebox | PCBM | no | 10.1 |
| Xia, F. et al., ACS Appl. Mater. Interfaces 7, 13659–13665 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMSO+GBL | MS | na | glovebox | PCBM-oleamide | no | 12.7 |
| Xiong, J. et al., Org. Electron. 24, 106–112 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM | no | 13.5 |
| Yang, Z. et al., Adv. Energy Mater. 5, 1500328 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | blade coat | no | DMF+DIO | 100 | 60 | ambient | PCBM+C60 | no | 11.3 |
| Yang, Z. et al., Adv. Energy Mater. 5, 1500328 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | 100 | 60 | glovebox | PCBM+C60 | no | 10.7 |
| Ye, S. et al., Nano Lett. 15, 3723–3728 (2015) | 2015 | CuSCN | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | C60 | BCP | 16.6 |
| Ye, S. et al., Nano Lett. 15, 3723–3728 (2015) | 2015 | CuSCN | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | C60 | BCP | 13.4 |
| Yeo, J.-S. et al., Nano Energy 12, 96–104 (2015) | 2015 | RGO | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 2 | glovebox | PCBM | BCP | 10.8 |
| Yeo, J.-S. et al., Nano Energy 12, 96–104 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 2 | glovebox | PCBM | BCP | 9.1 |
| Yeo, J.-S. et al., Nano Energy 12, 96–104 (2015) | 2015 | GO | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 2 | glovebox | PCBM | BCP | 4 |
| Yin, X. et al., J. Mater. Chem. A 3, 24495–24503 (2015) | 2015 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 14.4 |
| Yin, X. et al., J. Mater. Chem. A 3, 24495–24503 (2015) | 2015 | no | no | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 1.2 |
| Yin, X. et al., J. Mater. Chem. A 3, 24495–24503 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 11.7 |
| Yuan, D.-X. et al., Phys. Chem. Chem. Phys. 17, 26653–26658 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI2.4Br0.6 | one-step | spin | no | na | 100 | 15 | glovebox | PCBM | BCP | 13.1 |
| Yuan, D.-X. et al., Phys. Chem. Chem. Phys. 17, 26653–26658 (2015) | 2015 | PEDOT:PSS | 0 | MAPbI2.4Br0.6 | one-step | spin | no | na | 100 | 15 | glovebox | PCBM | no | 11 |
| Adam, G. et al., Sol. Energy Mater. Sol. Cells 157, 318–325 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | 110 | 45 | ambient | PCBM | no | 13 |
| Bag, S. and Durstock, M. F., Nano Energy 30, 542–548 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | no | 13.3 |
| Bag, M. et al., Mater. Lett. 164, 472–475 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-print | no | DMF | - | - | - | PCBM | no | 9.1 |
| Bag, M. et al., Mater. Lett. 164, 472–475 (2016) | 2016 | PEDOT:PSS | 0 | FAPbI3 | two-step | spin-print | no | DMF | - | - | - | PCBM | no | 1.4 |
| Bag, M. et al., Mater. Lett. 164, 472–475 (2016) | 2016 | PEDOT:PSS | 0 | MAFAPbI3 | two-step | spin-print | no | DMF | - | - | - | PCBM | no | 11.1 |
| Bai, Y. et al., Adv. Funct. Mater. 26, 2950–2958 (2016) | 2016 | NiOx | DEA | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | PCBM | no | 15.9 |
| Bai, Y. et al., Adv. Funct. Mater. 26, 2950–2958 (2016) | 2016 | NiOx | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 60 | glovebox | PCBM | no | 11.5 |
| Dai, S.-M. et al., J. Mater. Chem. A 4, 18776–18782 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | PCBM | no | 17.6 |
| Dong, S. et al., RSC Adv. 6, 57793–57798 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 6.1 |
| Dong, S. et al., RSC Adv. 6, 57793–57798 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM-PEI | no | 10.7 |
| Erten-Ela, S. et al., New J. Chem. 40, 2829–2834 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | BAFB | ZnO | 9.6 |
| Erten-Ela, S. et al., New J. Chem. 40, 2829–2834 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | 100 | 10 | na | PCBM | ZnO | 10.3 |
| Fu, W. et al., Sol. Energy Mater. Sol. Cells 155, 331–340 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | ZnO | 12 |
| Fu, W. et al., Sol. Energy Mater. Sol. Cells 155, 331–340 (2016) | 2016 | PTAA | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | ZnO | 17 |
| Fu, W. et al., Sol. Energy Mater. Sol. Cells 155, 331–340 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | ZnO | 13.6 |
| Fu, F. et al., Nat. Energy, 2, 16190 (2016) | 2016 | PTAA | 0 | MAPbI3 | two-step | spin | chlorobenzene | na | - | - | - | PCBM | ZnO | 8.8 |
| Gil-Escrig, L. et al., Org. Electron. 37, 396–401 (2016) | 2016 | PEDOT:PSS | polyTPD | MAPbI3 | one-step | CVD | no | na | na | na | glovebox | IPH (fullerene) | no | 15.2 |
| Gil-Escrig, L. et al., Org. Electron. 37, 396–401 (2016) | 2016 | PEDOT:PSS | polyTPD | MAPbI3 | one-step | CVD | no | na | na | na | glovebox | IPH (fullerene) | no | 13.9 |
| Gil-Escrig, L. et al., Org. Electron. 37, 396–401 (2016) | 2016 | PEDOT:PSS | polyTPD | MAPbI3 | one-step | CVD | no | na | na | na | glovebox | IPH (fullerene) | no | 13.7 |
| Guerrero, A. et al., ACS Nano 10, 218–224 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | ambient | PCBM | no | 12.1 |
| Guerrero, A. et al., ACS Nano 10, 218–224 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | ambient | PCBM | no | 12.1 |
| Guerrero, A. et al., ACS Nano 10, 218–224 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | ambient | PCBM | no | 8.8 |
| Guerrero, A. et al., ACS Nano 10, 218–224 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | ambient | PCBM | no | 7.3 |
| Guerrero, A. et al., ACS Nano 10, 218–224 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 90 | 120 | ambient | PCBM | no | 7 |
| Huang, Z. et al., Sol. Energy Mater. Sol. Cells 155, 166–175 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene+IPA | DMF | na | na | na | PCBM | no | 8.1 |
| Huang, Z. et al., Sol. Energy Mater. Sol. Cells 155, 166–175 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin |  | DMF | na | na | na | PCBM | no | 1.9 |
| Huang, Z. et al., Sol. Energy Mater. Sol. Cells 155, 166–175 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene+IPA | DMF | na | na | na | PCBM | no | 9.2 |
| Huang, Z. et al., Sol. Energy Mater. Sol. Cells 155, 166–175 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin |  | DMF | na | na | na | PCBM | no | 7.2 |
| Igbari, F. et al., J. Mater. Chem. A 4, 1326–1335 (2016) | 2016 | CuAlO2 | PEDOT:PSS | MAPbI3-xClx | one-step | spin | no | DMF | MS | 40 | glovebox | PCBM | no | 12.5 |
| Igbari, F. et al., J. Mater. Chem. A 4, 1326–1335 (2016) | 2016 | CuAlO2 | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | 40 | glovebox | PCBM | no | 10.1 |
| Igbari, F. et al., J. Mater. Chem. A 4, 1326–1335 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | 40 | glovebox | PCBM | no | 10.1 |
| Jeon, T. et al., ACS Nano, 10, 7907–7914 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | na | na | glovebox | PCBM | no | 12.6 |
| Jiang, Z. et al., Sol. Energy Mater. Sol. Cells 146, 35–43 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | na | PCBM | no | 11.8 |
| Jiang, Z. et al., Sol. Energy Mater. Sol. Cells 146, 35–43 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | na | PCBM | no | 11.5 |
| Jiang, Z. et al., Sol. Energy Mater. Sol. Cells 146, 35–43 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | na | PCBM | no | 8 |
| Kang, R. et al., Nano Energy 27, 175–184 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM | BCP | 7.5 |
| Kang, R. et al., Nano Energy 27, 175–184 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+CHP | 100 | 10 | glovebox | PCBM | BCP | 10.8 |
| Kang, R. et al., Nano Energy 27, 175–184 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF+CHP | - | - | - | PCBM | BCP | 8.9 |
| Kang, R. et al., Nano Energy 27, 175–184 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF+CHP | - | - | - | PCBM | BCP | 4.2 |
| Kim, J. et al., Sci. Rep. 6, 27773 (2016) | 2016 | NGO-NR | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | ZnO | no | 13 |
| Kim, J. et al., Sci. Rep. 6, 27773 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | ZnO | no | 10.9 |
| Lee, D.-Y. et al., Nanoscale 8, 1513–1522 (2016) | 2016 | GO | PEDOT:PSS | MAPbI3 | one-step | spin | no | 2 methoxy ethanol+CHP | 140 | 0.5 | glovebox | PCBM | LiF | 9.8 |
| Lee, D.-Y. et al., Nanoscale 8, 1513–1522 (2016) | 2016 | GO | 0 | MAPbI3 | one-step | spin | no | 2 methoxy ethanol+CHP | 140 | 0.5 | glovebox | PCBM | LiF | 6.8 |
| Lee, D.-Y. et al., Nanoscale 8, 1513–1522 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | 2 methoxy ethanol+CHP | 140 | 0.5 | glovebox | PCBM | LiF | 8.3 |
| Li, B. et al., Org. Electron. 34, 97–103 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM+C60 | no | 14.8 |
| Li, B. et al., Org. Electron. 34, 97–103 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 120 | na | PCBM+C60 | no | 13.8 |
| Li, C. et al., Org. Electron. physics, Mater. Appl. 33, 194–200 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 120 | glovebox | PCBM | no | 8.3 |
| Li, C. et al., Org. Electron. physics, Mater. Appl. 33, 194–200 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | glovebox | PCBM | no | 14.9 |
| Li, C. et al., Org. Electron. physics, Mater. Appl. 33, 194–200 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 10.8 |
| Li, D. et al., Sol. Energy 131, 176–182 (2016) | 2016 | PEDOT:PSS | GO | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | glovebox | PCBM | no | 13.1 |
| Li, D. et al., Sol. Energy 131, 176–182 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 15 | glovebox | PCBM | no | 10 |
| Li, S. et al., Org. Electron. 39, 304–310 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 14.3 |
| Li, S. et al., Org. Electron. 39, 304–310 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 8.4 |
| Lin, Q. et al., Adv. Opt. Mater., 5, 1600819 (2017) | 2016 | PCDTBT | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 110 | 40 | glovebox | PCBM | no | 14.8 |
| Lin, Z. et al., Sol. Energy Mater. Sol. Cells 157, 783–790 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 13.2 |
| Lin, Z. et al., Sol. Energy Mater. Sol. Cells 157, 783–790 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 8.5 |
| Lin, Z. et al., Sol. Energy Mater. Sol. Cells 157, 783–790 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 12 |
| Lin, Z. et al., Sol. Energy Mater. Sol. Cells 157, 783–790 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 14.8 |
| Ling, L. et al., Adv. Funct. Mater. 26, 5028–5034 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 5 | glovebox | PCBM+C60 | BCP | 10 |
| Ling, L. et al., Adv. Funct. Mater. 26, 5028–5034 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+H2O | 100 | 5 | glovebox | PCBM+C60 | BCP | 16 |
| Liu, X. et al., Nano Energy 30, 417–425 (2016) | 2016 | NiOx-Cu | 0 | MAPbI3 | one-step | spin 2-3 | no | DMSO+GBL+DFC60 | 100 | 10 | na | PCBM+C60 | no | 18.5 |
| Liu, X. et al., Nano Energy 30, 417–425 (2016) | 2016 | NiOx-Cu | 0 | MAPbI3 | one-step | spin 2-3 | no | DMSO+GBL | 100 | 10 | na | PCBM+C60 | no | 16.3 |
| Liu, J. et al, J. Power Sources 301, 242–250 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | PCBM | no | 12.3 |
| Liu, Z. et al, Nano Energy, 28, 151–157 (2016) | 2016 | P3HT | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | na | PCBM | no | 16.2 |
| Liu, Z. et al, Nano Energy, 28, 151–157 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | na | PCBM | no | 14 |
| Liu, Z. et al, Nano Energy, 28, 151–157 (2016) | 2016 | P3HT | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | MS | na | na | PCBM | no | 14.6 |
| McLeod, J. A. et al., Nanoscale 8, 6361–6368 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 20 | glovebox | PCBM | ZnO | 10.8 |
| Park, S. M. et al., Sol. Energy Mater. Sol. Cells 155, 14–19 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | roll | no | DMF | - | - | - | PCBM | BCP | 6.4 |
| Park, S. M. et al., Sol. Energy Mater. Sol. Cells 155, 14–19 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | roll-spin | no | DMF | - | - | - | PCBM | BCP | 9.5 |
| Park, S. M. et al., Sol. Energy Mater. Sol. Cells 155, 14–19 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | roll | no | DMF+CHP | - | - | - | PCBM | BCP | 7.4 |
| Perumallapelli, G. R. et al., Org. Electron. physics, Mater. Appl. 31, 142–148 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | diethyl ether | DMSO+GBL | 100 | 60 | glovebox | PCBM | no | 9.2 |
| Perumallapelli, G. R. et al., Org. Electron. physics, Mater. Appl. 31, 142–148 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMSO+GBL | 100 | 60 | glovebox | PCBM | no | 8 |
| Qing, J. et al., Org. Electron. physics, Mater. Appl. 38, 144–149 (2016) | 2016 | PEDOT:PSS | 0 | Cs0.15FA0.85PbI3 | one-step | spin | toluene | DMF+DMSO+MACl | 120 | 10 | glovebox | C60 | BCP | 14.5 |
| Qing, J. et al., Org. Electron. physics, Mater. Appl. 38, 144–149 (2016) | 2016 | PEDOT:PSS | 0 | Cs0.15FA0.85PbI3 | one-step | spin | toluene | DMF+DMSO | 120 | 10 | glovebox | C60 | BCP | 12.1 |
| Ran, C. et al., J. Mater. Chem. A, 4, 8566–8572 (2016). | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF | 110 | 15 | glovebox | no | no | 9.8 |
| Ran, C. et al., J. Mater. Chem. A, 4, 8566–8572 (2016). | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+PCBM | 110 | 15 | glovebox | PCBM | no | 15.3 |
| Rao, H. et al., Nano Energy 27, 51–57 (2016) | 2016 | CuOx | 0 | MAPbI3 | one-step | spin | no | DMF | 80 | 10 | glovebox | PCBM+C60 | BCP | 14.4 |
| Rao, H. et al., Nano Energy 27, 51–57 (2016) | 2016 | CuOx | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 10 | glovebox | PCBM+C60 | BCP | 19 |
| Savva, A. et al., Adv. Energy Mater. 6, 1600285 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM | AZO | 13.3 |
| Savva, A. et al., Adv. Energy Mater. 6, 1600285 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 120 | glovebox | PCBM | no | 8.1 |
| Sun, W. et al., Nanoscale 8, 10806–10813 (2016) | 2016 | CuOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | C60 | BCP | 17.1 |
| Sun, W. et al., Nanoscale 8, 10806–10813 (2016) | 2016 | no | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | C60 | BCP | 12.1 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 15.1 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 14.7 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 13.1 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 12.2 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | BCP | 16.3 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | BCP | 14.3 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 18.9 |
| Sun, X. et al., Nano Energy 28, 417–425 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 18.1 |
| Sun, W. et al., Nanoscale 8, 15954–15960 (2016) | 2016 | CuI | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | C60 | BCP | 16.8 |
| Sun, W. et al., Nanoscale 8, 15954–15960 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | C60 | BCP | 13.3 |
| Tseng, Z.-L. et al., Sol. Energy 139, 484–488 (2016) | 2016 | Mox | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 13.1 |
| Tseng, Z.-L. et al., Sol. Energy 139, 484–488 (2016) | 2016 | Wox | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 9.8 |
| Wang, J. et al., Org. Electron. , 39, 1–9 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 20 | glovebox | PCBM | no | 12.6 |
| Wang, J. et al., Org. Electron. , 39, 1–9 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 20 | glovebox | PCBM | no | 10.5 |
| Wang, B. et al.,Electrochim. Acta 218, 263–270 (2016) | 2016 | CuSCN | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | PCBM | no | 16.4 |
| Wang, B. et al.,Electrochim. Acta 218, 263–270 (2016) | 2016 | CuSCN | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | PCBM | no | 12.5 |
| Wang, B. et al.,Electrochim. Acta 218, 263–270 (2016) | 2016 | CuSCN | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | na | PCBM | no | 12.4 |
| Xie, J. et al., Nano Energy 28, 330–337 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | ambient | PCBM | PCBDAN | 17.2 |
| Xie, J. et al., Nano Energy 28, 330–337 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | ambient | PCBM | no | 13.8 |
| Xiong, J. et al., Org. Electron. physics, Mater. Appl. 30, 30–35 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM | no | 12.7 |
| Xiong, J. et al., Org. Electron. physics, Mater. Appl. 30, 30–35 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM | no | 11.4 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | HSL2 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 16.6 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | HSL1 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 15.4 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 14.2 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | HSL2 | MAPb(I0.3Br0.7)xCl3-x | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 10.3 |
| Xue, Q. et al., Adv. Energy Mater. 6, 1502021 (2016) | 2016 | PEDOT:PSS | 0 | MAPb(I0.3Br0.7)xCl3-x | one-step | spin | no | DMF | 100 | 60 | na | PCBM | no | 8.5 |
| Yao, K. et al., Chem. Mater. 28, 3131–3138 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 100 | 10 | na | PCBM | LiF | 15.4 |
| Yao, K. et al., Chem. Mater. 28, 3131–3138 (2016) | 2016 | PEDOT:PSS | 0 | (PEI)2(MA)6Pb7I22 | one-step | spin | no | DMF | na | na | na | PCBM | LiF | 8.9 |
| Yin, X. et al., ACS Nano 10, 3630–3636 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 16.5 |
| Yin, X. et al., ACS Nano 10, 3630–3636 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 13.4 |
| Yin, X. et al., J. Power Sources 329, 398–405 (2016) | 2016 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | PCBM | no | 16.7 |
| Yusoff, A. R. bin M. et al., ChemSusChem, 9, 1736–1742 (2016) | 2016 | DNA-CTMA | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | no | 16.2 |
| Yusoff, A. R. bin M. et al., ChemSusChem, 9, 1736–1742 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | no | 12.5 |
| Mohd Yusoff, A. R. bin et al., Nanoscale 8, 6328–6334 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Zr(acac) | no | 12 |
| Mohd Yusoff, A. R. bin et al., Nanoscale 8, 6328–6334 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | Ru(acac) | no | 9.7 |
| Yu, Y. et al., RSC Adv. 6, 90248–90254 (2016) | 2016 | PEDOT:PSS | polyTPD | MASnI3 | one-step | CVD | no | na | na | na | glovebox | C60 | BCP | 1.7 |
| Yu, Y. et al., RSC Adv. 6, 90248–90254 (2016) | 2016 | PEDOT:PSS | 0 | MASnI3 | one-step | CVD | no | na | na | na | glovebox | C60 | BCP | 0.5 |
| Yu, W. et al., Nanoscale 8, 6173–6179 (2016) | 2016 | Cu2O | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | PCBM | no | 11 |
| Zhang, Y. et al., Org. Electron. physics, Mater. Appl. 30, 281–288 (2016) | 2016 | no | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | na | na | glovebox | PCBM | no | 12.5 |
| Zhang, Y. et al., Org. Electron. physics, Mater. Appl. 30, 281–288 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | na | na | glovebox | PCBM | no | 13.6 |
| Zhang, Y. et al., Nano Energy 20, 126–133 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | BCP | 9.3 |
| Zhang, F. et al., J. Mater. Chem. A 4, 3438–3445 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | sec-butyl alcohol | DMF+DMSO | 100 | 30 | glovebox | PCBM | no | 14.3 |
| Zhao, L. et al., Sol. Energy Mater. Sol. Cells, 157, 79–84 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 120 | glovebox | C60 | no | 13.9 |
| Zhao, L. et al., Sol. Energy Mater. Sol. Cells, 157, 79–84 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 120 | glovebox | C60 | no | 12.7 |
| Zhou, Z. et al., Sol. Energy 136, 210–216 (2016) | 2016 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF+HI | - | - | - | PCBM | Ca | 19.1 |
| Akbulatov, A. F. et al., Adv. Energy Mater., 7, 1700476 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 100 | 15 | glovebox | PCBM | no | 10 |
| Akbulatov, A. F. et al., Adv. Energy Mater., 7, 1700476 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 100 | 15 | glovebox | PDI+EH | no | 10.3 |
| Baltakesmez, A. et al., J. Radiat. Res. Appl. Sci., 11, 124–129 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 90 | ambient | PCBM | no | 12.8 |
| Baltakesmez, A. et al., J. Radiat. Res. Appl. Sci., 11, 124–129 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 25 | ambient | PCBM | no | 9.9 |
| Brus, V. V. et al., Adv. Electron. Mater., 3, 1600438 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | no | 4.7 |
| Chai, G. et al., Mater. Des. 125, 222–229 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin-spray | no | DMF | - | - | - | PCBM | BCP | 13.4 |
| Chai, G. et al., Mater. Des. 125, 222–229 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xBrx | two-step | spin-spray | no | DMF | - | - | - | PCBM | BCP | 13.4 |
| Chen, Q. et al., Nano Lett. 17, 3231–3237 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL+Ag | 100 | 10 | na | PCBM | TiOx | 18.4 |
| Chen, Q. et al., Nano Lett. 17, 3231–3237 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | TiOx | 16 |
| Chen, Q. et al., Nano Lett. 17, 3231–3237 (2017) | 2017 | NiOx | 0 | MAPbI3-xClx | one-step | spin | toluene | DMSO+GBL | 85 | 120 | na | PCBM | TiOx | 11.2 |
| Chen, Q. et al., Nano Lett. 17, 3231–3237 (2017) | 2017 | NiOx | 0 | MAPbI3-xClx | one-step | spin | toluene | DMSO+GBL+Ag | 85 | 120 | na | PCBM | TiOx | 15.4 |
| Chen, W. et al., J. Phys. Chem. Lett. 8, 591–598 (2017) | 2017 | PEDOT:PSS | BPQDs | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | PCBM | ZrAcAc | 16.7 |
| Chen, W. et al., J. Phys. Chem. Lett. 8, 591–598 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 10 | glovebox | PCBM | ZrAcAc | 14.1 |
| Chen, S. et al., J. Power Sources 353, 123–130 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 20 | na | CoSe+PCBM | no | 14.9 |
| Chen, S. et al., J. Power Sources 353, 123–130 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 20 | na | PCBM | no | 11.4 |
| Chen, Q. et al., Dye. Pigment., 147, 113–119 (2017) | 2017 | TTA | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | PCBM+C60 | BCP | 16.7 |
| Chen, Q. et al., Dye. Pigment., 147, 113–119 (2017) | 2017 | no | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | PCBM+C60 | BCP | 11.6 |
| Chen, Z. et al., Nat. Commun., 8, 1890 (2017) | 2017 | PTAA | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 60 | na | PCBM+C60 | BCP | 17.8 |
| Chen, Z. et al., Nat. Commun., 8, 1890 (2017) | 2017 | PTAA | 0 | MAPbI3 | one-step | spin | no | GBL | 100 | 60 | na | PCBM+C60 | BCP | 16.1 |
| Chiang, Y.-H. et al., J. Mater. Chem. A, 5, 25485–25493 (2017) | 2017 | NiOx | mNiOx-Li | CsI, FAI, MABr, PbBr2, and PbI2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | C60 | no | 14 |
| Chiang, Y.-H. et al., J. Mater. Chem. A, 5, 25485–25493 (2017) | 2017 | NiOx | mNiOx-Li | CsI, FAI, MABr, PbBr2, and PbI2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | IZO | no | 16.2 |
| Chiang, Y.-H. et al., J. Mater. Chem. A, 5, 25485–25493 (2017) | 2017 | NiOx | mNiOx-Li | CsI, FAI, MABr, PbBr2, and PbI2 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 60 | na | ZnO | no | 12 |
| Chung, C.-C. et al., J. Mater. Chem. A 5, 13957–13965 (2017) | 2017 | GO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | MS | na | na | PCBM | no | 12.3 |
| Chung, C.-C. et al., J. Mater. Chem. A 5, 13957–13965 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF | MS | na | na | PCBM | no | 12.6 |
| Chung, C.-C. et al., J. Mater. Chem. A 5, 13957–13965 (2017) | 2017 | GO | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+GO | MS | na | na | PCBM | no | 15.2 |
| Chung, C.-C. et al., J. Mater. Chem. A 5, 13957–13965 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+GO | MS | na | na | PCBM | no | 14 |
| Dai, S.-M. et al., Inorganica Chim. Acta 468, 146–151 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | BDNC | no | 7.4 |
| Dai, S.-M. et al., Inorganica Chim. Acta 468, 146–151 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | EDNC | no | 12.6 |
| Dai, S.-M. et al., Inorganica Chim. Acta 468, 146–151 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | PCBM | no | 15 |
| Fu, G. et al., Sol. Energy Mater. Sol. Cells 165, 36–44 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DIO | na | na | na | PCBM | TIPD | 19.1 |
| Fujihara, T. et al., J. Mater. Chem. C 5, 1121–1127 (2017) | 2017 | PEDOT:PSS | 0 | MASnI3 | one-step | spin | toluene | DMF | 100 | 5 | glovebox | C60 | BCP | 2.5 |
| Ge, J. et al., J. Mater. Chem. A 5, 2920–2928 (2017) | 2017 | no | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | PCBM | no | 3.5 |
| Ge, J. et al., J. Mater. Chem. A 5, 2920–2928 (2017) | 2017 | Cu2BaSnS4 | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | PCBM | no | 14.9 |
| Ge, J. et al., J. Mater. Chem. A 5, 2920–2928 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+DMSO | MS | na | glovebox | PCBM | no | 8.5 |
| He, M. et al., Nat. Commun. 8, 16045 (2017) | 2017 | PTAA-Li:TBP | 0 | FA0.85MA0.15PbI2.55Br0.45 | one-step | MASP | no | DMSO | na | na | na | PCBM | BCP | 19.5 |
| He, M. et al., Nat. Commun. 8, 16045 (2017) | 2017 | PTAA-Li:TBP | 0 | FA0.85MA0.15PbI2.55Br0.45 | one-step | spin 2-3 | no | DMSO | 150 | 20 | na | PCBM | BCP | 17 |
| Heo, J. H. et al., J. Mater. Chem. A, 5, 20615–20622 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+HI | 100 | 2 | na | NDI+PM | no | 18.4 |
| Heo, J. H. et al., J. Mater. Chem. A, 5, 20615–20622 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+HI | 100 | 2 | na | PCBM | no | 18.9 |
| Heo, J. H. et al., J. Mater. Chem. A, 5, 20615–20622 (2017) | 2017 | PEDOT:PSS | 0 | FAPbI3-xBr | two-step | spin | no | DMF+DMSO | - | - | - | NDI+PM | no | 19.6 |
| Heo, J. H. et al., J. Mater. Chem. A, 5, 20615–20622 (2017) | 2017 | PEDOT:PSS | 0 | FAPbI3-xBr | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | no | 20 |
| Heo, J. H. et al., J. Mater. Chem. A, 5, 21146–21152 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+HI | 100 | 2 | ambient | PCBM | no | 15.8 |
| Hong, S. C. et al., ACS Appl. Mater. Interfaces 9, 7879–7884 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | electrospray | no | DMSO | 100 | 5 | na | C60 | BCP | 13.3 |
| Hu, Z. et al., Org. Electron. physics, Mater. Appl., 45, 97–103 (2017) | 2017 | NiOx | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | na | na | na | PCBM | no | 14.4 |
| Hu, Z. et al., Org. Electron. physics, Mater. Appl., 45, 97–103 (2017) | 2017 | NiOx | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | na | na | na | PCBM | no | 9.5 |
| Islam, M. B. et al., ACS Omega 2, 2291–2299 (2017) | 2017 | NiOx | 0 | MAPbI3-xClx | two-step | spin | no | na | - | - | - | PCBM | AZO | 15.2 |
| Jošt, M. et al., ACS Photonics 4, 1232–1239 (2017) | 2017 | PTAA | 0 | MAPbI3 | one-step | spin | no | DMF+HPA | 80 | 5 | glovebox | PCBM | BCP | 16.3 |
| Kakavelakis, G. et al., Adv. Energy Mater. 7, 1602120 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 40 | glovebox | PCBM | PFN | 12.9 |
| Kakavelakis, G. et al., Adv. Energy Mater. 7, 1602120 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 75 | glovebox | PCBM | PFN | 12.3 |
| Kakavelakis, G. et al., Adv. Energy Mater. 7, 1602120 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 40 | glovebox | PCBM-Rgo | PFN | 14.5 |
| Kakavelakis, G. et al., Adv. Energy Mater. 7, 1602120 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 75 | glovebox | PCBM-Rgo | PFN | 13.5 |
| Karuppuswamy, P. et al., Sol. Energy Mater. Sol. Cells 169, 78–85 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xBrx | two-step | spin | no | DMSO | - | - | - | PCBM+C60 | BCP | 10 |
| Karuppuswamy, P. et al., Sol. Energy Mater. Sol. Cells 169, 78–85 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xBrx | two-step | spin | no | DMSO | - | - | - | PDI+C60 | BCP | 11 |
| Kim, H.-S. et al., ACS Omega 2, 9074–9079 (2017) | 2017 | NiOx-Cs | 0 | FAPbI3, MAPbBr3, CsI | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 50 | glovebox | PCBM | BCP | 17.2 |
| Kim, H.-S. et al., ACS Omega 2, 9074–9079 (2017) | 2017 | NiOx | 0 | FAPbI3, MAPbBr3, CsI | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 50 | glovebox | PCBM | BCP | 15.3 |
| Kim, G. H. et al., Nano Lett., 17, 6385–6390 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | PCBM | EFGnPs-F | 14.3 |
| Kim, G. H. et al., Nano Lett., 17, 6385–6390 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 10 | na | PCBM | no | 14.7 |
| Liao, H. C. et al., Adv. Energy Mater., 7, 1601660 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin | no | na | na | na | glovebox | PCBM | no | 15.5 |
| Liao, H. C. et al., Adv. Energy Mater., 7, 1601660 (2017) | 2017 | NiOx | 0 | MAPbI3-xClx | one-step | spin | no | na | na | na | glovebox | PCBM | no | 18.2 |
| Lin, Q. et al., Interfaces, 9, 9096–9101 (2017) | 2017 | no | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 5 | glovebox | PCBM | no | 5.4 |
| Lin, Q. et al., Interfaces, 9, 9096–9101 (2017) | 2017 | 1 | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 5 | glovebox | PCBM | no | 16.5 |
| Lin, W. K. et al., Vaccum 140, 82–88 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | no | no | 0.7 |
| Lin, W. K. et al., Vaccum 140, 82–88 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | no | 2.1 |
| Lin, W. K. et al., Vaccum 140, 82–88 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | methylbenzene | DMF | - | - | - | PCBM | no | 4.7 |
| Lin, W. K. et al., Vaccum 140, 82–88 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | two-step | spin | methylbenzene | DMF | - | - | - | PCBM | no | 7.8 |
| Lin, Y. et al., Adv. Mater., 29, 1700607 (2017) | 2017 | PTAA | 0 | (FA0.83MA0.17)0.95Cs0.05Pb(I0.6Br0.4)3 | one-step | spin 2-3 | toluene | DMF+DMSO | MS | na | glovebox | ICBA+tran3+C60 | BCP | 18.3 |
| Liu, T. et al., Sol. Energy Mater. Sol. Cells 171, 43–49 (2017) | 2017 | F4-TCNQ-PTAA | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 20 | na | PCBM | no | 11 |
| Liu, T. et al., Sol. Energy Mater. Sol. Cells 171, 43–49 (2017) | 2017 | F4-TCNQ-PTAA | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 20 | na | PCBM | no | 5.3 |
| Liu, C. et al., Nanoscale, 9, 13967–13975 (2017) | 2017 | PEDOT:PSS | 0 | MAPb0.75Sn0.25I3 | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | BCP | 12.9 |
| Liu, C. et al., Nanoscale, 9, 13967–13975 (2017) | 2017 | PEDOT:PSS | 0 | MAPb0.75Sn0.25I3 | two-step | spin | no | DMF+DMSO+C60 | - | - | - | PCBM | BCP | 13.9 |
| Liu, D. et al., J. Mater. Chem. A 5, 5701–5708 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | BCP | 13.3 |
| Liu, D. et al., J. Mater. Chem. A 5, 5701–5708 (2017) | 2017 | PEDOT:PSS-F4-TCNQ | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | BCP | 17.2 |
| Liu, H. et al., Org. Electron. physics, Mater. Appl. 47, 220–227 (2017) | 2017 | PEDOT:PSS | PSSNa | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 70 | glovebox | PCBM | no | 12.3 |
| Liu, H. et al., Org. Electron. physics, Mater. Appl. 47, 220–227 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 95 | 70 | glovebox | PCBM | no | 7.9 |
| Liu, J. et al., ChemPhysChem 18, 617–625 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | glovebox | PCBM | BCP | 14.2 |
| Liu, J. et al., ChemPhysChem 18, 617–625 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | glovebox | PCBM+C60 | no | 8.3 |
| Liu, J. et al., ChemPhysChem 18, 617–625 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | glovebox | BCP | no | 5.1 |
| Liu, J. et al., ChemPhysChem 18, 617–625 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | glovebox | C60 | no | 13.3 |
| Liu, J. et al., ChemPhysChem 18, 617–625 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 10 | glovebox | PCBM | no | 10.2 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | V2O5 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 13.3 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | MoO3 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 12.2 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | GeO2 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 12.1 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | CrO3 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 10.2 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 14.1 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | PEDOT:PSS-V2O5 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 18 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | PEDOT:PSS-GeO2 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 16.2 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | PEDOT:PSS-MoO3 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 15.7 |
| Lou, Y.-H. and Wang, Z.-K., Nanoscale, 9, 13506–13514 (2017) | 2017 | PEDOT:PSS-CrO3 | 0 | MAPbI3-xClx | na | na | no | na | na | na | glovebox | PCBM | no | 14.5 |
| Luo, D. et al., Adv. Mater. 29, 1604758 (2017) | 2017 | PTAA-F4-TCNQ | 0 | MA0.6FA0.4PbI3 | one-step | spin | no | DMF | 140 | 10 | glovebox | PCBM+C60 | BCP | 20.2 |
| Mamun, A. et al., Phys. Chem. Chem. Phys. 19, 17960–17966 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | ambient | PCBM | no | 10.6 |
| Mamun, A. et al., Phys. Chem. Chem. Phys. 19, 17960–17966 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | ambient | PCBM | carbon | 16.2 |
| Mamun, A. et al., Phys. Chem. Chem. Phys. 19, 17960–17966 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | ambient | PCBM+C60 | no | 14 |
| Mamun, A. Al et al., Phys. Chem. Chem. Phys., 19, 19487–19495 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | na | na | ambient | PCBM | carbon | 16.2 |
| Niu, J. et al., Org. Electron. physics, Mater. Appl. 48, 165–171 (2017) | 2017 | PEDOT:PSS | 0 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 150 | 6 | glovebox | PCBM | BCP | 12 |
| Niu, J. et al., Org. Electron. physics, Mater. Appl. 48, 165–171 (2017) | 2017 | PEDOT:PSS-GO | 0 | (FAPbI3)0.85(MAPbBr3)0.15 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 150 | 6 | glovebox | PCBM | BCP | 14.2 |
| Savva, A. et al., J. Mater. Chem. A, 5, 20381–20389 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 5 | glovebox | PCBM | AZO | 15.3 |
| Savva, A. et al., J. Mater. Chem. A, 5, 20381–20389 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 80 | 5 | glovebox | PCBM | AZO | 10.6 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMF | 100 | 10 | glovebox | PCBM | BCP | 5.1 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMF+DMSO | 100 | 10 | glovebox | PCBM | BCP | 15.1 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO | 100 | 10 | glovebox | PCBM | BCP | 12.5 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | glovebox | PCBM | BCP | 9.5 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+NMP | 100 | 10 | glovebox | PCBM | BCP | 11.1 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | GBL | 100 | 10 | glovebox | PCBM | BCP | 3.6 |
| Seo, Y. H. et al., Appl. Mater. Today, 9, 598–604 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | NMP | 100 | 10 | glovebox | PCBM | BCP | 10.5 |
| Sun, W. et al., Org. Electron. physics, Mater. Appl. 46, 22–27 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMF | 80 | 10 | glovebox | C60 | BCP | 14.4 |
| Sun, W. et al., Org. Electron. physics, Mater. Appl. 46, 22–27 (2017) | 2017 | PEDOT:PSS-ammonia | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMF | 80 | 10 | glovebox | C60 | BCP | 15.5 |
| Tombe, S. et al., J. Mater. Chem. C 5, 1714–1723 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF | na | na | na | PCBM | no | 9.2 |
| Tombe, S. et al., J. Mater. Chem. C 5, 1714–1723 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xBrx | one-step | spin 2-3 | no | DMF | na | na | na | PCBM | no | 5.4 |
| Tombe, S. et al., J. Mater. Chem. C 5, 1714–1723 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | no | DMF | na | na | na | PCBM | no | 12.5 |
| Vaagensmith, B. et al., ACS Appl. Mater. Interfaces 9, 35861–35870 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 12.4 |
| Wang, K. et al., ACS Omega, 2, 6250–6258 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 15 | glovebox | PCBM | BCP | 15.3 |
| Wang, K. et al., ACS Omega, 2, 6250–6258 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMSO+GBL | 100 | 15 | glovebox | PCBM | no | 15.2 |
| Wang, K. et al., ACS Omega, 2, 6250–6258 (2017) | 2017 | PEDOT:PSS | 0 | MA0.7FA0.3PbI3-x Clx | one-step | spin | toluene | DMSO+GBL | 100 | 15 | glovebox | PCBM | BCP | 18 |
| Wang, N. et al., Adv. Energy Mater. 7, 1700522 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 100 | 5 | glovebox | HATNT | LiF | 18.1 |
| Wang, N. et al., Adv. Energy Mater. 7, 1700522 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF | 100 | 5 | glovebox | PCBM | LiF | 16.6 |
| Wang, C. et al., RSC Adv. 7, 29944–29952 (2017) | 2017 | PEDOT:PSS | rub | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 30 | glovebox | PCBM | BCP | 14.4 |
| Wang, C. et al., RSC Adv. 7, 29944–29952 (2017) | 2017 | rub | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 30 | glovebox | PCBM | BCP | 14.3 |
| Wang, C. et al., RSC Adv. 7, 29944–29952 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMSO+GBL | 100 | 30 | glovebox | PCBM | BCP | 12.7 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | TS–CuPc | 0 | MAPbI3 | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 12.1 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 5.7 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | PEDOT:PSS-TS–CuPc | 0 | MAPbI3 | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 14.1 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | TS–CuPc | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 6.3 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 13.3 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | PEDOT:PSS-TS–CuPc | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 17.3 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | TS–CuPc | 0 | (NH2CH=NH2PbI3)0.83(MAPbBr3)0.17 | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 13.1 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | PEDOT:PSS | 0 | (NH2CH=NH2PbI3)0.83(MAPbBr3)0.17 | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 6.1 |
| Wang, J. M. et al., ACS Appl. Mater. Interfaces, 9, 13240–13246 (2017) | 2017 | PEDOT:PSS-TS–CuPc | 0 | (NH2CH=NH2PbI3)0.83(MAPbBr3)0.17 | one-step | spin | no | DMF | MS | na | glovebox | PCBM | no | 15.4 |
| Wei, J. et al., Adv. Energy Mater., 7, 1700492 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | MS | 50 | glovebox | PCBM | no | 16.6 |
| Wu, H. et al., Org. Electron. physics, Mater. Appl. 45, 302–307 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | doctor-blade | no | DMF | na | na | na | PCBM | no | 11.3 |
| Wu, T. et al., ACS Nano, 11, 11542–11549 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | PEI | 12.4 |
| Wu, T. et al., ACS Nano, 11, 11542–11549 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 10 | na | PCBM | PEI | 18.2 |
| Wu, T. et al., ACS Nano, 11, 11542–11549 (2017) | 2017 | PEDOT:PSS | 0 | Cs-FAPbI3 | one-step | spin | toluene | DMF+DMSO | 150 | 10 | na | PCBM | PEI | 14.3 |
| Xi, Q. et al., Nanoscale 9, 6136–6144 (2017) | 2017 | CuSCN | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | C60 | Bphen | 11.4 |
| Xia, Y. et al., J. Mater. Chem. A 5, 3193–3202 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 1 | glovebox | PCBM | FPI-PEIE | 18.1 |
| Xia, Y. et al., J. Mater. Chem. A 5, 3193–3202 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 1 | glovebox | PCBM | FPI-PEIE | 14.6 |
| Xia, Y. et al., J. Mater. Chem. A 5, 3193–3202 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+H2O | 100 | 1 | glovebox | PCBM | FPI-PEIE | 10.8 |
| Xu, X. et al., J. Power Sources 360, 157–165 (2017) | 2017 | polyTPD | 0 | MAPbI3 | one-step | spin | toluene | DMF+DMSO | 100 | 10 | na | C60 | BCP | 18.2 |
| Xu, X. et al., J. Power Sources 360, 157–165 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | toluene | DMF+DMSO | 100 | 10 | na | C60 | BCP | 12.9 |
| Xue, Q. et al., Adv. Energy Mater. 7, 1602333 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 15 | glovebox | C60(CH2) | no | 18.1 |
| Xue, Q. et al., Adv. Energy Mater. 7, 1602333 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | toluene | DMSO+GBL | 100 | 15 | glovebox | PCBM | no | 16.2 |
| Yang, Y. et al., Sci. Rep. 7, 46724 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 100 | glovebox | PCBM | no | 14.4 |
| Yang, Y. et al., Sci. Rep. 7, 46724 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 30 | glovebox | PCBM | no | 12.1 |
| Yao, K. et al., Nano Energy, 40, 155–162 (2017) | 2017 | NiOx-Cu | mNiOx-Cu | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | PCBM+C60 | no | 19.8 |
| Yao, K. et al., Nano Energy, 40, 155–162 (2017) | 2017 | NiOx | mNiOx-Cu | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | PCBM+C60 | no | 18.6 |
| Yao, K. et al., Nano Energy, 40, 155–162 (2017) | 2017 | NiOx | mNiOx | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | PCBM+C60 | no | 17 |
| Yao, K. et al., Nano Energy, 40, 155–162 (2017) | 2017 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | PCBM+C60 | no | 15.6 |
| Yao, K. et al., Nano Energy, 40, 155–162 (2017) | 2017 | NiOx-Cu | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 100 | 10 | na | PCBM+C60 | no | 17 |
| Yao, X. et al., Org. Electron. physics, Mater. Appl. 47, 85–93 (2017) | 2017 | Vox | APPA | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | BCP | 14 |
| Yao, X. et al., Org. Electron. physics, Mater. Appl. 47, 85–93 (2017) | 2017 | PEDOT:PSS | APPA | MAPbI3 | two-step | spin | no | DMF | - | - | - | PCBM | BCP | 13.3 |
| Yoon, J. et al., Energy Environ. Sci. 10, 337–345 (2017) | 2017 | PEDOT:PSS-F4-TCNQ | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | ambient | C60 | BCP/LiF | 17.3 |
| Yu, W. et al., J. Power Sources 358, 29–38 (2017) | 2017 | PEDOT:SAF | 0 | MAPbI3-xClx | one-step | spin | no | DMSO+GBL | 100 | 20 | glovebox | PCBM | BCP | 14.1 |
| Yu, W. et al., J. Power Sources 358, 29–38 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMSO+GBL | 100 | 20 | glovebox | PCBM | BCP | 13.3 |
| Zhang, H. et al., Adv. Mater. 29, 1604695 (2017) | 2017 | NiOx | 0 | MAPbI3 | two-step | spin-dip | no | DMF | - | - | - | C60 | no | 17.1 |
| Zhao, D. et al., Nat. Energy 2, 17018 (2017) | 2017 | PEDOT:PSS | 0 | (FASnI3)0.6(MAPbI3)0.4 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 7 | glovebox | C60 | BCP | 17.5 |
| Zhao, J. et al., Adv. Energy Mater., 7, 1602599 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 90 | glovebox | PCBM | AZO | 11.8 |
| Zheng, X. et al., Nat. Energy, 2, 17102 (2017) | 2017 | PTAA | 0 | FA0.83MA0.17Pb(I0.83Br0.17)3 | one-step | spin 2-3 | no | DMF+DMSO | MS | na | na | choline chloride+C60 | BCP | 21 |
| Zheng, X. et al., Nat. Energy, 2, 17102 (2017) | 2017 | PTAA | 0 | MAPbI3 | two-step | spin | no | DMF | - | - | - | choline chloride+C60 | BCP | 20 |
| Zheng, X. et al., Nat. Energy, 2, 17102 (2017) | 2017 | PTAA | 0 | FAxMA1-xPb(Br1-xIx)3 | two-step | spin | no | DMF | - | - | - | choline chloride+C60 | BCP | 20.2 |
| Zheng, X. et al., Nat. Energy, 2, 17102 (2017) | 2017 | PTAA | 0 | FAxMA1-xPb(Br1-xIx)3 | two-step | spin | no | DMF | - | - | - | PCBM+C60 | BCP | 18.7 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS | 0 | MAPbBr3 | one-step | spin 2-3 | toluene | DMF | 100 | 2 | glovebox | PCBM | no | 4.7 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS-Na | 0 | MAPbBr3 | one-step | spin 2-3 | toluene | DMF | 100 | 2 | glovebox | PCBM | no | 4.8 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS-Na | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF | 100 | 30 | glovebox | PCBM | no | 15.6 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin 2-3 | no | DMF | 100 | 30 | glovebox | PCBM | no | 12.4 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS | 0 | MAPbI2Br | one-step | spin 2-3 | no | DMF+NH4Cl | 100 | 30 | glovebox | PCBM | no | 10.2 |
| Zuo, C. and Ding, L., Adv. Energy Mater. 7, 1601193 (2017) | 2017 | PEDOT:PSS-Na | 0 | MAPbI2Br | one-step | spin 2-3 | no | DMF+NH4Cl | 100 | 30 | glovebox | PCBM | no | 11.6 |
| Alsari, M. et al., Sci. Rep., 8, 5977 (2018) | 2018 | PEDOT:PSS | polyTPD | MAPbI3 | one-step | spin | no | DMF+HPA | 100 | 5 | glovebox | PCBM | BCP | 15.4 |
| Alsari, M. et al., Sci. Rep., 8, 5977 (2018) | 2018 | PEDOT:PSS | polyTPD | MAPbI3-xClx | one-step | spin | no | DMF | 100 | 90 | glovebox | PCBM | BCP | 12 |
| Alsari, M. et al., Sci. Rep., 8, 5977 (2018) | 2018 | PEDOT:PSS | polyTPD | FA0.83Cs0.17Pb(I0.8Br0.2)3 | one-step | spin 2-3 | anisole | DMF+DMSO | 100 | 60 | glovebox | PCBM | BCP | 18.5 |
| Chang, C.-Y. et al., J. Mater. Chem. A, 6, 4179–4188 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 3 | glovebox | PCBM | PEI | 14.1 |
| Chang, C.-Y. et al., J. Mater. Chem. A, 6, 4179–4188 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+3F+PC61BM | 100 | 3 | glovebox | PCBM | PEI | 16.2 |
| Chang, C.-Y. et al., J. Mater. Chem. A, 6, 4179–4188 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | no | DMF+5F+PC61BM | 100 | 3 | glovebox | PCBM | PEI | 12.4 |
| Chen, W. et al., Org. Electron., 58, 283–289 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | toluene | DMSO+GBL+ASCl | 100 | 20 | glovebox | PCBM | no | 14.5 |
| Chen, W. et al., Org. Electron., 58, 283–289 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | toluene | DMSO+GBL | 100 | 20 | glovebox | PCBM | no | 14.9 |
| Thrithamarassery Gangadharan, D. et al., Sol. RRL 2, 1700215 (2018) | 2018 | PEDOT:PSS | 0 | (PEA)2(MA)3Pb4I13 | one-step | spin | no | DMF | na | na | glovebox | PCBM | no | 5.5 |
| Thrithamarassery Gangadharan, D. et al., Sol. RRL 2, 1700215 (2018) | 2018 | PEDOT:PSS | 0 | (PEA)2(MA)3Pb4I13 | one-step | spin | toluene | DMF | 100 | 20 | glovebox | PCBM | no | 3.9 |
| Han, C. et al., J. Mater. Chem. C (2018). doi:10.1039/C8TC01033A | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene-ITIC | DMSO+GBL | 100 | 5 | na | PCBM | PEI | 17.2 |
| Han, C. et al., J. Mater. Chem. C (2018). doi:10.1039/C8TC01033A | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL+ITIC | 100 | 5 | na | PCBM | PEI | 16.3 |
| Han, C. et al., J. Mater. Chem. C (2018). doi:10.1039/C8TC01033A | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 5 | na | PCBM | PEI | 17.9 |
| Heo, J. H. et al., J. Mater. Chem. A, 6, 8251–8258 (2018) | 2018 | PEDOT:PSS | 0 | FAPbI3-xBrx | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | no | 18.9 |
| Heo, J. H. et al., J. Mater. Chem. A, 6, 8251–8258 (2018) | 2018 | PEDOT:PSS | 0 | FAPbI3-xBrx | two-step | spin | no | DMF+DMSO | - | - | - | PCBM | no | 13.8 |
| Hsu, K. C. et al., Org. Electron. physics, Mater. Appl., 57, 221–225 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3 | one-step | electrospray | no | DMF | na | na | na | C60 | BCP | 0.9 |
| Hsu, K. C. et al., Org. Electron. physics, Mater. Appl., 57, 221–225 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | electrospray | no | DMF | na | na | na | C60 | BCP | 8.1 |
| Hsu, K. C. et al., Org. Electron. physics, Mater. Appl., 57, 221–225 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3 | two-step | vasp | no | DMF | - | - | - | C60 | BCP | 10.7 |
| Ito, N. et al., J. Phys. Chem. Lett., 9, 1682–1688 (2018) | 2018 | PEDOT:PSS | 0 | FA0.75MA0.25Sn0.95Ge0.05I3 | one-step | spin | toluene | DMF+DMSO | 70 | 10 | na | C60 | BCP | 6.9 |
| Ito, N. et al., J. Phys. Chem. Lett., 9, 1682–1688 (2018) | 2018 | PEDOT:PSS | 0 | FA0.75MA0.25SnI3 | one-step | spin | toluene | DMF+DMSO | 70 | 10 | na | C60 | BCP | 3.6 |
| Kang, J. S. et al., Advanced Energy Materials 8, 1703114 (2018) | 2018 | CoN | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | C60 | BCP | 15 |
| Kang, J. S. et al., Advanced Energy Materials 8, 1703114 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | MS | na | na | C60 | BCP | 16.8 |
| Lee, H. et al., Sci. Rep. 8, 5590 (2018) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMF+DMSO | 100 | 30 | na | PCBM | BCP | 10.1 |
| Li, J. et al., Nano Energy, 46, 331–337 (2018) | 2018 | P3CT-K | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | PCBM | ZnO | 16.6 |
| Li, J. et al., Nano Energy, 46, 331–337 (2018) | 2018 | P3CT-K | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | MS | na | glovebox | PCBM-GD | ZnO-GD | 20 |
| Li, W. et al., Energy Environ. Sci., 11, 286–293 (2018) | 2018 | NiOx | 0 | CsxFA1-xPbI3–[GaAA3]4 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 30 | dry air | PCBM | BCP | 18.2 |
| Li, W. et al., Energy Environ. Sci., 11, 286–293 (2018) | 2018 | NiOx | 0 | CsxFA1-xPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 30 | dry air | PCBM | BCP | 15.8 |
| Liu, C. et al., J. Am. Chem. Soc., 140, 3825–3828 (2018) | 2018 | NiOx | 0 | CsPbI2Br | one-step | spin 2-3 | no | DMSO | MS | na | na | ZnO-C60 | no | 13.3 |
| Liu, C. et al., J. Am. Chem. Soc., 140, 3825–3828 (2018) | 2018 | NiOx | 0 | CsPbI2Br | one-step | spin 2-3 | no | DMSO | MS | na | na | C60 | no | 10.3 |
| Liu, C. et al., J. Am. Chem. Soc., 140, 3825–3828 (2018) | 2018 | NiOx | 0 | CsPbI2Br | one-step | spin 2-3 | no | DMSO | MS | na | na | ZnO | no | 9.3 |
| Liu, D. et al., Adv. Sci., 5, 1700484 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DMSO | 80 | 10 | glovebox | C60 | BCP | 19.1 |
| Liu, D. et al., Adv. Sci., 5, 1700484 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xClx | one-step | spin | no | DMF+DMSO+H2O | 80 | 10 | glovebox | C60 | BCP | 20.1 |
| Niu, G. et al., J. Mater. Chem. A , 6, 4721–4728 (2018) | 2018 | NiMgLiO | 0 | MAPbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 90 | 10 | na | PCBM | BCP | 17.6 |
| Niu, G. et al., J. Mater. Chem. A , 6, 4721–4728 (2018) | 2018 | NiMgLiO | 0 | Cs0.05FA0.15MA0.8PbI3 | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 90 | 10 | na | PCBM | BCP | 19.2 |
| Sha, W. E. I. et al., Adv. Energy Mater., 8, 1701586 (2017) | 2018 | NiOx | 0 | MAPbI3-xClx | one-step | spin | chlorobenzene | DMF | 100 | 10 | glovebox | PCBM+C60 | no | 19.4 |
| Shao, S. et al., Adv. Energy Mater., 8, 1702019 (2018) | 2018 | PEDOT:PSS | 0 | PEA2FAn-1SnnI3n+1 | one-step | spin | diethyl ether | DMF+DMSO | 65 | 20 | glovebox | C60 | BCP | 9 |
| Shao, S. et al., Adv. Energy Mater., 8, 1702019 (2018) | 2018 | PEDOT:PSS | 0 | FASnI3 | one-step | spin | diethyl ether | DMF+DMSO | 65 | 20 | glovebox | C60 | BCP | 6 |
| Wu, W.-Q. et al., Nat. Commun., 9, 1625 (2018) | 2018 | no | 0 | MAPbI3 | one-step | spin | no | DMF+F4TCNQ | 100 | 30 | glovebox | C60 | BCP | 20.2 |
| Wu, W.-Q. et al., Nat. Commun., 9, 1625 (2018) | 2018 | no | 0 | MAPbI3 | one-step | spin | no | DMF | 100 | 30 | glovebox | C60 | BCP | 11 |
| Yoon, Y. et al., Nano Energy, 48, 543–550 (2018) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 130 | 10 | na | PCBM | no | 14.8 |
| Yoon, Y. et al., Nano Energy, 48, 543–550 (2018) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin | diethyl ether | DMF+DMSO | 100 | 10 | na | PCBM | no | 17 |
| Yu, J. C. et al., Sci. Rep. 8, 1070 (2018) | 2018 | PEDOT:GO | 0 | MAPbI3-xBrx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 20 | glovebox | PCBM | ZnO | 18.1 |
| Yu, J. C. et al., Sci. Rep. 8, 1070 (2018) | 2018 | PEDOT:PSS | 0 | MAPbI3-xBrx | one-step | spin 2-3 | chlorobenzene | DMSO+GBL | 100 | 20 | glovebox | PCBM | ZnO | 15 |
| Zhang, J. et al., Adv. Energy Mater., 8, 1701981 (2017) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO+LiI | 95 | na | na | PCBM | no | 16 |
| Zhang, J. et al., Adv. Energy Mater., 8, 1701981 (2017) | 2018 | NiOx | 0 | MAPbI3 | one-step | spin | chlorobenzene | DMF+DMSO | 95 | na | na | PCBM | no | 19.5 |

Table S11. Additional data to Cs based perovskites (Section 3.2)

| Article | Year | Perovskite | PCEbest (%) |
| --- | --- | --- | --- |
| Ma, Q. et al., Adv. Energy Mater. 6, 1502202 (2016) | 2016 | CsPbI3-xBrx | 4.7 |
| Chang, X. et al., ACS Appl. Mater. Interfaces 8, 33649–33655 (2016) | 2016 | CsPbBr3 | 3.9 |
| Zhou, S. et al., Adv. Mater. 29, 1703682 (2017) | 2017 | CsPbBr3 | 8.3 |
| Lau, C. F. J. et al., ACS Energy Lett. 2, 2319–2325 (2017) | 2017 | CsPbI3-xBrx | 7.7 |
| Nam, J. K. et al., Nano Lett. 17, 2028–2033 (2017) | 2017 | CsPbI3-xBrx | 8.2 |
| Frolova, L. A. et al., J. Phys. Chem. Lett. 8, 67–72 (2017) | 2017 | CsPbI3 | 10.5 |
| Yonezawa, K. et al., Jpn. J. Appl. Phys. 56, 04CS11 (2017) | 2017 | CsPbI3 | 5.7 |
| Wang, Y. et al., Sol. RRL 2, 1700180 (2017) | 2017 | CsPbI3-xBrx | 10.6 |

Table S12. Additional data to mixed cation perovskite combinations (Section 3.2)

| Article | Year | Mixed cation type | PCEbest (%) |
| --- | --- | --- | --- |
| Mei, A. et al., Science 345, 295–8 (2014) | 2014 | (5-AVA)x(MA)1-xPbI3 | 12.8 |
| Sheng, Y. et al., J. Mater. Chem. A 6, 2360–2364 (2018) | 2018 | (5-AVA)0.034MA0.966PbI2.95(BF4)0.05 | 15.5 |
| Li, F. R. et al., J. Mater. Chem. A 5, 10374–10379 (2017) | 2017 | (5-AVA)0.05(MA)0.95PbI3 | 11.3 |
| Xu, C. et al., J. Energy Chem. 27, 764–768 (2018) | 2018 | PEA-MA | 8.7 |
| Thrithamarassery Gangadharan, D. et al., Sol. RRL 2, 1700215 (2018) | 2018 | PEA-MA | 4.7 |
| Gan, X. et al., Sol. Energy Mater. Sol. Cells 162, 93–102 (2017) | 2017 | PEA-MA | 3.7 |
| Chen, J. et al., ACS Appl. Mater. Interfaces 9, 36338–36349 (2017) | 2017 | PEA-MA | 19.8 |
| Cohen, B. El et al., Sustain. Energy Fuels 1, 1935–1943 (2017) | 2017 | PEA-MA | 5.9 |
| Niemann, R. G. et al., J. Mater. Chem. A 4, 17819–17827 (2016) | 2016 | Cs-MA | 6.9 |
| Iagher, L. and Etgar, L., ACS Energy Lett. 3, 366–372 (2018) | 2018 | Cs-MA | 14.6 |
| Murugadoss, G. et al., Electrochim. Acta 257, 267–280 (2017) | 2017 | Cs-MA | 10.0 |

Table S13. Additional data to high temperature short-time annealed perovskite cells (Section 3.4)

| Article | Year | Annealing temperature (°C) | Annealing time (seconds) | PCEbest (%) |
| --- | --- | --- | --- | --- |
| Kim, M. et al., ACS Nano 11, 6057–6064 (2017) | 2017 | 100 | 1800 | 17.6 |
| Kim, M. et al., ACS Nano 11, 6057–6064 (2017) | 2017 | 200 | 60 | 18.5 |
| Kim, M. et al., ACS Nano 11, 6057–6064 (2017) | 2017 | 300 | 8 | 19.3 |
| Kim, M. et al., ACS Nano 11, 6057–6064 (2017) | 2017 | 400 | 4 | 20.8 |
| Cao, X. et al., J. Colloid Interface Sci. 524, 483–489 (2018) | 2018 | 100 | 1200 | 12.4 |
| Cao, X. et al., J. Colloid Interface Sci. 524, 483–489 (2018) | 2018 | 175 | 60 | 14.2 |
| Cao, X. et al., J. Colloid Interface Sci. 524, 483–489 (2018) | 2018 | 250 | 10 | 16.4 |
| Jeon, M. K. et al., Mol. Cryst. Liq. Cryst. 660, 79–84 (2018) | 2018 | 100 | 60 | 8.3 |
| Jeon, M. K. et al., Mol. Cryst. Liq. Cryst. 660, 79–84 (2018) | 2018 | 100 | 600 | 10.9 |
| Jeon, M. K. et al., Mol. Cryst. Liq. Cryst. 660, 79–84 (2018) | 2018 | 150 | 60 | 10.7 |
| Zuo, C. et al., Nano Energy 46, 185–192 (2018) | 2018 | 300 | 30 | 19.5 |

Table S14. Additional data to cells without ETL in regular structure (Section 3.5)

| Article | Year | ETL | PCEbest (%) |
| --- | --- | --- | --- |
| Wei, X. et al., Sol. RRL 2, 1700222 (2018) | 2018 | no | 12.6 |

Table S15. Additional data to inorganic HTLs (Section 3.6)

| Article | Year | HTL | PCEbest (%) |
| --- | --- | --- | --- |
| Gharibzadeh, S. et al., ChemSusChem 9, 1929–1937 (2016) | 2016 | CuI | 7.4 |
| Huckaba, A. J. et al., ChemistrySelect 1, 5316–5319 (2016) | 2016 | FeS2 | 11.2 |
| Jung, M. et al., ChemSusChem 9, 2592–2596 (2016) | 2016 | CuSCN | 18.0 |
| Koo, B. et al., Adv. Funct. Mater. 26, 5400–5407 (2016) | 2016 | FeS2 | 12.6 |
| Madhavan, V. E. et al., ACS Energy Lett. 1, 1112–1117 (2016) | 2016 | CuSCN | 16.6 |
| Paulo, S. et al., Synth. Met. 222, 17–22 (2016) | 2016 | carbon QDs | 3.0 |
| Pydzińska, K. et al., ChemSusChem 9, 1647–1659 (2016) | 2016 | CuSCN | 6.8 |
| Pydzińska, K. et al., ChemSusChem 9, 1647–1659 (2016) | 2016 | CuSCN | 5.7 |
| Cheng, M. et al., Adv. Energy Mater. 7, 1602556 (2017) | 2017 | V2O5 | 11.3 |
| Huang, A. et al., Langmuir 33, 3624–3634 (2017) | 2017 | Co1-yCuyOx | 10.0 |
| Im, K. et al., Chem. Eng. J. 330, 698–705 (2017) | 2017 | MoO2 | 15.7 |
| Im, K. et al., Chem. Eng. J. 330, 698–705 (2017) | 2017 | MoO2-Ti | 15.8 |
| Jin, X. et al., J. Mater. Chem. A 5, 19884–19891 (2017) | 2017 | Cu2−xGeS3 | 14.5 |
| Lei, H. et al., Sol. RRL 1, 1700038 (2017) | 2017 | CuxS | 18.5 |
| Li, X. et al., ACS Appl. Mater. Interfaces 9, 41354–41362 (2017) | 2017 | CuI | 17.6 |
| Sepalage, G. A. et al., Nano Energy 32, 310–319 (2017) | 2017 | CuSCN | 9.6 |
| Takahashi, K. & Suzuki, Y., Jpn. J. Appl. Phys. 56, 08MC04 (2017) | 2017 | CuI | 2.2 |
| Xu, L. et al., Nanoscale Res. Lett. 12, 159 (2017) | 2017 | CuIn0.1Ga0.9(S0.9Se0.1)2 | 9.2 |
| Yang, I. S. et al., Nano Energy 32, 414–421 (2017) | 2017 | CuSCN | 17.1 |
| Zhang, H. et al., Adv. Mater. 29, 1604984 (2017) | 2017 | CuGaO2 | 18.5 |

Table S16. Additional data to average of CuI (Section 3.6)

| Article | Year | HTL | PCEbest (%) |
| --- | --- | --- | --- |
| Nazari, P. et al., J. Phys. Chem. C 121, 21935–21944 (2017) | 2017 | CuI | 9.2 |
| Li, X. et al., ACS Appl. Mater. Interfaces 9, 41354–41362 (2017) | 2017 | CuI | 17.6 |
| Karuppuchamy, S. et al., J. Mater. Sci. Mater. Electron. 29, 8847–8853 (2018) | 2018 | CuI | 3.4 |

Table S17. Additional data to PEDOT:PSS-doped and PTAA-doped HTLs (Section 3.7)

| Article | Year | HTL | PCEbest (%) |
| --- | --- | --- | --- |
| Li, J. F. et al., Chinese Phys. B 25, 028402 (2015) | 2015 | PEDOT:PSS-glycerol | 11.4 |
| Sun, Z. et al., Org. Electron. physics, Mater. Appl. 52, 309–316 (2018) | 2018 | PEDOT:PSS-AuAg@AuAg core-shell alloy nanocrystals | 16.8 |
| Watson, B. L. et al., J. Mater. Chem. A 5, 19267–19279 (2017) | 2017 | PTAA-Li+TBP-TPBA | 17.7 |
| Luo, J. et al., Energy Environ. Sci. (2018). doi:10.1039/C8EE00036K | 2018 | PTAA-Li+TBP | 19.0 |
| Bi, C. et al., Nat. Commun. 6, 7747 (2015) | 2015 | PTAA-F4-TCNQ | 18.1 |

[1]	Q. Tai, P. You, H. Sang, Z. Liu, C. Hu, H. L. W. Chan, F. Yan, Nat. Commun. 2016, 7, 11105.

[2]	Y. H. Chiang, H. M. Cheng, M. H. Li, T. F. Guo,  P. Chen, ChemSusChem 2016, 9, 2620–2627.

[3]	W. Ke, C. Xiao, C. Wang, B. Saparov, H. S. Duan, D. Zhao, Z. Xiao, P. Schulz, S. P. Harvey, W. Liao, W. Meng, Y. Yu, A. J. Cimaroli, C. S. Jiang, K. Zhu, M. Al-Jassim, G. Fang, D. B. Mitzi, Y. Yan, Adv. Mater. 2016, 28, 5214.

[4]	M. K. Kim, T. Jeon, H. Il Park, J. M. Lee, S. A. Nam, S. O. Kim, CrystEngComm. 2016, 18, 6090.